## Slide 1: A Novel Approach to Predicting Upward Flame Spread over Polymers
Isaac T. Leventon
Stanislav I. Stoliarov

## Slide 2: The Fire Problem
Surface flame spread is a key determinant of early fire growth
Flame to surface heat feedback controls material burning rate
Widely used standards assessing material flammability show:
  Limited predictive capabilities outside of standard test conditions
  Conflicting assessments between tests
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
UL 94 Test Schematic

## Slide 3: Thermal Model of Upward Flame Spread
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Notes: Flame spread is known to be controlled by a positive feedback between coupled processes of solid degradation and gas phase combustion.
As gaseous degradation products react with the ambient oxidizer in a diffusion flame, a fraction of heat produced in this reaction is transferred back to the solid,
causing further degradation and production of flammable gases.
In vertical wall flames, this process has a potential for rapid growth because gasified fuel moves upward, driven by natural convection,
and burns downstream from where it is created, thus allowing for heat transfer to a region of the solid that is not yet degrading.

## Slide 4: Early Flame Spread Models
Early analytical models
Additional influences to consider
  Heat transfer mechanism
  Transient flame/material behaviors
  Temperature dependent material properties
  Sample thickness/width/aspect ratio
  Transition to turbulence
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Notes: Assumptions
constant flame height
single values of flame to surface heat flux to describe the heat feedback profile
simplified in-depth heat transfer
Simplified material degradation mechanisms
Assume, a priori, linear or exponential growth rate

## Slide 5: Early Flame Spread Models
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Computational Models
  Predict material response to a flame induced heat flux
How to describe this heat flux
  Flame height
  Heat feedback profile
    Steady state (peak) heat flux
    Form/shape, decay region
Notes: This image is from Hasemi, 1984 [Experimental Wall Flame Heat Transfer Correlations for the Analysis of Upward Wall Flame Spread]
A careful understanding of incident heat flux is required in any attempt at predicting material burning rate – Rhodes/Quintiere
Solid phase pyrolysis models have evolved from one-dimensional, steady-state formulations to two-dimensional, time-resolved solvers with multi-reaction degradation chemistry and temperature and composition resolved thermophysical properties[10], [11].
20-35 kW/m2 constant heat flux:
[9] J.L. Consalvi, Y. Pizzo, B. Porterie, Fire Saf. J.43 (2008) 351–362
[11] K. Tsai, J. Turnbull, G. Will, D. Drysdale, Fire Saf. Sci.7 (2002) 117–128

## Slide 6: Purpose of Study
Better resolve flame to surface heat feedback at the critical length scale
Predict flame to surface heat feedback solely as a function of
material burning rate
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Notes: I should be clear here. The development of this expression dates back almost two years and was presented at the 2011 Combustion Symposium.
In that work, a flame heat flux expression was developed based on highly spatially refined measurements of flame heat flux taken at 1 cm intervals from 2 to 15 cm above the base that was ignited to allow for upward flame spread
In this study, we have refined that expression with additional measurements taken on samples ignited by a new burner

## Slide 7: Purpose of Study
Couple empirical model of flame heat feedback with advanced pyrolysis model to simulate early stages of upward flame spread
Generalize model to describe the burning behavior of a range of materials through straightforward scaling
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work

## Slide 8: Test Apparatus
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work

## Slide 9: Test Apparatus
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Notes: A straightforward extension of the above methodology to provide height-resolved heat flux measurements is to canvass a sample with multiple heat flux gauges; however, such an approach, while efficient, has significant drawbacks. The most notable among them are potential distortions in the temperature and flow structure of the gaseous boundary layer and temperature of the burning material due to a contact with multiple thermostated elements. Therefore, in this work, height-resolved heat flux was obtained by preparing samples with heights ranging from 2 to 15 cm in 1 cm increments, measuring heat flux at the top of each one as a representative section of the full sized sample, and combining these measurements to produce a complete heat feedback profile across a 15 cm sample
Originally we studied this profile with a 1 cm spatial resolution for heat flux measurements  16 measurements from x = 2 to 15 cm
In these tests, we had a burner issue (go to next page)

## Slide 10: Experimental Procedure
Ignite sample base with propane burner; 125 s exposure
Allow flame to propagate freely upwards for 475 s or until full sample involvement
Measure flame to surface heat feedback at 8 heights (from 3 to 17.5 cm above base of sample)
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Notes: A straightforward extension of the above methodology to provide height-resolved heat flux measurements is to canvass a sample with multiple heat flux gauges; however, such an approach, while efficient, has significant drawbacks. The most notable among them are potential distortions in the temperature and flow structure of the gaseous boundary layer and temperature of the burning material due to a contact with multiple thermostated elements. Therefore, in this work, height-resolved heat flux was obtained by preparing samples with heights ranging from 2 to 15 cm in 1 cm increments, measuring heat flux at the top of each one as a representative section of the full sized sample, and combining these measurements to produce a complete heat feedback profile across a 15 cm sample
Originally we studied this profile with a 1 cm spatial resolution for heat flux measurements  16 measurements from x = 2 to 15 cm
In these tests, we had a burner issue (go to next page)

## Slide 11: Ignition Source Heat Flux Profile
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Chart: q" (kW/m2)
| 47.448713004444471 | 49.482383951111096 | 47.07078463555554 | 41.762631511111131 | 31.831824432592647 | 28.937233057777789 | 36.222947946666665 | 41.836752737777829 | 8.3576685786666847 | 7.5079130208888865 | 5.4281405462222141 | 3.638966678444445
Original burner configuration [13] | 0 | 0.5 | 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5
Chart: q" (kW/m2)
| 47.448713004444471 | 49.482383951111096 | 47.07078463555554 | 41.762631511111131 | 31.831824432592647 | 28.937233057777789 | 36.222947946666665 | 41.836752737777829 | 8.3576685786666847 | 7.5079130208888865 | 5.4281405462222141 | 3.638966678444445
Original burner configuration [13] | 0 | 0.5 | 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5
New burner configuration | 0 | 0.5 | 1 | 1.5 | 2 | 2.25 | 2.5 | 3 | 3.5 | 4
Notes: New burner was designed to eliminate complications (a stretched/dual flame structure) observed shortly after ignition in previous tests

## Slide 12: Flame Spread
t = 15 s t = 60 s t = 105 s t = 150 s t = 240 s
Notes: Early stages after ignition, nice small, uniform (across the sample’s width) laminar flame.
Not wholly turbulent, but we begin to see that LT transition as the flame grows.

## Slide 13: Sample Mass Loss Rate
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Chart: t (s)
Chart: t (s)
Chart: t (s)

## Slide 14: Sample Mass Loss Rate
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Chart: t (s)
Chart: t (s)
Chart: t (s)

## Slide 15: Measured Flame Heat Flux
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
x = 7.5 cm
Chart: t (s)
Chart: t (s)
Chart: t (s)

## Slide 16: Measured Flame Heat Flux
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Chart: t (s)

## Slide 17: Measured Flame Heat Flux
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
:
Chart: t (s)
Chart: t (s)

## Slide 18: Steady State Flame Heat Flux
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Chart: t (s)
x = 17.5 cm
Chart: t (s)
Chart: t (s)
q"steady | 32.2957 | 32.3555 | 32.3571 | 32.3177 | 32.2897 | 32.0613 | 31.9585 | 31.9595 | 31.9862 | 31.9846 | 31.8812 | 31.7909 | 31.7232 | 31.7228 | 31.8496 | 31.9615 | 32.1242 | 32.1084 | 32.1612 | 32.202 | 32.1919 | 32.3567 | 32.4327 | 32.41 | 32.393 | 32.3221 | 32.2033 | 32.1782 | 32.2748 | 32.201 | 32.1006 | 32.048 | 32.057 | 32.065 | 31.9975 | 31.9729 | 31.9253 | 31.9113 | 31.8743 | 31.7449 | 31.6607 | 31.5703 | 31.5839 | 31.6367 | 31.5043 | 31.6212 | 31.6648 | 31.739 | 31.8368 | 32.0125 | 32.2457 | 32.294 | 32.471 | 32.5436 | 32.5222 | 32.6527 | 32.6876 | 32.617 | 32.557 | 32.3941

## Slide 19: Steady State Flame Heat Flux
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Chart: x (cm)
| 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 7.5 | 12.5 | 17.5
Avg | 40.8636 | 40.1022 | 39.8896 | 38.8659 | 35.9329 | 35.066 | 33.6216 | 31.928 | 31.6963 | 30.6354 | 37.0304 | 35.7803 | 33.8688 | 32.9935 | 33.3828 | 32.0943 | 33.5248
2-5 cm | 39.8166 | 39.8166
6-15 cm | 33.6841 | 33.6841

## Slide 20: Normalized Flame Heat Flux
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
20
Chart: t (s)
Chart: t (s)

## Slide 21: Flame Heat Flux Profile
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work

## Slide 22: Flame Heat Flux Profile
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Heat feedback profile across a 17.5cm sample
(90s after ignition; dm’/dt = 0.037 g s-1cm-1)
Chart: x (cm)
| 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
90 s | 0.95962 | 0.96866 | 0.98493 | 0.95645 | 0.76656 | 0.58177 | 0.25635 | 0.14238

## Slide 23: Determining Flame Height, xf
Flame height is defined as the highest position along the sample at which
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Chart: dm'/dt '(g s-1 cm-1)
| 1.612405099408899E-3 | 2.1217825836965408E-3 | 3.3596791847380126E-3 | 4.0246515685085967E-3 | 4.8189379183593631E-3 | 1.0169591601145883E-2 | 1.3946409906153489E-2 | 1.8574960622217841E-2
Measured | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
Fitted | -21.04 | -5.1917 | -2.9006 | -1.4098 | 0.0019208 | 0.64407 | 1.428 | 2.113 | 2.7231 | 3.2746 | 3.7788 | 4.8815 | 5.8186 | 6.6374 | 7.3668 | 8.0261 | 8.6288 | 9.1848 | 9.7015 | 10.1846 | 10.6386 | 11.0672 | 11.4734 | 11.8597 | 12.228 | 12.5803 | 12.9179 | 13.2422 | 13.5543 | 13.8551 | 14.1456 | 14.4265 | 14.6985 | 14.9623 | 15.2182 | 15.4669 | 15.7088 | 15.9443 | 16.1737 | 16.3975 | 16.6158 | 16.8291 | 17.0374 | 17.2412 | 17.4406 | 17.6358 | 17.827

## Slide 24: Flame Heat Flux Beyond xf
Chart: x (cm)
| 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
15 s | 1.0004 | 0.92336 | 0.76817 | 0.48753 | 0.22484 | 0.16486 | 0.045742 | 0.039486
45 s | 0.98063 | 1.0078 | 0.9277 | 0.71809 | 0.47941 | 0.35948 | 0.10563 | 0.075354
90 s | 0.95962 | 0.96866 | 0.98493 | 0.95645 | 0.76656 | 0.58177 | 0.25635 | 0.14238
150 s | 0.94799 | 0.96124 | 0.9985 | 1.0053 | 0.97262 | 0.77182 | 0.49137 | 0.27389
270 s | 0.94143 | 0.94894 | 0.9985 | 1.02 | 1.0125 | 0.93669 | 0.85172 | 0.59207
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Chart: x* = x/xf
Chart: x* = x/xf

## Slide 25: Flame Heat Flux Model
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work

## Slide 26: Flame Heat Feedback Model Predictions
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Chart: q" (kW m-2)
| 36.135261820000011 | 32.20800182000005 | 28.79463316
360 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
240 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
120 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
60 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
15 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
Chart: q" (kW m-2)
| 36.135261820000011 | 32.20800182000005 | 28.79463316
360 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
240 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
120 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
60 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
15 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
15 p | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
Chart: q" (kW m-2)
| 36.135261820000011 | 32.20800182000005 | 28.79463316
360 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
240 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
120 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
60 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
60p | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
15 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
15 p | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
Chart: q" (kW m-2)
| 36.135261820000011 | 32.20800182000005 | 28.79463316
360 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
240 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
120 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
120p | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
60 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
60p | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
15 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
15 p | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
Chart: q" (kW m-2)
| 36.135261820000011 | 32.20800182000005 | 28.79463316
360 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
240 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
240p | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
120 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
120p | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
60 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
60p | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
15 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
15 p | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
Chart: q" (kW m-2)
| 36.135261820000011 | 32.20800182000005 | 28.79463316
360 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
360p | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
240 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
240p | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
120 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
120p | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
60 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
60p | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
15 | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
15 p | 3 | 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5

## Slide 27: Solid Phase Material Response
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Flexible, computational
pyrolysis solver – ThermaKin2D
  Computes the rate of material degradation and gaseous fuel production from physical and chemical properties of a solid
  Components are defined by a series of temperature dependent material properties
Volatiles
Chemical reaction
Virgin layer
Condensed phase is represented by a mixture of components (A, B,C), which interact chemically and physically.
A B + C
Conduction
Flame
Heat Flux
Notes: ThermaKin2D is a flexible computational pyrolysis solver, was used in this study to calculate the material response of PMMA– specifically, its gasification rate- when subjected to external heat.
Fully validated, predict the behavior of non-charring (PMMA, PS, HDPE) and charring materials (PC PVC)

## Slide 28: Degradation Mechanism
Material degradation mechanism defined by:
  First order Arrhenius Reaction rates:
  Temperature dependent material properties (density, heat capacity, thermal conductivity, gas transfer)
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Notes: ξ is the concentration of a given component expressed in the units of mass per unit volume ((mass fraction) ρ ).
Emissivity, and absorption coefficient defined as constant values
In a previous work [1], data collected from milligram-scale tests of 7 non-charring materials, including PMMA, was used to obtain their degradation mechanisms, thermodynamic properties of material components, and the energetics associated with the thermal degradation processes. In this manuscript, an extension of that work is presented in which bench scale experiments on PMMA provided its thermal transport properties (i.e. thermal conductivity). Temperature measurements taken in these tests, along with the results of detailed pyrolysis modeling, were used to determine a final degradation mechanism for this material, which included a glass transition state, and its corresponding (temperature dependent) thermal conductivity. The pyrolysis model constructed here was validated by comparison against an independent set of gasification experiments that provided sample mass loss rate (MLR) history in response to three different external heat fluxes (which capture a range of boundary conditions typical of likely fire scenarios).

## Slide 29: Degredation Mechanism
Milligram Scale Testing
Thermogravimetric Analyzer (TGA)
  Kinetics: A, E
Differential Scanning Calorimetry (DSC)
  Thermodynamics
  Specific heat, Cp
  Heats of
    Decomposition, hdecomp
    Melting, hmelt
Bench Scale Testing
Cone Calorimeter
  Thermal Conductivity, k
  Absorption coefficient, a
Acknowledgements: Jing Li, University of Maryland

## Slide 30: Simulation of Upward Flame Spread
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work

## Slide 31
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work

## Slide 32: Additional Materials, ABS
10 x 5 cm ABS slabs following burning in
the horizontal and vertical configuration

## Slide 33: Additional Materials, ABS
Chart: x = 5 cm
q"max (shielded) | 45.3477 | 39.5432 | 39.2375
Chart: x = 7 cm
q"max (shielded) | 40.3314 | 41.9615 | 43.487 | 33.6564 | 45.3477 | 28.819 | 34.8468 | 37.7429
Chart: x = 11 cm
q"max (shielded) | 21.8783 | 24.0211 | 35.911 | 32.8146 | 35.9245 | 37.2725
Chart: x = 15 cm
q"max (shielded) | 17.2156 | 18.7013 | 29.8521 | 26.5886 | 40.8151 | 38.3147

## Slide 34: Additional Materials, HIPS
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Chart: HIPS - 10cm
Chart: HIPS - 5cm

## Slide 35: Additional Materials, POM
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Chart: POM - 10cm
Chart: POM - 5cm

## Slide 36: Conclusions
Carefully obtained highly resolved measurements of heat feedback profile of an upward spreading flame
Created correlation predicting flame to surface heat flux, solely as a function of sample burning rate
Testing additional polymers (ABS, POM, HIPS) to determine how flame heat flux model can be generalized through straightforward scaling
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work

## Slide 37: Conclusions
Coupled flame heat flux model with solid phase computational pyrolysis solver, ThermaKin2D
Developed a fully parameterized model to simulated upward flame spread
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work

## Slide 38: Flame Heat Flux Beyond xf
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Chart: Measurement Height, x (cm)
| 4 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5
New Burner | 2.055 | 2.083 | 1.918 | 1.973 | 2.062 | 2.403 | 3.233
Avg, new burner | 2.394 | 2.394
Fitted, new burner; a=2+0.03exp(0.5(x-10)) | 2.0009 | 2.0015 | 2.0025 | 2.0041 | 2.0067 | 2.011 | 2.0182 | 2.03 | 2.0495 | 2.0815 | 2.1345 | 2.2217 | 2.3655 | 2.6026 | 2.9935 | 3.6379 | 4.7005

## Slide 39: Comparison of xf expressions
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Chart: Q' (kW/m) Pizzo et al. show transition at Q' = 17 kW/m for 5 cm wide samples
Q'<20 kW/m | 3 | 4 | 5 | 7.5 | 10
Q' > 20 kW/m | 12.5 | 15 | 17.5
QSW | 60 | 60.5 | 105 | 112 | 115 | 180 | 190

## Slide 40: Flame Spread
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Chart: Time After Burner Removal, t (s)
Notes: To justify combining measurements in this fashion, one must consider the main assumption in doing so - measuring the heat flux at the top of a shorter sample of PMMA yields the same result as measuring the heat flux at that sample height in a 15 cm tall sample. This assumption is reasonable because relatively minor changes in the conditions downstream of the measurement location (associated with the replacement of PMMA with Kaowool PM insulation) are expected to have negligible effect on the state of the reacting flow at the measurement location.

## Slide 41: Effects of Heat Flux Gauge Water Temperature
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
Chart: t (s)
Chart: t (s)
x =5 cm
x = 15 cm

## Slide 42: Flame Heat Flux Uniformity Across Sample Width
Introduction
The Fire Problem
Thermal Model
Early Models of Flame Spread
Purpose of Study
Experimental Work
Experimental Process
Flame Spread
Experimental Results
Material Burning Behavior
Measured Heat Flux
Flame Heat Flux Model
Modeling Work
Flame Heat Feedback
Flame Spread
Conclusions and Future Work
x =7.5 cm
x = 15 cm
Chart: t (s)
Chart: t (s)

## Slide 43: Soot Deposition on ABS
Notes: To justify combining measurements in this fashion, one must consider the main assumption in doing so - measuring the heat flux at the top of a shorter sample of PMMA yields the same result as measuring the heat flux at that sample height in a 15 cm tall sample. This assumption is reasonable because relatively minor changes in the conditions downstream of the measurement location (associated with the replacement of PMMA with Kaowool PM insulation) are expected to have negligible effect on the state of the reacting flow at the measurement location.

## Slide 44: Soot Deposition on HIPS
Notes: To justify combining measurements in this fashion, one must consider the main assumption in doing so - measuring the heat flux at the top of a shorter sample of PMMA yields the same result as measuring the heat flux at that sample height in a 15 cm tall sample. This assumption is reasonable because relatively minor changes in the conditions downstream of the measurement location (associated with the replacement of PMMA with Kaowool PM insulation) are expected to have negligible effect on the state of the reacting flow at the measurement location.