## Slide 1: Inherently FST Thermosets Solution for Aerospace Interior Composites
Kuanqiang Gao, PhD
The Eighth Triennial International Fire & Cabin Safety Research Conference
October 24 – 27, 2016

## Slide 2
Outlines
HUNTSMAN in Aerospace
Structural FST thermoset solution for interior composites Araldite® FST 40002 / 40003
Cost effective EHS friendly FST alternative to phenolics Benzoxazine Araldite® MT 35710 FST
Improving current composites epoxy systems LME 11082
New adhesives & syntactics for interior Epocast®1645 FR and Epibond® 8000 FR
Conclusion
Notes: Huntsman has recently developed two new epoxies and one benzoxazine resins that meet FST/ heat release according to FAR 25.853/ABD 0031.
Aradite FST 40002/40003 is a two part epoxy system, it is meet FST requirements, and has good mechanical property to be used in structural application, such as interior wall panel,

## Slide 3: Our Business Divisions
Huntsman Corporation
Amines
Surfactants
Maleic Anhydride
Upstream Intermediates
MDI
Polyols
PO/MTBE
TPU
PU Systems
Composites
Adhesives
Resins
Dyes
Chemicals
Apparel
Home & Institutional
Technical Textiles
Titanium Dioxide
Functional Additives
Color Pigments
Timber Treatment
Water Treatment
Polyurethanes
Performance
Products
Advanced
Materials
Textile Effects
Pigments &
Additives

## Slide 4
Advanced Materials Markets
Improving product performance through chemistry

## Slide 5: HUNTSMAN in Aerospace
OEM
TIER
PREPREGGER
FORMULATOR
SPECIALTY
COMPONENTS
FORMULATED SYSTEMS
TIER
HUNTSMAN
AERO PORTFOLIO
SPECIALTY
COMPONENTS
FORMULATED SYSTEMS
200+ PRODUCTS (EPOXY, CURING AGENTS, BISMALEIMIDE, BENZOXAZINE)
5 QUALIFIED MANUFACTURING SITES
100+ PRODUCTS (ADHESIVES, SYNTACTICS, COMPOSITES, REPAIR)
2 QUALIFIED MANUFACTURING SITES

## Slide 6
Outlines
HUNTSMAN in Aerospace
Structural FST thermoset solution for interior composites Araldite® FST 40002 / 40003
Cost effective EHS friendly FST alternative to phenolics Benzoxazine Araldite® MT 35710 FST
Improving current composites epoxy systems LME11082
New adhesives & syntactics for interior Epocast® 1645 FR, Epibond® 8000 FR
Conclusion

## Slide 7: Unique combination of performance
Araldite® FST 40002 / 40003
FST
Design complexity
Structural
Phenolic Prepreg
Phenolic Liquid Process
Epoxy Liquid Process
Epoxy prepreg
Thermoplastic organosheets
Araldite® FST 40002 / 40003
5
1
2
3
4
1
2
3
4
5

## Slide 8: Unique combination of performance
Araldite® FST 40002 / 40003
Inherently flame
retardant
FST according to
FAR 25.853
Unfilled
Low viscosity
Latent
Design complexity
RTM & Infusion
High mechanicals
Structural applications
Fast cure
Low exotherm
High productivity
Efficient production of interior
structural CFRP / GFRP
with maximized weight savings
Complex parts &
function integration
High productivity of
small / medium parts
Large parts
High thickness
Features
Capability
Applications

## Slide 9: Processing
Araldite® FST 40002 / 40003
Viscosity versus injection temperature
High quality versatile processing
  2-component liquid system
  Injection capability 50 -150°C
  Very low reaction energy (ca. 220 J/g):
    low risk of exotherm
    high temperature injection of high thickness parts

## Slide 10: Processing
Araldite® FST 40002 / 40003
Viscosity build-up versus temperature
Production cycle examples
High quality versatile processing
  Large part production with low cost / low temperature resistance molds
  High productivity of small / medium part (pre-cure of 5 min 150°C)
  Putrusion speed of ca. 10 meters / hour
(1) optional depending on in-mould cure conditions
(2) 5H Satin, 370 gsm, TVf 50%
 | In-mould cure | Free-stand post-cure (1)
Large part | 1H100ºC + 1H120ºC | 2H180ºC
ILSS 23ºC CFRP (2) | 56 MPa | 64 MPa
Small / medium part | 5 min 150ºC | 2H180ºC
ILSS 23ºC CFRP (2) | 54 MPa | 65 MPa

## Slide 11: Mechanicals
Araldite® FST 40002 / 40003
Highly structural solution
  High Tg and ILSS
  High tensile and medium toughness
 | Test | Araldite® FST 40002 / 40003 | Standard
NEAT | Dry DMA Tg | 260ºC | ISO 6721
 | Wet DMA Tg | 185ºC | 
 | K1C | 0.9 MPa.√m | ISO 13586
 | G1C | 270 J/m2 | 
 | Tensile modulus | 3000 MPa | ISO 527
 | Tensile strength | 100 MPa | 
 | Tensile elongation | 5 % | 
CFRP UD (1) | ILSS at 23ºC | 97 MPa | ASTM D2344
 | ILSS at 120ºC | 65 MPa | 
 | ILSS at 160ºC | 55 MPa | 
(1) UD, 6K, 270 gsm, TVf 60%

## Slide 12: Flame, Smoke & Toxicity
Araldite® FST 40002 / 40003
5H Satin, 6K, 270 gsm, TVf 50%
(2) 8H Satin, 300 gsm, TVf 50%
FST compliant solution
  Meets FST in all configurations: glass & carbon in all thickness
  Meets Heat release in low thickness. Heat release version under development (see Latest dev. column)
 | Araldite® FST 40002 / 40003 |  |  |  | Latest dev. | 
Fiber type | CFRP(1) |  | GFRP(2) |  | GFRP(2) | 
Thickness (mm) | 0.3 | 2 | 0.3 | 4 | 4 | FAR 25.853 requirements
Vertical burn 12s Burn length (mm) After flame time (s) Drip flame time(s) | 88 9 0 |  | 48 15 0 |  |  | AITM 2.0002B <203 <15 <5
Vertical burn 60s Burn length (mm) After flame time (s) Drip flame time (s) | 82 0 0 | 47 6 0 | 65 0 0 |  |  | AITM 2.0002A <152 <15 3
Heat release HRR max (kW/m2) HR (kW.min/m2) | 63 32 | 85 90 | 45 25 | 74 16 | 32 11 | AITM 2.0006 <65 <65
Toxicity (flaming mode) Components toxicity level | pass |  |  |  |  | AITM 3.0005
Smoke After 4 min | 23 | 12 | 16 |  | 46 | AITM 2.0007A <200

## Slide 13
Outlines
HUNTSMAN in Aerospace
Structural FST thermoset solution for interior composites Araldite® FST 40002 / 40003
Cost effective EHS friendly FST alternative to phenolics Benzoxazine Araldite® MT 35710 FST
Improving current composites epoxy systems LME 11082
New adhesives & syntactics for interior Epocast® 1645 FR, Epibond® 8000 FR
Conclusion

## Slide 14: Unique combination of performance
Benzoxazine Araldite® MT 35710 FST
FST
EHS
Cost
1
2
3
Phenolic Prepreg
Bis-F Benzoxazine
Araldite® MT 35700
Benzoxazine
Araldite® XU 35710 FST
1
2
3

## Slide 15: Unique combination of performance
Benzoxazine Araldite® MT 35710 FST
Inherently Flame
Retardant
FST & heat release
FAR 25.853 &
ABD 0031
Liquid
Prepreg w/w and w/o
solvent &
Liquid Process
Medium Mechanicals
Semi Structural
Cost effective
Competitive to
Phenolics
Features
Capability
Applications
No Volatile
EHS friendly
No porosity & high
laminate quality
Cost effective,
high quality,
EHS friendly,
production of
non-structural up to
semi- structural
interior composites

## Slide 16: Processing
Benzoxazine Araldite® MT 35710 FST
 | Araldite® MT 35710 FST | Bis/F Benzoxazine Araldite® MT 35700
Physical Form | Amber viscous liquid | Solid
Viscosity at 60oC | 1500 mPas | 
Melting point (°C) |  | 55 - 65
Liquid
Prepreg w/w and w/o
solvent &
Liquid Process
Improvement vs. Araldite® MT 35700 (Bis-F Benzoxazine)
  Liquid at 23°C, < 100 mPas above 100°C
  Cost effective for phenolic substitution
can find applications in prepreg hot-melt and solvent based as well as direct process
Cost effective
Competitive to
Phenolics

## Slide 17: Mechanical & FST
 | Test | Araldite® MT 35710 FST | Typical Areo Phenolic | Standard
NEAT | Tg DSC (ºC) | 140 |  | ISO 11357-2
 | K1C (MPa.√m) | 0.92 |  | ISO 13586
 | G1C (J/m2) | 200 |  | 
 | Tensile modulus (MPa) | 4900 |  | ISO 527
 | Tensile strength (MPa) | 60 |  | 
 | Tensile elongation (%) | 1.3 |  | 
GFRP (1) | Tensile modulus (warp) (GPa) | 28 | 19-24 | ISO 527
 | Tensile strength (warp) (MPa) | 457 | 380-400 | 
 | Compression modulus (warp) (GPa) | 29 | 20-24 | ISO 14126
 | Compression strength (warp) (MPa) | 555 | 350-380 | 
 | ILSS (warp) (MPa) | 50 | 24-50 | ISO 14130
 | Araldite® MT 35710 FST | 
Fiber type | GFRP(1) | 
Thickness (mm) | 0.6 | FAR 25.853 requirements
Vertical burn 60s Burn length (mm) After flame time (s) Drip flame time (s) | 94 0 0 | AITM 2.0002A <152 <15 <3
Heat release HRR max (kW/m2) HR (kW.min/m2) | 18 29 | AITM 2.0006 <65 <65
Toxicity (flaming mode) Components toxicity level | pass | AITM 3.0005
Smoke After 4 min | 11 | AITM 2.0007A <200
(1) 8H Satin, 300 gsm, TVf 50%
Semi-structural FST solution
  Medium Tg of 140°C
  Medium toughness
  Meets FST and heat release
  according to FAR 25.853 / ABD 0031
Inherently Flame
Retardant
FST & heat release
FAR 25.853 &
ABD 0031
Medium Mechanicals
Semi Structural applications
better performance than phenolics
Benzoxazine Araldite® MT 35710 FST

## Slide 18
Outlines
HUNTSMAN in Aerospace
Structural FST thermoset solution for interior composites Araldite® FST 40002 / 40003
Cost effective EHS friendly FST alternative to phenolics Benzoxazine Araldite® MT 35710 FST
Improving current composites epoxy systems LME 11082
New adhesives & syntactics for interior Epocast® 1645 FR, Epibond® 8000 FR
Conclusion

## Slide 19: LME 11082
New inherently FST epoxy
Test |  | LME 11082 | Bis-A | Standard
 |  | With hardener XB 3473 |  | 
NEAT | DMA Tg (ºC) | 180 | 185 | ISO 6721
 | K1C (MPa.√m) | 0.6 | 0.6 | ISO 13586
 | G1C (J/m2) | 140 | 165 | 
 | Tensile modulus (MPa) | 2700 | 2500 | ISO 527
 | Tensile strength (MPa) | 50 | 47 | 
 | Tensile elongation (%) | 2.5 | 2.65 | 
 | LME11082 XB 3473 | 
Fiber type | GFRP(1) | 
Cure cycle | 2H120ºC + 2H140ºC + 2H180ºC | 
Thickness (mm) | 0.3 | FAR 25.853 requirements
Vertical burn 12s Burn length (mm) After flame time (s) Drip flame time (s) | 80 0 0 | AITM 2.0002B <203 <15 <5
Vertical burn 60s Burn length (mm) After flame time (s) Drip flame time (s) | 85 0 0 | AITM 2.0002A <152 <15 <3
Heat release HRR max (kW/m2) HR (kW.min/m2) | 38 21 | AITM 2.0006 <65 <65
Toxicity (flaming mode) Components toxicity level | pass | AITM 3.0005
Smoke After 4 min | 43 | AITM 2.0007A <200
(1) 8H Satin, 300 gsm, TVf 50%
Structural inherently FST epoxy (tested with a typical high Tg curing agent):
  Meets FST and heat release according to FAR 25.853 / ABD 0031
  Similar mechanical performance as Bis-A epoxy
can substitute standard epoxy, novolac in structural prepreg and RTM (interior & exterior)

## Slide 20
Outlines
HUNTSMAN in Aerospace
Structural FST thermoset solution for interior composites Araldite® FST 40002 / 40003
Cost effective EHS friendly FST alternative to phenolics Benzoxazine Araldite® MT 35710 FST
Improving current composites epoxy systems LME 11082
New adhesives & syntactics for interior Epocast® 1645 FR, Epibond® 8000 FR
Conclusion

## Slide 21: New adhesives and syntactics
Epibond® 8000 FR A/B
Two-part epoxy adhesive
Honeycomb panels bonding
Metals and composite bonding
Insert bonding
Epocast® 1645 FR A/B
Two-parts epoxy syntactic
Honeycomb edge filling
Honeycomb void filling
FST acc to FAR 25.853
High shear, peel & compressive strength
High productivity, 55 min work life
Extrudable 2:1 cartridge
Ultra low density 0.48
12s vertical (FAR 25.853B)
Fast gel time of 65 min
Quickly sandable
Product
Application
Features
Drivers
Fast assembly
REACH
Weight savings
100% FR / FST
in Interior

## Slide 22: Inherently FST Thermosets Resins
Araldite® FST 40002/40003
Benzoxazine Araldite® MT 35710FST
LME 11082
Design complexity
RTM & Infusion
Structure Application
High productivity
EHS Friendly
Prepreg or infusion
Interior application
Cost effective
Substitute standard epoxy novolac
Prepreg /RTM Process
Structural application
Low viscosity
Unfilled
Latent
High mechanicals
Fast cure
Low exotherm
Liquid resin
No volatile release
Medium mechanicals
High quality laminate w/o porosity
Competitive to phenolics
Special epoxy resin
Similar mechanical performance to DGEBA
Summary
All meets FST/ heat release according to FAR 25.853/ABD 0031

## Slide 24
Question?
kuanqiang_gao@huntsman.com
todd_holder@huntsman.com
Advanced Materials