## Slide 1: Controlled Atmosphere Pyrolysis Apparatus II (CAPA II)
Josh Swann
Yan Ding
Mark McKinnon
Stanislav Stoliarov

## Slide 2
Outline
Background and Objectives
Experimental Setup
Quantification of Boundary Conditions
PVC Case Study
Conclusions

## Slide 3
Methodology
Milligram-scale
Gram-scale
Comprehensive Pyrolysis Model
Rates of gasification, burning, and flame spread on bench-scale [1-6]

## Slide 4
Controlled Atmosphere Pyrolysis
Apparatus (CAPA)
Augmentation to standard cone calorimeter
Sample size:
80 mm x 80 mm
Well-defined boundary conditions:
  Typical heat flux range
Up to 80 kW m‾²
  O₂ Concentration at surface
  ∼ 2.3 vol.% (225 SLPM N₂)
  Convection coefficient for top and bottom surfaces determined through inverse analysis
Simultaneously measure sample temperatures and mass loss rate (for model validation)

## Slide 5
Controlled Atmosphere Pyrolysis
Apparatus (CAPA)
Excellent mass and temperature measurements for non-swelling materials at relatively lower levels of radiation
Limitations for charring and intumescent materials:
  Unstable boundary conditions
    Non-thermally stable chamber walls
    Non-uniform gaseous conditions above sample surface
  Deviates from 1-D modeling framework
    Unable to quantitatively measure the intumescing sample shape profiles
    3-D behavior is very computationally expensive

## Slide 6
Objectives
Extend the current methodology to charring and intumescent materials
Investigate the importance of multi-dimensional behavior

## Slide 7
Experimental Setup
Well-defined boundary conditions:
  Oxygen concentration below 1 vol.% (185 SLPM N2)
  Axisymmetric radiation mapping, including angular variations
  Top and bottom surface convective losses from FDS modeling
Simultaneous measurements of:
  Mass (1 mg resolution)
  Back surface temperature
  Quantitative shape profile
Sample size: 0.07 m diameter

## Slide 8
Bottom of heater
h/H
r/R
0
1.25
Boundary Conditions: Radiation
Measured with Schmidt-Boelter heat flux transducer
Normalized height, h/H
  H = distance to bottom of heater from initial sample surface (0.04 m)
Normalized radius, r/R
  R = radius of sample (0.035 m)
Measurements taken at equally spaced positions

## Slide 9
Boundary Conditions: Radiation

## Slide 10
Boundary Conditions: Radiation

## Slide 11
Boundary Conditions: Radiation
r/R
r/R

## Slide 12
Boundary Conditions: Radiation
Angular radiation coefficient

## Slide 13
Boundary Conditions: Convection
Axisymmetric DNS model in FDS
  Radiation was neglected
  Constant wall temperatures
  Insulator properties the same as sample
  Neglected opening between outer chamber wall and heater
Three modeled geometries

## Slide 14
Boundary Conditions: Convection
t = 0 s
t = 18 s
T [K]
Period-averaged convection coefficient:
Convective heat flux, q’’, and convection coefficient, hc:

## Slide 15
Boundary Conditions: Convection
t = 0 s
t = 18 s
T [K]
Period-averaged convection coefficient:
Convective heat flux, q’’, and convection coefficient, hc:

## Slide 16
30 kW m-2
60 kW m-2
PVC Case Study – Mass
Poly(vinyl chloride) samples
  6.35 mm thick
  Conditioned in desiccator
Two step decomposition for lower fluxes as seen in TGA for PVC [7]

## Slide 17
PVC Case Study – Temperature
30 kW m-2
60 kW m-2
Infrared Camera
  Non-invasive measurements
  Samples painted with high emissivity paint (≈0.95)

## Slide 18
PVC Case Study - Shape
30 kW m-2
t=50s
t=300s
t=420s
t=300s
t=480s
t=240s
60 kW m-2

## Slide 19
PVC Case Study – Projected Heat Flux
h/H
r/R

## Slide 20
PVC Case Study – Projected Heat Flux
30 kW m-2
60 kW m-2

## Slide 21
Conclusions
A new experiment was designed to provide highly accurate mass, spatially-resolved temperature, and multi-dimensional shape profile diagnostics for highly intumescent materials
Well-defined boundary conditions throughout the gasification chamber were achieved to account for the evolution of sample shape during pyrolysis
Results indicate a multi-dimensional framework is required to fully capture the thermal transport and swelling dynamics of highly intumescent materials

## Slide 22
Acknowledgements
This and ongoing work is made possible by funding from:
The National Science Foundation CAREER Award #1347196 under the grant monitor Dr. Ruey-Hung Chen

## Slide 23
References
[1] M.R. Semmes, X. Liu, M.B. Mckinnon, S.I. Stoliarov, A. Witkowski, A Model for Oxidative Pyrolysis of Corrugated Cardboard, Fire Saf. Sci. 11 (2014) 111–123. doi:10.3801/IAFSS.FSS.11-111.
[2] J. Li, J. Gong, S.I. Stoliarov, Gasification experiments for pyrolysis model parameterization and validation, Int. J. Heat Mass Transf. 77 (2014) 738–744.
[3] J. Li, J. Gong, S.I. Stoliarov, Development of pyrolysis models for charring polymers, Polym. Degrad. Stab. 115 (2015) 138–152.
[4] M.B. Mckinnon, S.I. Stoliarov, Pyrolysis model development for a multilayer floor covering, Materials (Basel). 8 (2015) 6117–6153.
[5] I.T. Leventon, J. Li, S.I. Stoliarov, A flame spread simulation based on a comprehensive solid pyrolysis model coupled with a detailed empirical flame structure representation, Combust. Flame. 162 (2015) 3884–3895. doi:10.1016/j.combustflame.2015.07.025.
[6] S.I. Stoliarov, R.E. Lyon, FAA Technical Note; DOT/FAA/AR-TN08/17.
[7] S.I. Stoliarov, S. Crowley, R.E. Lyon, G.T. Linteris, Prediction of the burning rates of charring polymers, Combust. Flame. 157 (2010) 2024–2034. doi:10.1016/j.combustflame.2008.11.010

## Slide 24
Thank you!