## Slide 1
Combustion Products of Polymers at Constant Fuel/Oxygen Ratios
Louise C. Speitel, Richard N. Walters, & Richard E. Lyon

## Slide 2
Approach
Develop rapid laboratory test to screen flame retardants and FR plastics for:
  Gas phase activity
  Combustion toxicity
103 kg
1 kg
10-6 kg

## Slide 3
Strategy
  Generate fire effluents in the the Microscale Combustion Calorimeter (MCC) at various fuel/oxygen () ratios
  Measure combustion gases using
    CO and CO2 analyzers
    Fourier Transform Infrared (FTIR) spectrometer
  Develop FTIR method/s for those combustion gases
Measure Fire Effluents at Micro Scale

## Slide 4
Microscale Combustion Calorimeter

## Slide 5: Fuel / Oxygen Ratio in MCC

## Slide 6: Fuel / O2 Control and Measurement

## Slide 7
Combustion Chemistry Changes with Fire Stage

## Slide 8: Schematic MCC-FTIR

## Slide 9: MCC w/ FTIR Evolved Gas Analysis

## Slide 10: Multi-Point Calibration

## Slide 11
Spectra for 15 Combustion Gases

## Slide 12
Spectral Regions for Combustion Gases:
Method 1

## Slide 13
Spectral Regions for Combustion Gases:
Method 2

## Slide 14: Multi-Point Calibration Spectral Regions

## Slide 15: Multi-Point Calibration

## Slide 16
HF From Polyvinylflouride (PVF)

## Slide 17
FTIR of Sulfurous Gases from PPS

## Slide 18
Sulfurous Product Yields  Weight Fraction Sulfur

## Slide 19: HCN vs  for N-Containing Polymers

## Slide 20
Comparison of All Vitiated PA66 Yields

## Slide 21
Toxic Gas Yields for p-Polyaramid (KEVLAR)

## Slide 22
Toxic Gas Yields for Polyimide (KAPTON)

## Slide 23
Toxic Gas Yields for Polyetherimide (ULTEM)

## Slide 24
Toxic Gas Yields (FTIR): Weight Basis
Phi | Material | CO (g/g) | CO2 (g/g) | COF2 (g/kg) | COS (g/kg) | HBr (g/kg) | HCN (g/kg) | HCl (g/kg) | HF (g/kg) | NO (g/kg) | NO2 (g/kg) | SO2 (g/kg)
0.5 | ABS | 0.000 | 4.397 | 0.00 | 0.00 | 0.05 | 0.30 | 0.00 | 0.00 | 36.28 | 0.00 | 0.12
1 | ABS | 0.070 | 4.197 | 0.00 | 0.00 | 0.17 | 1.47 | 0.00 | 0.00 | 15.63 | 0.00 | 0.08
2 | ABS | 1.080 | 1.903 | 0.00 | 0.11 | 0.00 | 40.14 | 0.03 | 0.00 | 2.03 | 0.00 | 0.08
0.5 | AModelA-1002 | 0.007 | 3.134 | 0.00 | 0.00 | 0.00 | 1.36 | 0.12 | 0.62 | 37.57 | 0.00 | 0.00
1 | AModelA-1002 | 0.348 | 2.377 | 0.00 | 0.20 | 0.00 | 38.83 | 0.09 | 0.09 | 11.29 | 0.00 | 0.00
2 | AModelA-1002 | 0.670 | 1.213 | 0.09 | 0.21 | 0.00 | 101.50 | 0.16 | 0.00 | 5.20 | 0.00 | 0.00
0.5 | AModelAF-1133 | 0.136 | 1.425 | 0.00 | 0.03 | 0.00 | 13.84 | 0.15 | 0.00 | 15.10 | 0.00 | 0.06
1 | AModelAF-1133 | 0.246 | 1.070 | 0.03 | 0.07 | 0.00 | 28.51 | 2.90 | 0.09 | 11.42 | 0.00 | 0.00
2 | AModelAF-1133 | 0.372 | 0.649 | 0.05 | 0.03 | 0.00 | 38.91 | 6.41 | 0.21 | 6.66 | 0.01 | 0.00
0.5 | Boltaron 9815E | 0.003 | 0.533 | 0.60 | 0.07 | 13.19 | 0.10 | 401.47 | 12.58 | 1.54 | 0.00 | 0.66
1 | Boltaron 9815E | 0.046 | 0.458 | 0.14 | 0.02 | 3.65 | 0.15 | 387.16 | 7.20 | 1.44 | 0.04 | 1.08
2 | Boltaron 9815E | 0.168 | 0.230 | 0.00 | 0.06 | 9.89 | 0.34 | 378.41 | 10.28 | 1.03 | 0.00 | 0.20
0.5 | HIPS | 0.000 | 4.448 | 0.00 | 0.01 | 0.00 | 0.40 | 0.14 | 0.00 | 0.03 | 0.00 | 0.00
1 | HIPS | 0.042 | 4.230 | 0.00 | 0.01 | 0.04 | 0.09 | 0.07 | 0.00 | 0.00 | 0.00 | 0.08
2 | HIPS | 1.095 | 1.764 | 0.01 | 0.04 | 0.00 | 0.18 | 0.05 | 0.00 | 0.00 | 0.00 | 0.00
0.5 | Isoplast PU | 0.000 | 2.990 | 0.00 | 0.00 | 0.00 | 0.12 | 6.09 | 0.80 | 43.13 | 0.00 | 0.41
1 | Isoplast PU | 0.303 | 2.339 | 0.00 | 0.03 | 0.00 | 20.96 | 2.29 | 0.22 | 18.54 | 0.00 | 0.43
2 | Isoplast PU | 0.791 | 1.116 | 0.07 | 0.10 | 0.00 | 56.56 | 0.29 | 0.00 | 6.33 | 0.00 | 0.69
0.5 | Kadel E-1000 | 0.000 | 1.649 | 0.00 | 0.01 | 0.00 | 0.03 | 0.14 | 0.11 | 0.06 | 0.00 | 0.22
1 | Kadel E-1000 | 0.103 | 1.319 | 0.00 | 0.02 | 0.00 | 0.11 | 0.54 | 0.09 | 0.24 | 0.00 | 0.38
2 | Kadel E-1000 | 0.474 | 0.623 | 0.00 | 0.02 | 0.00 | 0.05 | 0.48 | 0.00 | 0.05 | 0.00 | 0.69
0.5 | Kadel E-1230 | 0.084 | 0.911 | 0.00 | 0.01 | 0.00 | 0.06 | 0.58 | 0.00 | 0.29 | 0.00 | 0.06
1 | Kadel E-1230 | 0.208 | 0.606 | 0.01 | 0.02 | 0.00 | 0.12 | 0.36 | 0.09 | 0.02 | 0.00 | 0.06
2 | Kadel E-1230 | 0.255 | 0.487 | 0.02 | 0.06 | 0.00 | 0.06 | 0.53 | 0.00 | 0.02 | 0.00 | 0.00

## Slide 25
Toxic Gas Yields (FTIR): Weight Basis
Phi | Material | CO (g/g) | CO2 (g/g) | COF2 (g/kg) | COS (g/kg) | HBr (g/kg) | HCN (g/kg) | HCl (g/kg) | HF (g/kg) | NO (g/kg) | NO2 (g/kg) | SO2 (g/kg)
0.5 | Kevlar | 0.000 | 1.485 | 0.01 | 0.00 | 0.00 | 0.00 | 0.03 | 0.00 | 38.60 | 0.00 | 0.00
1 | Kevlar | 0.004 | 1.452 | 0.00 | 0.00 | 0.00 | 0.35 | 0.12 | 0.00 | 29.55 | 0.00 | 0.36
2 | Kevlar | 0.409 | 0.694 | 0.01 | 0.03 | 0.00 | 70.61 | 0.04 | 0.19 | 15.78 | 0.00 | 0.50
0.5 | PA66 | 0.000 | 3.169 | 0.00 | 0.00 | 0.00 | 0.25 | 0.16 | 0.00 | 31.99 | 0.00 | 0.47
1 | PA66 | 0.120 | 2.735 | 0.01 | 0.02 | 0.06 | 2.80 | 0.00 | 0.00 | 8.07 | 0.00 | 1.57
2 | PA66 | 0.634 | 1.333 | 0.05 | 0.02 | 0.25 | 71.33 | 0.15 | 0.00 | 1.69 | 0.00 | 0.24
0.5 | PE | 0.000 | 4.351 | 0.00 | 0.01 | 0.36 | 0.58 | 0.04 | 0.00 | 0.58 | 0.00 | 0.00
1 | PE | 0.491 | 3.319 | 0.11 | 0.01 | 0.00 | 0.00 | 0.06 | 0.00 | 0.02 | 0.00 | 0.23
2 | PE | 0.933 | 1.894 | 0.36 | 0.14 | 0.00 | 0.11 | 0.07 | 0.00 | 0.08 | 0.00 | 0.07
0.5 | Polyimide | 0.000 | 0.685 | 0.00 | 0.00 | 0.00 | 0.04 | 0.02 | 0.61 | 23.18 | 0.00 | 0.00
1 | Polyimide | 0.020 | 0.640 | 0.00 | 0.00 | 0.00 | 0.99 | 0.08 | 0.00 | 17.41 | 0.00 | 0.00
2 | Polyimide | 0.163 | 0.397 | 0.00 | 0.00 | 0.00 | 15.17 | 0.05 | 0.00 | 9.09 | 0.00 | 0.00
0.5 | Polybromo3styrene | 0.012 | 2.714 | 0.00 | 0.00 | 0.87 | 0.00 | 2.90 | 8.57 | 1.60 | 0.00 | 0.03
1 | Polybromo3styrene | 0.440 | 0.786 | 0.05 | 0.00 | 40.78 | 0.12 | 10.94 | 44.41 | 0.40 | 0.00 | 0.16
2 | Polybromo3styrene | 0.817 | 0.464 | 0.98 | 0.02 | 117.25 | 0.10 | 7.76 | 36.52 | 0.45 | 0.00 | 0.00
0.5 | POM | 0.000 | 2.484 | 0.00 | 0.02 | 0.00 | 0.23 | 0.06 | 0.00 | 0.06 | 0.00 | 0.00
1 | POM | 0.033 | 2.218 | 0.00 | 0.00 | 0.00 | 0.00 | 0.09 | 0.00 | 0.07 | 0.00 | 0.04
2 | POM | 0.470 | 0.949 | 0.00 | 0.02 | 0.00 | 0.14 | 0.00 | 0.00 | 0.16 | 0.00 | 0.04
0.5 | PPS | 0.001 | 1.343 | 0.00 | 0.01 | 0.00 | 0.00 | 0.07 | 12.25 | 1.95 | 0.00 | 777.48
1 | PPS | 0.086 | 1.215 | 0.00 | 0.86 | 0.07 | 0.07 | 0.85 | 6.20 | 1.21 | 0.00 | 757.49
2 | PPS | 0.481 | 0.517 | 0.01 | 16.12 | 0.00 | 0.31 | 4.40 | 8.41 | 0.56 | 0.00 | 306.87
0.5 | PVF | 0.000 | 2.401 | 0.14 | 0.02 | 0.00 | 0.04 | 10.88 | 270.02 | 0.00 | 0.01 | 0.00
1 | PVF | 0.136 | 1.931 | 0.00 | 0.12 | 0.12 | 0.49 | 2.22 | 287.25 | 0.12 | 0.00 | 0.00
2 | PVF | 0.780 | 0.497 | 0.00 | 0.25 | 0.12 | 0.12 | 0.99 | 230.64 | 0.00 | 0.00 | 0.12

## Slide 26
Toxic Gas Yields (FTIR): Weight Basis
Phi | Material | CO (g/g) | CO2 (g/g) | COF2 (g/kg) | COS (g/kg) | HBr (g/kg) | HCN (g/kg) | HCl (g/kg) | HF (g/kg) | NO (g/kg) | NO2 (g/kg) | SO2 (g/kg)
0.5 | Radel R5200 | 0.000 | 1.759 | 0.00 | 0.02 | 0.02 | 0.11 | 1.09 | 0.78 | 0.02 | 0.00 | 241.19
1 | Radel R5200 | 0.010 | 1.822 | 0.00 | 0.03 | 0.00 | 0.10 | 0.69 | 0.24 | 0.02 | 0.00 | 236.54
2 | Radel R5200 | 0.402 | 0.622 | 0.00 | 2.14 | 0.14 | 0.15 | 1.84 | 0.23 | 0.01 | 0.00 | 198.52
0.5 | Radel R7200 | 0.019 | 1.029 | 0.12 | 0.00 | 0.00 | 0.06 | 0.03 | 0.13 | 0.02 | 0.00 | 171.70
1 | Radel R7200 | 0.120 | 0.906 | 0.07 | 0.23 | 0.00 | 0.04 | 0.33 | 0.30 | 0.00 | 0.00 | 190.16
2 | Radel R7200 | 0.271 | 0.519 | 0.13 | 1.29 | 0.00 | 0.12 | 1.04 | 0.19 | 0.02 | 0.00 | 175.44
0.5 | Radel R7700GY | 0.000 | 1.811 | 0.00 | 0.00 | 0.05 | 0.11 | 7.87 | 0.46 | 0.04 | 0.00 | 256.45
1 | Radel R7700GY | 0.047 | 1.798 | 0.01 | 0.07 | 0.00 | 0.26 | 8.03 | 0.88 | 0.13 | 0.00 | 267.21
2 | Radel R7700GY | 0.437 | 0.634 | 0.00 | 1.94 | 0.00 | 0.10 | 7.66 | 0.23 | 0.02 | 0.00 | 230.79
0.5 | Tedlar TCW20BE5 | 0.000 | 1.302 | 0.59 | 0.02 | 0.00 | 0.10 | 3.97 | 111.21 | 0.19 | 0.00 | 0.00
1 | Tedlar TCW20BE5 | 0.028 | 1.234 | 0.50 | 0.01 | 0.10 | 0.15 | 2.62 | 138.32 | 0.06 | 0.00 | 0.00
2 | Tedlar TCW20BE5 | 0.369 | 0.425 | 0.49 | 0.06 | 0.00 | 0.16 | 1.74 | 143.90 | 0.10 | 0.00 | 0.00
0.5 | Torlon 4203L | 0.000 | 0.741 | 0.00 | 0.03 | 0.13 | 0.04 | 0.73 | 0.00 | 22.44 | 0.00 | 0.00
1 | Torlon 4203L | 0.001 | 1.017 | 0.02 | 0.02 | 0.21 | 0.10 | 0.67 | 0.15 | 17.39 | 0.00 | 0.22
2 | Torlon 4203L | 0.131 | 0.524 | 0.00 | 0.07 | 0.09 | 9.74 | 0.14 | 0.00 | 12.19 | 0.00 | 0.72
0.5 | Ultem 9075 | 0.068 | 1.257 | 0.00 | 0.01 | 0.00 | 0.13 | 0.00 | 0.00 | 22.65 | 0.00 | 0.00
1 | Ultem 9075 | 0.137 | 1.212 | 0.01 | 0.00 | 0.00 | 0.48 | 0.07 | 0.00 | 19.58 | 0.00 | 0.00
1.5 | Ultem 9075 | 0.242 | 0.968 | 0.01 | 0.19 | 0.00 | 7.37 | 0.02 | 3.72 | 12.31 | 0.00 | 0.05
2 | Ultem 9075 | 0.360 | 0.746 | 0.06 | 0.01 | 0.00 | 8.46 | 0.04 | 0.00 | 7.83 | 0.00 | 0.00
0.5 | Xydar G930 | 0.000 | 1.286 | 0.00 | 0.00 | 0.00 | 0.00 | 0.35 | 0.00 | 0.05 | 0.00 | 0.21
1 | Xydar G930 | 0.020 | 1.117 | 0.00 | 0.00 | 0.00 | 0.28 | 1.36 | 0.00 | 0.12 | 0.00 | 0.16
2 | Xydar G930 | 0.251 | 0.569 | 0.01 | 0.02 | 0.00 | 0.07 | 0.99 | 1.25 | 0.03 | 0.00 | 0.05

## Slide 27
  Fractional effective dose (FED): FEDI = ∑FEDI Gases
  “Incapacitation” (50%) occurs when FEDIncapacitation = 1
      CO, CO2, HCN
      Do not include contribution of acid gases to incapacitation
  Lethality or post-exposure lethality (50%) occurs when FEDLethality = 1
      Acid gases: HF, HCl, HBr, NO2. SO2
  Sensory irritation occurs well before lethality
  Sensory Irritant Model: Acid Gases: HF, HCl, HBr, NO2, SO2
  Sensory irritants may impede escape or cause irreversible damage.
Toxicity Modeling for MCC at Various Φs

## Slide 28: Present / Future Work
Generate new FT-IR calibration spectra & develop method more
Test more materials & flame retardants
Examine higher combustion temperatures
Update toxicity models for asphyxiant and irritant gases:
Consider applying ISO 13571 standard
Consider using a sensory irritation model
Apply toxicity model to MCC-Φ gas yields

## Slide 29: Conclusions
MCC-FTIR technique shows promise for monitoring combustion gas species using milligram samples in a 15 minute test with accurate control of equivalence ratio.
The MCC-FTIR methodology will be used to screen novel chemical compounds (e.g., organometallics) for gas phase flame inhibition activity.
The toxic gas yields may be incorporated into mixture fraction models for toxicity assessments.