## Slide 1: An Overview of FAA Fire Safety Research Since the Previous Triennial Conference in 2013
Gus Sarkos
Manager, Fire Safety Branch
FAA Wm. J. Hughes Technical Center
Atlantic City International Airport, NJ 08405

## Slide 2: Aircraft Fire Safety Areas of Concern
Postcrash Fire
In-flight Fire

## Slide 3: Program Drivers
New Technology (Composite Fuselage, Magnesium Alloys, Fuel Cells)
New Fire Threats (Lithium Batteries)
Accidents/Incidents
NTSB Recommendations
EPA Restrictions on Effective Fire Safety Technology (Halon Extinguishing Agents, Brominated Flame Retardants)
Inherent Fire Risks in Aircraft Design and Operation

## Slide 4: Accidents/Incidents in 2013
Standards contributed to survivability
Event suggests more research is needed

## Slide 5: Material Fire Tests & Material Fire Behavior
New Material Flammability Test Methods/Standards
Improved Required Flammability Test Methods/Standards
Material Fire Behavior During
  Small-Scale Fire Tests
  Intermediate-Scale Fire Tests
  Full-Scale Fire Tests

## Slide 6: Examined Composite Structure Fire Behavior in Relation to the Ethiopian 787 Fire
9 min
Measured Inboard Flame Temperatures

## Slide 7: Determined Conditions Impacting Composite Structure Fire Behavior
Measured Burn Length for
Various Panel Thicknesses
Chart: Sample ID
| 4 Ply | 8 Ply | 16 Ply | 24 Ply | 32 Ply | HC Core
 | 11.25 | 21.25 | 5 | 0 | 0 | 44.75
Chart: Sample ID
| 4 Ply | HC Core
Baseline | 11.25 | 44.75
Insulated | 45.375
Cooled | 0 | 45.5
Comparison of Three Heat Transfer
Conditions for 4 Ply and HC Core

## Slide 8: Continued Development of a VFP Test for Composite Fuselage Structures
Unit #1
Unit #2
Unit #3
Average Burn Length – 4 Ply CFRP
Histogram

## Slide 9: Conducted Riser Fire Tests in Fuselage Section Rig
Test Rig Configuration
Foam Block Fire Source
Silicone/Nylon Duct – During Test
Silicone/Nylon Duct – After Test
Silicone/Steel Duct – After Test
Results Demonstrate Inadequacy of
VBB Test

## Slide 10: Continued Development of VFP Test for Electrical Wiring and Ducting

## Slide 11
Improved Standardization of a Flammability Test Method for Magnesium Alloy Seat Structure
Final Report: DOT/FAA/TC-13/52

## Slide 12
Developing Criteria for Flammability Testing of Magnesium Alloys in Other Seat and Cabin Applications

## Slide 13
0.001
0.01
0.1
1
10
0
0.5
1
1.5
2
2.5
CO / CO2
Fuel / Air Ratio
Late Stage Cabin Fire
Early Stage Cabin Fire
Increasing toxicity
Adapted the Microscale Combustion Calorimeter (MCC) to Examine Gas Emissions in Vitiated Air
FAA microscale combustion calorimeter (MCC) with infrared analysis of toxic combustion products from burning plastics.

## Slide 14
Improving Material Flammability Tests
Currently Required by Regulation

## Slide 15
Conducted OSU Round Robins to Evaluate Impact of Improvements on Test Data Reproducibility

## Slide 16
Developing Improved Version of the OSU Rate of Heat Release Apparatus (HR2)

## Slide 17
Implementing NexGen (Sonic) Burner Into Required Flammability Tests
Sonic and Park Burner Comparison
Park Burner
NexGen Burner

## Slide 18
Evaluated the Impact of Non-Low Heat Release Panels on Postcrash Fire Survivability

## Slide 19
non-OSU-Compliant Materials
OSU-Compliant Materials

## Slide 20: Systems Fire Protection:
Lithium Batteries
Cargo Compartment Fire Protection
Halon Replacement
Fuel Cells

## Slide 21: Evaluated Fire Containment Covers (FCCs) Against Lithium Battery Fires
4800 Li Metal Cells
1000 Lithium-ion Cells

## Slide 22: Evaluated Fire Resistant Containers (FRCs) Against Lithium Battery Fires

## Slide 23: Evaluated Water Mist System for Class-E Cargo Compartment Fire Protection
~84 Liters of water used
~34 Kg of nitrogen used

## Slide 24: Measured Flammable Gasses Vented by Lithium Batteries in Thermal Runaway
Chart: State of Charge (%)
| 100 | 50 | 90 | 80 | 70 | 60 | 40 | 30 | 20 | 10
Gas Volume (liters (10psi)) | 7.85 | 2.2498 | 5.2314 | 5.0493 | 4.2391 | 2.8109 | 2.0897 | 1.4934 | 1.3239 | 1.0432
Chart: State of Charge (%)
| 100 | 50 | 90 | 80 | 70 | 60 | 40 | 30 | 20 | 10
 | 0.70338 | 0.39494 | 0.5642 | 0.51212 | 0.4557 | 0.36022 | 0.33852 | 0.23002 | 0.17794 | 0.12152
Chart: State of Charge (%)
| 100 | 50 | 90 | 80 | 70 | 60 | 40 | 30 | 20 | 10
 | 1.5301 | 0.43244 | 1.012 | 0.93084 | 0.84721 | 0.65825 | 0.4419 | 0.096131 | 0.06484 | 0.04366
Chart: State of Charge (%)
| 100 | 50 | 90 | 80 | 70 | 60 | 40 | 30 | 20 | 10
 | 2.1344 | 0.11718 | 1.6796 | 1.5103 | 1.2065 | 0.24304 | 0.099819 | 0.03472 | 0.03038 | 0.0217

## Slide 25: Measured Effectiveness of Halon 1301 in Preventing the Explosion of Lithium Battery Vented Flammable Gasses

## Slide 26: Measured Pressure Rise from Ignition of Battery Gasses and Number of Batteries Required to Activate Pressure Relief Panels
Chart: Sea Level, 50% SOC
| 4.9901999999999997 | 20 | 8
 | 0.252 | 1.219 | 0.594

## Slide 27: Measured the Minimum Inerting Concentration (MIC) of Halon 1301 for a Vented Lithium Battery Flammable Gas Mixture
Test Setup
Chart: %vol Halon 1301
| 0 | 5 | 7 | 8 | 8.5970000000000013
LFL | 7.88 | 13.8 | 16.15 | 17.62 | 19.52
UFL | 37.14 | 26 | 22.8 | 21.84 | 19.52
Nonflammable | 21.0117 | 18.3954 | 19.8021 | 19.9235 | 20.4155 | 19.8619 | 19.8299 | 18.9524 | 19.0034 | 19.5103 | 19.532 | 19.5034 | 19.6993 | 19.2966 | 20.1984 | 19.7892 | 19.5041 | 19.4443 | 19.5041 | 19.3993 | 19.4973 | 19.7504 | 19.6967
Flammable | 19.0071 | 20.0095 | 18.9838 | 19.7757 | 19.8007 | 19.207 | 19.5007 | 19.4619 | 19.5892 | 19.4966 | 19.5272

## Slide 28: Characterized the Fire Hazards of Numerous Lithium Battery Chemistries and Sizes 45 in Thermal Runaway
Heater
Thermocouples
Thermocouples
Heater
Chart: Number of Cells to have Runaway in 5 Cell Propagation Test
LiCoO2 (18650) | 5
LiCoO2 (AA) | 5
LiCoO2 (AAAcheck data) | 1
LiCoO2 (CR123) | 1

LiFePO4 (AA) | 1
LiFePO4 (C-Long) | 1
LiFePO4 (CR123) | 1
LiFePO4 (D) | 1

LiMnNi | 5

Li-Ion Propagation

## Slide 29: Quantified the Energy Release of Lithium Ion Batteries in Thermal Runaway Under Anaerobic Conditions

## Slide 30: Examined the Potential Fire Hazard of E-Tablets Stored in a Galley Cart (Simulated In-Flight Entertainment System)

## Slide 31: Determined Certification Criteria for Blended Gas Halon Replacement Agent in Nacelle Fire Simulator
NACELLE FIRE SIMULATOR
EXHAUST
TEST SECTION
FIRE EXTINGUISHER
INLET
sta453
sta551
TEST SECTION
FIRE EXTINGUISHING AGENT INJECTION
POOL FIRE THREAT
SPRAY FIRE THREAT
/ | MPSHRe Outcome (%v/v)
CF3I | 7.1
HFC-125 | 17.6
FK-5-1-12 | 6.1
MSSI Blend A | 30.6
halon 1301 | 6 ( per FAA AC 20-100, not the MPSHRe )
Fire
Extinguishing
Agent

## Slide 32: Measured the Flammability Envelope of Hydrogen, Air and Halon 1301 Mixtures
Chart: %vol Halon 1301
| 0 | 10 | 20 | 25 | 26 | 26.72
LFL | 4.95 | 9.02 | 11.55 | 13.47 | 14.75 | 16.2
UFL | 76.52 | 45.7 | 28.39 | 19.34 | 17.85 | 16.2
Chart: %vol Halon 1301
| 0 | 10 | 20 | 25 | 26 | 26.72
LFL | 4.95 | 9.02 | 11.55 | 13.47 | 14.75 | 16.2
UFL | 76.52 | 45.7 | 28.39 | 19.34 | 17.85 | 16.2
Nonflammable | 21.9861 | 20.2449 | 19.3859 | 13.0102 | 12.0249 | 16.4082 | 15.0619 | 14.2804 | 18.0245 | 14.2576 | 17.9611 | 16.4719 | 16.1973 | 15.7106 | 16.7358
Flammable | 18.0108 | 14.0147 | 13.5142 | 16.4111 | 16.2635 | 16.1927

## Slide 33
Burner Actuator
Blow-out panels
H2 Analyzer
Camera
Bunsen Burner
Test sample
Igniters
Chart: 1/16" Woven Carbon Fiber
| 0 | 0 | 0 | 3.15E-2 | 3.1649999999999998E-2 | 3.4099999999999998E-2 | 3.9849999999999997E-2 | 3.925E-2 | 4.02E-2 | 2.1000000000000001E-2 | 2.0049999999999998E-2 | 2.0899999999999998E-2 | 1.06E-2 | 1.0800000000000001E-2 | 1.085E-2
Flame Time | 43 | 39 | 38 | 213 | 193 | 202 | 172 | 181 | 169 | 204 | 165 | 208 | 142 | 192 | 170
FT Fail | 15 | 15
Burn Length | 0.7 | 0.6 | 0.6 | 11.9 | 11.7 | 11.7 | 11.7 | 11.4 | 11.6 | 10.5 | 9.2 | 10.7 | 4.8 | 5.5 | 7.3
BL Fail | 8 | 8
Examined the Flammability of Materials in a Low-Concentration Hydrogen Environment (<LFL)

## Slide 34: Conducted Destructive Testing of Fuel Cells to Determine Consequences of Failure Modes

## Slide 35: Examined the Oxygen Depleted Air (ODA) By-Product from a Fuel Cell for Cargo Compartment Fire Suppression in a 737

## Slide 36: www.fire.tc.faa.gov