## Slide 1: Measuring toxic potency of smoke over a range of fire stages using milligram samples
Louise C. Speitel, Richard N. Walters, Natallia Safronava, & Richard E. Lyon
Federal Aviation Administration, Fire Safety Branch
http://www.fire.tc.faa.gov
9thTriennial Cabin Fire and Cabin Safety Conference
Atlantic City, NJ
October 28 - 31, 2019

## Slide 2
  Make conditions of micro combustion calorimeter (MCC) similar to the physical/chemical processes of flaming combustion by varying the fuel/oxygen ratio relative to stoichiometric (Φ) and increasing the combustor temperature to the range of flame temperatures, TF = 1300⁰C-1800⁰C.
  This MCC methodology combined with analysis of combustion products is hoped to be a valuable tool in combustion toxicity assessments for aircraft materials and commercial/residential furnishings over a range of fire stages from initiation to flashover.
Motivation

## Slide 3
  Upgrade the MCC combustion furnace to reach flame temperatures.
  Upgrade the FTIR method .
  Hold the equivalence ratio, Φ , and combustion temperature constant over the entire constant heating rate pyrolysis history.
  Run selected materials in the MCC-Φ with:
    Combustor Temperatures, Tc = 750⁰C, 1000⁰C, 1250⁰C and 1500⁰C
    Constant Φ = 0.5 to 1.75 (fuel lean to fuel rich).
Evaluate the gaseous combustion products as a function of Tc and Φ using FTIR and gas analyzers.
Strategy

## Slide 4
Fuel / Oxygen Ratio in MCC

## Slide 5
Specific Heat Release Rate, Q, and Φ in the Standard Test
(ASTM D7309)
In contrast, in MCC-Φ, the equivalence ratio is held constant (square wave shape)

## Slide 6
MCC-Φ (Constant Φ):
Fuel / O2 Control and Measurement
Pyrolysis
(Ramp T)
Pyrolyzer
Cold Trap
Flow
Meter
O2
Analyzer
O2
N2
Sample
Exhaust
Premixed
Combustion
(Constant T)
CO2
CO

750C - 1500 C
DAQ
Pyrolyzer
Desiccant
Flow
Meter
O2
Analyzer
O2
N2
Sample
Exhaust
CO2
CO
Computer controls MFCs maintaining constant 

(Up to 1600C)
DAQ

## Slide 7: Schematic MCC-Φ-FTIR
Pyrolysis
(Ramp T)
Pyrolyzer
O2, CO2, CO
Analyzers
O2
N2
Sample
Exhaust
Premixed
Combustion
(Constant T)
Control From Look-up Table Maintaining Constant 

(up to 1600 C)
DAQ
Heated
Line
(165 C)
Filter
(160 C
Tube oven)
FTIR
90 ml cell
(170  C)
0.5 cm-1 resolution
Desiccant
Filter
Notes: FTIR and gas analyzers run concurrently to check quantification accuracy.

## Slide 8: Ultra High Temperature Combustion Furnace
Combustor temperatures within the range of flame temperatures,
TF = 1300⁰C-1800⁰C
Run combustor at temperatures:
  750⁰C
  1000⁰C
  1250⁰C
  1500⁰C

## Slide 9
Spectral Regions for Combustion Gases: Method
CO
NO2
CO2
NO
HCN
SO2
N2O
COS
H2O
CS2
C2H2
CH4
C2H6
C2H4
C3H8
C6H5OH
Wavenumbers (cm-1)
Absorbance
Notes: All spectra shown are for maximum calibration concentrations
Up to 32 spectra are included in the method for some gases eg.) CO2:
Nonlinear calibration curves
Normalized spectra changing shapes
Each region must start or end at the baseline ( Zero absorbance)

## Slide 10
Spectral Regions for Combustion Gases: HCN and C2H2
Notes: Each region must start or end at the baseline

## Slide 11
CO Yields in the MCC- Φ by NDIR
Chart: PMMA
| 0.5 | 1 | 1.5
750°C (smouldering) | 0.649 | 0.64 | 0.521
1000°C | 0.003 | 0.0872 | 0.8166
1250°C | 0.001 | 0.119 | 0.847
1500°C | 0.01 | 0.082 | 0.78583
Chart: PS
| 0.5 | 1 | 1.5
750°C | 0.979 | 0.989 | 0.775
1000°C | 0.004 | 0.1466 | 1.4498
1250°C | 0.001 | 0.154 | 1.249
1500°C | 0.001 | 0.101 | 1.0008
Chart: PA66
| 0.5 | 0.75 | 1 | 1.25 | 1.5 | 1.75
750°C | 0.367 | 0.703 | 0.769 | 0.649 | 0.567 | 0.461
1000°C | 0.006 | 0.01 | 0.0536 | 0.434 | 0.6688 | 0.956
1250°C | 0.002 | 0.002 | 0.0635 | 0.4 | 0.662 | 0.804
1500°C | 0.001 | 0.001 | 0.0674 | 0.474 | 0.7624 | 0.884
Chart: PPS
| 0.5 | 0.75 | 1 | 1.25 | 1.5 | 1.75
750°C | 0.39 | 0.331 | 0.281 | 0.253 | 0.216 | 0.196
1000°C | 0.009 | 0.015 | 0.1648 | 0.437 | 0.4252 | 0.414
1250°C | 0.001 | 0.036 | 0.211 | 0.486 | 0.521 | 0.535
1500°C | 0.001 | 0.023 | 0.0886 | 0.293 | 0.4158 | 0.482
Notes: Yields

## Slide 12
CO2 Yields in the MCC- Φ by NDIR
Chart: PMMA
| 0.5 | 1 | 1.5
750°C (smouldering) | 0.778 | 0.214 | 0.177
1000°C | 2.139 | 1.9458 | 0.7734
1250°C | 2.203 | 1.921 | 0.939
1500°C | 2.128 | 1.969 | 0.90767
Chart: PS
| 0.5 | 1 | 1.5
750°C | 1.08 | 0.13 | 0.086
1000°C | 3.362 | 3.092 | 0.969
1250°C | 3.416 | 3.106 | 1.46
1500°C | 3.321 | 3.1894 | 1.52
Chart: PA66
| 0.5 | 0.75 | 1 | 1.25 | 1.5 | 1.75
750°C | 1.281 | 0.536 | 0.343 | 0.193 | 0.151 | 0.14
1000°C | 2.115 | 2.169 | 2.02 | 1.3998 | 0.8222 | 0.518
1250°C | 2.227 | 2.223 | 2.064 | 1.423 | 0.975 | 0.67
1500°C | 2.15 | 2.134 | 2.034 | 1.317 | 0.8996 | 0.656
Chart: PPS
| 0.5 | 0.75 | 1 | 1.25 | 1.5 | 1.75
750°C | 0.147 | 0.107 | 0.096 | 0.073 | 0.097 | 0.082
1000°C | 1.077 | 1.012 | 0.6964 | 0.309 | 0.2026 | 0.171
1250°C | 1.09 | 1.03 | 0.783 | 0.48 | 0.326 | 0.229
1500°C | 1.066 | 1.007 | 0.8602 | 0.621 | 0.4758 | 0.418

## Slide 13
CO2/CO Yield Ratios in the MCC- Φ by NDIR
Chart: PS
| 0.5 | 1 | 1.5
MCC 750ºC | 1.1 | 0.13 | 0.11
MCC 1000ºC | 841 | 21 | 0.67
MCC 1250ºC | 3416 | 20 | 1.2
MCC 1500ºC | 3321 | 32 | 1.5
Chart: PMMA
| 0.5 | 1 | 1.5
750ºC | 1.2 | 0.33 | 0.34
1000ºC | 713 | 22 | 0.95
1250ºC | 2203 | 16 | 1.1
1500ºC | 213 | 24 | 1.2
Chart: PA66
| 0.5 | 0.75 | 1 | 1.25 | 1.5 | 1.75
MCC 750ºC | 3.5 | 0.76 | 0.45 | 0.3 | 0.27 | 0.3
MCC 1000ºC | 353 | 217 | 38 | 3.2 | 1.2 | 0.54
MCC 1250ºC | 1114 | 1112 | 33 | 3.6 | 1.5 | 0.83
MCC 1500ºC | 2150 | 2134 | 30 | 2.8 | 1.2 | 0.74
Chart: PPS
| 0.5 | 0.75 | 1 | 1.25 | 1.5 | 1.75
MCC 750ºC | 0.38 | 0.32 | 0.34 | 0.29 | 0.45 | 0.42
MCC 1000ºC | 120 | 67 | 4.2 | 0.71 | 0.48 | 0.41
MCC 1250ºC | 1090 | 29 | 3.7 | 0.99 | 0.63 | 0.43
MCC 1500ºC | 1066 | 44 | 9.7 | 2.1 | 1.1 | 0.87

## Slide 14
Yields of COx Normalized for the Theoretical
COx Maximums at 1000⁰C, 1250⁰C and 1500⁰C

## Slide 15
Chart: SO2*
| 0.5 | 0.75 | 1 | 1.25 | 1.5 | 1.75

750°C (smouldering) | 392.9806 | 400.3127 | 390.3701 | 374.8452 | 365.3217 | 364.6201

1000°C | 379.819 | 422.6638 | 394.3211 | 396.6968 | 397.5889 | 427.1727

1250°C | 410.9027 | 409.6652 | 369.6839 | 358.7958 | 393.0411 | 337.9774

1500°C | 412.8419 | 412.7125 | 381.0678 | 394.9689 | 441.591 | 328.641

Chart: COS
| 0.5 | 0.75 | 1 | 1.25 | 1.5 | 1.75

750°C (smouldering) | 6.6762 | 6.315 | 6.4062 | 6.5998 | 6.617 | 6.591

1000°C | 0 | 0 | 0.014639 | 0.46151 | 0.55992 | 0.48622

1250°C | 3.5953 | 5.2608 | 5.0657 | 0.22282 | 0.49478 | 2.0628

1500°C | 1.0832 | 0.58951 | 6.9752 | 8.834 | 8.8924 | 10.3372
Chart: CS2
| 0.5 | 0.75 | 1 | 1.25 | 1.5 | 1.75

750C | 3.797 | 4.1625 | 4.8604 | 5.4601 | 6.0858 | 6.7903

1000C | 0 | 0 | 1.1795 | 6.5408 | 7.2706 | 0.68583

1250C | 11.8289 | 24.3168 | 33.6288 | 0 | 0 | 0

1500C | 0 | 0 | 0.048599 | 0 | 0 | 0
MCC-Φ Yields of SO2, COS, and CS2 by FTIR for PPS
* Maximum theoretical SO2 yield = 592g/kg

## Slide 16
Chart: HCN*
| 0.5 | 0.75 | 1 | 1.25 | 1.5 | 1.75

750C | 60.9638 | 109.2383 | 116.178 | 111.61 | 102.5308 | 96.7718

1000C | 0 | 0 | 6.4567 | 60.9318 | 81.3499 | 125.9156

1250C | 0 | 0 | 8.2619 | 67.2648 | 99.7219 | 139.0038

1500C | 0 | 0 | 0 | 0 | 8.339 | 31.7628
Chart: N2O
| 0.5 | 0.75 | 1 | 1.25 | 1.5 | 1.75







PHI

750C N2O
750C | 45.2013 | 32.5941 | 22.122 | 19.3949 | 16.9956 | 15.6452

Chart: NO
| 0.5 | 0.75 | 1 | 1.25 | 1.5 | 1.75







PHI

750C N2O


MCC-Φ Yields of HCN, N2O, and NO by FTIR for PA66
* Maximum theoretical HCN yield = 239g/kg
Notes: High levels of HCN at 750C for all phis (smoldering)
Lowest HCN levels at 1500C
No NO2 detected.
NO2 Limit of detection high due to NO2 absorbing in spectral area with a lot of water.

## Slide 17
Gas Yields in Vitiated Small/ Full/ Bench Scale: Nylon 66
Chart: HCN
| 0.5 | 0.75 | 1 | 1.25 | 1.5 | 1.75 | 2
750C | 61 | 109.2 | 116.2 | 111.6 | 102.5 | 96.8
1000C | 0 | 0 | 6.5 | 60.9 | 81.3 | 125.9
1250C | 0 | 0 | 8.3 | 67.3 | 99.7 | 139
1500C | 0 | 0 | 0 | 0 | 8.3 | 31.8
ISO Room 1/3 scale
ISO Room | 0.05 | 3.5 | 11 | 40
FPA
Steady-State Tube Furnace | 0 | 0 | 3.5 | 20 | 35 | 47.5 | 62
Chart: CO
| 0.5 | 0.75 | 1 | 1.25 | 1.5 | 1.75 | 2
750C | 367 | 703 | 769 | 649 | 567 | 461
1000C | 6 | 10 | 53.6 | 434 | 668.8 | 956
1250C | 2 | 2 | 63.5 | 400 | 662 | 804
1500C | 1 | 1 | 67.4 | 474 | 762.4 | 884
ISO Room 1/3 scale | 30 | 70 | 110 | 270 | 430
ISO Room | 10 | 15 | 40 | 120
Steady-State Tube Furnace (ISO TS 19700 & BS 7990) | 10 | 10 | 40 | 90 | 135 | 210 | 275


FPA (ASTM E2058) predicted | 38 | 41.6517 | 150.2923 | 418.355 | 690.2085 | 896.0246 | 1038.8502


A. Stec & R. Hull, Fire Toxicity, 2010
A. Tewarson, The SFPE Handbook of Fire Protection Engineering, Sec.3, Ch. 4., 2008

## Slide 18
CO, CO2, and HCN Variance for PA66 in MCC-Φ at 1000C
Chart: CO +/- 1σ
| 1 | 1.25 | 1.5
Test #
CO MCC | 53.6 | 434 | 668.8
CO FTIR 1.69m
CO FTIR 2m
CO FTIR Peak, % 1.69m
CO2 FTIR 1.69m
CO2 Peak, %
CO2 FTIR 2m

Chart: CO2 +/- 1σ
| 1 | 1.25 | 1.5
Test #
CO FTIR 1.69m
CO FTIR 2m
CO FTIR Peak, % 1.69m
CO2 MCC | 2020 | 1399.75 | 822.2
CO2 FTIR 1.69m
CO2 Peak, %
CO2 FTIR 2m

Chart: HCN +/- 1σ
| 1 | 1.25 | 1.5
Test #
CO FTIR 1.69m
CO FTIR 2m
CO FTIR Peak, % 1.69m
CO2 FTIR 1.69m
CO2 Peak, %
CO2 FTIR 2m
HCN | 6.4567 | 60.9318 | 81.3499


## Slide 19: Yields of CO2 and Water at 1500⁰C Relative to Theoretical Yield in Excess Oxygen (Φ= 0.5)
Sample | CO2 Analyzer | CO2 FTIR | Water FTIR
PMMA | 0.97 | 0.97 | 1.02
PS | 0.98 | 0.89 | 0.81
PA66 | 0.92 | 0.97 | 0.86
PPS* | 0.44 | 0.42 | 0.90
*Does not account for carbon in char

## Slide 20
Φ= 0.5 1 1.5 0.5 1 1.5 0.5 1 1.5 0.5 1 1.5
Arrows indicate large FTIR errors
Comparison of CO Yields: NDIR and FTIR for PMMA
Notes: Large FTIR errors are seen as indicated at 1.5 phi at 1000 and 1250 deg C

## Slide 21
Comparison of Normalized CO Spectra for PMMA
Large
Yield
Errors
1.0 +/- 0.15 percent CO
Wavenumbers (cm-1 )
Notes: Frequencies wobble back and forth within 19 days
The resultant errors are not acceptable
A more robust method is needed:

## Slide 22
Comparison of CO Normalized Spectra for PMMA
MCC and Calibration Spectra: 200 +/- 20ppm
Significant shifting observed
Wavenumbers (cm-1 )

## Slide 23
CO Normalized Spectra at High and Low Resolution
0.5 cm-1
2 cm-1
1083 ppm CO
Wavenumbers (cm-1 )
Notes: CO accuracy will be improved for wobbly spectra by decreasing the resolution from 0.5 to 2 cm.

## Slide 24
1083ppm CO Spectra at High and Low Resolution
Wavenumbers (cm-1 )
0.5 cm-1
2 cm-1
Normalized
Notes: Collecting spectra at a lower resolution (2cm-1) will minimize interferometer frequency shifting errors.
Advantages of high resolution (0.5 cm-1): better spectral discrimination (better discrimination, less likely to misidentify gases)
For our instrument, high 0.5 cm-1 is a disadvantage due to shifting (wobbly) spectra:
More likely to misidentify gas
Intermittant large quantification errors.
2 cm-1 should provide a more robust method.
Gases that will markedly benefit include H20, CO, HCN, HF, HCl, HBr, NO, CH4 and C2H2

## Slide 25: Conclusion
MCC- Φ at a range of combustion temperatures (Tc) and fuel/oxygen ratios (Φ) is a viable tool for generating gaseous and solid combustion products for various stages of fires.
The CO/CO2 ratio, FTIR gas analysis and gravimetric soot measurements determine which MCC test conditions best reproduce flaming combustion.
The FTIR interferometer at a resolution of 0.5 cm-1 has an intermittent frequency wobble causing significant intermittent errors for CO…….
 C  C

## Slide 26: Future Work
Run future MCC-Φ tests with FTIR resolution set to 2 cm-1 to improve quantification accuracy and robustness of the method, where shifting frequencies up to 0.25 cm-1 do not cause a problem.
Run more materials in the MCC-Φ.
Calculate the toxic potency of smoke from burning polymers over the entire range of fire conditions from early stage (over ventilated) to late stage (vitiated) for various combustor temperatures.
Determine whether flame retardants increase the toxic potency of combustion products.
Evaluate the use of solid state metal oxide sensors for NO, NO2 and SO2 etc. to supplement/ replace FTIR analysis of combustion gases.