## Slide 1: Effects of Thermal Conductivity on Flame Spread over Carbon-fiber Composites
Haiqing Guo1, Richard Walters2, Richard Lyon2, James Quintiere3, Sean Crowley2
1 C-FAR Services, USA
2 Fire Safety Branch, FAA William J. Hughes Technical Center, USA
3 Dept. of Fire Protection Engineering, Univ. of Maryland, USA
9th Triennial International Fire & Cabin Safety Research Conference
Oct 29 – 31, 2019
Atlantic City, NJ

## Slide 2: Background
Carbon fiber-reinforced polymer structural composite is widely used in commercial airplanes (high strength-to-weight ratio).
The polymeric binder (epoxy resin) is flammable. Fire in the inaccessible areas of an airplane is hazardous to in-flight safety.
In 2013, a composite fuselage Boeing 787 experienced a battery fire in the overhead space that propagated along the crown of the airplane.

## Slide 3: Background
In-plane thermal conductivity is about one magnitude larger than the in-depth thermal conductivity*.
While the upward flame spread is more dominated by the flame radiation, the downward flame spread is anticipated to be affected by the high in-plane thermal conductivity.
*McKinnon et al., 2016, Journal of Fire Science 35(1), pp.36-61.
Material:
  Material: 3KPW/TCR (3K plain weave fiber pre-impregnated with TCR resin.
  Three thickness: 4 ply (0.9 mm), 8 ply (1.8 mm), 16 ply (3.5 mm).

## Slide 4: Pyrolysis Kinetics
TGA tests in N2 at heating rates of: 1, 3, 10, and 30 ˚C/min
Residual: 69.7 ± 0.8 %.
ASTM E1641: E = 163 kJ / mol, and A = 2.76×1010 s-1. @ 5% mass conversion
Ignition T: 403 ˚C (based on 1.2 mg/g-s mass flow at 30 ˚C/min heating rate*)
*Lyon, R.E., Safronava, N., Crowley, S., 2018, Fire and Materials 42(6), pp.668-679.

## Slide 5: Heat Release
MCC (ASTM D7309)
  MCC: 1 ˚C/s heating rate (ASTM D7309).
  Peak HRR: 100 W/g at 440 ˚C.
  Heat of combustion (13.1 kJ/g-O2): 7.8 kJ/g initial sample, or 24.8 kJ/g volatile.
Cone (ASTM E1354)
  Heat flux: 16 ply composite at 20, 22.5, 25, 35, 50, 75, and 95 kW/m2.
  No ignition below 20 kW/m2.
  Separation of peaks at higher radiant heat flux.

## Slide 6: Ignition
Simultaneous ignition happens above 20 kW/m2.
Flame spread is anticipated below the critical heat flux.
Small difference is expected due to the difference in boundary condition and ignition source.

## Slide 7: Downward Flame Spread Diagram
Cone heater is used as external heat flux.
Ignitor: Premixed propane/air flame. (Ignites at Ts = 250 ˚C).
Mask (metal + ceramic paper) to avoid delamination and edge burning.

## Slide 8: Flame Spread
16 ply composite @ 22.5 kW/m2.
Steady state flame spread rate is calculated.
Highly parabolic flame front, indicating in-plane heat loss laterally.

## Slide 9: Flame Spread Rate
Heat fluxes: 20, 22.5, 25 kW/m2.
Flame spread rate ranges between 0.1 – 1.8 mm/s in the explored region.
Spread rate increases drastically as thickness decreases.

## Slide 10: 2-D Model
2-D downward flame spread model based on classic pure conduction theory.
  Assume steady state and thermally thin.
  Conductive heat loss in y-axis (both direction) comparable to that in x-axis.

## Slide 11: Normalized Flame Spread Rate
kx and ky is assumed about 10 times higher than the kz.
In-plane k effect becomes negligible when the sample is thin or the external heat flux is high, the ability of heat to penetrate the sample is dominating.

## Slide 12: Summary and Future Work
The flammability of a specific carbon fiber-reinforced epoxy composite 3KPW/TCR type is researched in this study.
The composite composes primarily carbon fiber (~ 70%) and the overall heat of combustion is as low as 7.8 kJ/g.
The relatively high ignition temperature and low critical heat flux does not leave much space for a steady downward flame spread study.
Downward flame spread on carbon fiber composite surface is studied at external heat fluxes between 20 – 25 kW/m2.
The flame spread rate was measured between a range of 0.1 – 1.8 mm/s.
In conditions where unconfined boundary exists and the heat also conducts laterally in-plane, the extra heat loss creates a parabolic flame front shape, and inhibits the flame spread rate.
In the future, the 3-aixs thermal conductivity needs to be accurately measured and a more detailed numerical model needs to be done.