## Slide 1: The Ninth Triennial International Fire & Cabin Safety Research Conference
28-31 October 2019
Greg Roberts
Northrop Grumman Corp.
Aerospace Systems
Concerns with Baseline Fire Barrier Recommendations of FAA AC 20-135

## Slide 2: Fire Barrier Requirements

## Slide 3: What Is A Fire Zone?
MIL-HDBK-221
  Compartments which contain flammable fluid components with potential leakage, and, potential ignition sources, if the following applies:
    One “single failure” can cause a fire or explosion. A combustor and turbine compartment is in this category if it contains external flammable fluid lines with leakage potential as well as an unprotected engine case hot enough to ignite the flammable fluid, or when a combustor burn through can cause leakage from the flammable fluid lines.
    A dual failure is needed to cause ignition, but the flammable fluid components and potential ignition sources are not sufficient~ separated and shielded, or are present in high concentration, so that contact of flammable fluid and vapor with ignition sources by gravity, ventilation airflow or squirt is likely. Accessory sections of engines are, and hydraulic and fuel service centers may be in this category
Similar to Definitions in JSSG 2009 and AC 20-135

## Slide 4: Where Is A Fire Zone
External fire zones
  Hanging from wing
    Engine Bays
      Commercial jets
  Fire barrier backside temperature cooled by surrounding airflow
Internal fire zones
  Internal to fuselage
    Engine Bays
      Modern Military Jets
      Conceptual Commercial Jets
      Auxiliary Power Units
        Commercial Jets
        Military Jets
  Fire barrier backside temperature transmitted to surrounding structure and adjacent bays
Internal Fire Zones Are Common On Military Aircraft

## Slide 5: External Fire Zones
Photo: Honest Version – Global Engine Nacelle Market 2019: Industry Growth, Size, Share and Analysis 2025
Photo: Airline world – WordPress.com

## Slide 6: Internal Fire Zones
Photo US Navy - Released
Photo: B-2 Stealth Bomber (@Whiteman AFB) | Twitter
Photo: Popular Mechanics
Photo: uaminc.blogspot.com

## Slide 7: Fire Barrier Requirements
Fire Barrier shall be fireproof
  Temperature = 2000°F
  Heat Flux Density > 9.3 BTU/ft2 sec.
  Time = 15 minutes
Previously Tested, Known Materials
  Stainless steel sheet, .015 inch thick.
  Mild steel sheet protected against corrosion, .018 inch thick.
  Titanium sheet, .016 inch thick.
  Monel metal sheet, .018 inch thick
  Steel or copper base alloy firewall fittings/fasteners
Fire Zones Are Contained By Fire Barriers

## Slide 8: Fire Barrier Testing
Photo: NGC Fire Barrier Test Stand - Courtesy Area 67

## Slide 9: Backside Temperatures – Graphite/Epoxy 0.25”Thick
Flame Temp
Jet A AI
Jet A MHSIT

## Slide 10: Backside Temperatures – 7075-T6 0.125” Thick
Photo: NGC Fire Barrier Test Stand - Courtesy Area 67
Photo: NGC Fire Barrier Test Stand - Courtesy Area 67

## Slide 11: Fire Barrier Testing
Observations
  The graphite/epoxy samples neither burned through nor experienced a backside fire resulting from a 15 minute exposure to the fire
  In all cases, the backside thermocouple data exceeded the autoignition temperature of the fuel
  In some cases, the backside thermocouple data exceed the minimum hot surface ignition temperature of the fuel

## Slide 12: Recommendations
When updating AC 20-135, consider/examine effects of internal fire zone backside temperature on adjacent bays with:
  Temperature sensitive primary structure
    Graphite/Epoxy Composite
  Flammable Contents (Flammable Zones)
  Flammable Leakage (Flammable Leakage Zone)