## Slide 1: UN Battery Classification Test Method Development and Testing

## Slide 2: Introduction
Currently all lithium batteries are classified as either lithium-ion or lithium metal
All lithium-ion or lithium metal batteries are not created equal
New classifications take into account actual hazards:
  Propagation
  Fire
  Gas Hazard
  Temperature Hazard

## Slide 3: Lithium Battery Classification
By Default, no testing will be required, all hazards would be considered worst case with common chemistry
Purpose of this testing is to determine worst case as well as developing test methods for individual batteries to be classified on their own
  Gas Volume Test (all gas emitted is assumed to be toxic)
  Propagation Test
  Flammability and temperature hazard determined in one of these tests

## Slide 4: Battery Gas Volume Measurements
Single cell placed in 21.7L pressure vessel and heated until thermal runaway
Instrumented with pressure transducers and thermocouples for heater, battery, and ambient air
Chamber is evacuated with vacuum pump, then filled with nitrogen at atmospheric pressure
Battery gas volume is calculated from temperature and pressure measurements
All cells at 100% SOC

## Slide 5: Battery Gas Volume Measurements
Chart: Battery Temperature (18650 @ 20°C/min)
Heating rate controlled with temperature controller
Cells heated at rates of 5°C, 10°C, and 20°C per minute
Example shows an 18650 cell heated at 20°C/min

## Slide 6: Battery Gas Volume Measurements
Chamber pressure and temperature data from same test
Calculated amount of gas (in moles) using ideal gas law
Converted to liters of gas at NIST normal temperature and pressure (NTP – 20°C and 1 atm)
This test produced 3.39L of gas
Chart: Chamber Pressure and Temperature
Initial pressure and temperature
Final pressure and temperature

## Slide 7: Battery Gas Volume Measurements
Repeated tests 3 times to get repeatability data for two cells
2600 mAh 18650:
2400 mAh 18650:
Chart: 2600 mAh 18650 Cell Repeatability
| 5°C/min | 10°C/min | 20°C/min
Test 1 | 3.3363 | 3.5582 | 3.4256
Test 2 | 3.3578 | 3.9422 | 3.3217
Test 3 | 3.4415 | 3.592 | 3.5282
 | 5°C/min | 10°C/min | 20°C/min
Average | 3.38 | 3.70 | 3.43
Std. Dev. | 0.06 | 0.21 | 0.10
% Std. Dev. | 1.64% | 5.75% | 3.02%
 | 5°C/min | 10°C/min | 20°C/min
Average | 3.19 | 3.25 | 3.29
Std. Dev. | 0.13 | 0.12 | 0.30
% Std. Dev. | 3.92% | 3.63% | 9.03%

## Slide 8: Battery Gas Volume Measurements
Tested 25 lithium-ion cells
  Size from AAA to large pouches
  LCO, NMC, LFP, LTO, LMN chemistries
Tested 10 lithium metal cells
  Size AAA, CR2, to 17500
  LiFeS2, LiMnO2, LiSOCl2 chemistries
Lithium-ion batteries tested
Lithium metal batteries tested

## Slide 9: Battery Gas Volume Measurements
Lithium-ion cells only
Comparing highest volume measured from each cell
Chart: Lithium-Ion Gas Volume Comparison
| 8.8800000000000008 | 9.6 | 5.18 | 2.96 | 1.8 | 1.2949999999999999 | 2.59 | 1.96 | 3.7 | 14.4
LCO | 3.29 | 3.6975 | 2.3832 | 1.2986 | 0.55622 | 0.57732 | 1.0005 | 0.50035 | 1.7415 | 6.4807
NMC | 4.4023 | 5.187 | 6.3394
LFP | 0.40789 | 0.38061 | 0.6179 | 1.0408 | 2.2574 | 1.963
LTO | 2.2221
Chart: Lithium-Ion Gas Volume Comparison
| 8.8800000000000008 | 9.6 | 5.18 | 2.96 | 1.8 | 1.2949999999999999 | 2.59 | 1.96 | 3.7 | 14.4 | 37 | 37
LCO | 3.29 | 3.6975 | 2.3832 | 1.2986 | 0.55622 | 0.57732 | 1.0005 | 0.50035 | 1.7415 | 6.4807 | 21.8726 | 21.1024
NMC | 4.4023 | 5.187 | 6.3394 | 19.2181
LFP | 0.40789 | 0.38061 | 0.6179 | 1.0408 | 2.2574 | 1.963 | 6.5354
LTO | 2.2221
LMN | 13.6528

## Slide 10: Battery Gas Volume Measurements
Lithium metal cells only
Comparing highest volume measured from each cell
Chart: Lithium-Metal Gas Volume Comparison
| 4.6500000000000004 | 4.6500000000000004 | 4.5 | 2.5499999999999998 | 8.6999999999999993
LiMnO2 | 1.6276 | 1.526 | 2.5954 | 1.0735 | 4.1741
LiFeS2 | 1.0913 | 0.84141 | 0.41732
LiSOCl2 | 3.556
LiSO2 | 2.6677

## Slide 11: Battery Gas Volume Measurements
Highest was LTO 18650 at 0.71 L/Wh
Highest LCO was 10,000 mAh pouch cell at 0.59 L/Wh
Highest LFP was AA at 0.32 L/Wh

## Slide 12: Battery Gas Volume Measurements
Highest was LiMnO2 CR123A at 0.58L/Wh

## Slide 13: Battery Propagation Testing
6 cells placed in a line in an insulated box to determine if thermal runaway will propagate down the line
Cell #1 heated at 20°C/min until thermal runaway occurs, then heater is turned off
Thermocouple placed on each cell to measure temperature
Top of box is vented to allow gas to escape
Spark ignitor placed 3 inches above the box
  To determine if gas is flammable
  Ignitor turned off after first cell goes into thermal runaway
All cells at 100% SOC
Tested 17 Li-ions and 14 Li metals so far

## Slide 14: Battery Propagation Testing
Notes: Video starts 7:39 after start of test

## Slide 15: Battery Propagation Testing
Tested repeatability for two sets of cells, both AA (14500) size
LiCoO2 cell propagated with very repeatable test results
Chart: LCO 14500 Battery Propagation Test 1
Chart: LCO 14500 Battery Propagation Test 2
Chart: LCO 14500 Battery Propagation Test 3
Time between cells: Avg.: 95.8s
Std. Dev.: 12.9%
Avg.: 87.4s
Std. Dev.: 15.1%
Avg.: 92.0s
Std. Dev.: 15.7%

## Slide 16: Battery Propagation Testing
LiFePO4 cell did not propagate
Second cell vented for all three tests
Chart: LFP 14500 Battery Propagation Test 1
Chart: LFP 14500 Battery Propagation Test 2
Chart: LFP 14500 Battery Propagation Test 3

## Slide 17: Battery Propagation Testing
All LCO cells propagated except AAA size
No LFP cells fully propagated
All cells produced flammable gas
Chart: Propagation Testing of Various Cells
| LiCoO2 18650 | LiCoO2 18650 | LiCoO2 18500 | LiCoO2 AA | LiCoO2 14430 | LiCoO2 1.96Wh Pouch | LiCoO2 9V | LiCoO2 AAA | LiCoO2 AAA | Li2TiO3 18650 | LiFePO4 AA | LiFePO4 AA | LiFePO4 RCR123A | LiFePO4 18650 | LiFePO4 32600 | LiFePO4 26650 | LiFePO4 32Wh Pouch
 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 0 | 0 | 5 | 0 | 0 | 0 | 0 | 0 | 0 | 1

## Slide 18: Battery Propagation Testing
LiFeS2 propagated at AA size for one brand, not AAA
All cells produced flammable gas except LiSO2
Small CR2430 button cell propagated (0.855 Wh)
Chart: Propagation Testing of Various Cells
| LiFeS2 AA | LiFeS2 AA | LiFeS2 AAA | LiMnO2 CR123A | LiMnO2 CR123A | LiMnO2 CR123A | LiMnO2 CR2477 | LiMnO2 CR2477 | LiMnO2 CR2 | LiMnO2 17500 | LiMnO2 CR2430 | LiMnO2 CR2430 | LiSOCl2 17500 | LiSO2 G36/2
 | 5 | 0 | 0 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 5 | 0 | 0 | 0

## Slide 19
LiSOCl2 17500 Cells
Exploded at ~175°C

## Slide 20: Conclusion and Future Work
Battery gas volume increases with battery capacity in lithium-ion and lithium metal cells
  Different chemistries produce different L/Wh measurements
Battery propagation test works well for testing propagation and flammability
  Ignitor placed above cell #1 always ignited flammable gases
  Cells must be secured in box
Future testing includes multi-cell batteries

## Slide 21: Questions?
Contact:
Steven Rehn
Federal Aviation Administration
William J. Hughes Technical Center
Fire Safety Branch, Bldg. 203
Atlantic City Int’l Airport, NJ 08405
(609) 485-5587
steven.rehn@faa.gov