## Slide 1: Development of a Laboratory Scale Flame Propagation Test Method for Structural Composites

## Slide 2: Review from Singapore
Intermediate scale tests were performed on aerospace grade structural composite material of varying thickness
  4, 8, 16, 24, 32 plies and a honeycomb sandwich panel
  Various configurations were tested
    Exposed backside
    Insulated backside
    Water-cooled backside
  Backside heat loss found to have a significant effect on inboard-side burning

## Slide 3: Lab-Scale Test Method Development
The foam block fire source was characterized by measuring the heat flux gradient along an insulated board for the duration of the foam burning event
This heat flux gradient will then be used to impose a similar heat flux on a smaller sample in a lab-scale test apparatus

## Slide 4: Heat Flux Gradient – Intermediate Scale

## Slide 5: Vertical Radiant Panel (VRP) Development
Objective: to develop a “new” radiant panel type test that will:
  Simulate conditions of a foam block test
    Incident heat flux on sample
    Duration
    Geometry
  Correlate results from foam block test
    Use current database of materials already tested
      Aerospace/non-aerospace grade composites (1/8” thick)
      Aerospace grade carbon epoxy, varying thicknesses
      Cargo liners and floor panels, varying thicknesses

## Slide 6
Radiant Panel Heater
Calorimeter Board
3.2
1.36
.54
.18

## Slide 7
VRP Configuration
Heat flux gradient
  A tilted panel was used to attempt to achieve the same measured gradient as the foam block test
  Furthest backward tilt (70°) could not achieve steep enough gradient
  Zero position heat flux too low
Next attempt:
  Separate emitter strips into 3 individually controlled pairs to control the heat flux gradient

## Slide 8
Leg 1
Leg 2
Leg 3
Current Configuration
New Configuration
Temp
Controller
Relay
Temp
Controller 1
Relay 1
Temp
Controller 2
Relay 2
Temp
Controller 3
Relay 3
3-Phase 208V in

## Slide 10
Radiant Panel Heater
Radiant Panel Heater
Radiant Panel Heater
Calorimeter Board
3.2
1.36
.54
.18

## Slide 11
Bottom 2 Strips Only

## Slide 12: Recent research

## Slide 13: Modifications to VRP
Swivel doors added to make switching between calibration and testing quick and easy

## Slide 14: Original Pilot Burner

## Slide 15: Original Radiant Panel Pilot Burner

## Slide 17: Unidirectional NBS Chamber Pilot Burner
2”

## Slide 18
Foam Block
Multiple Flamelet Burner

## Slide 21: 16 ply ACF1

## Slide 22: Observations
16 ply ACF1 performed very well in all foam block tests with minimal evidence of burning
Pilot flame gas flow rate for this test produced a tall flame with a large footprint
Reduce flow rate and re-test

## Slide 23: 16 ply ACF1 – smaller flame

## Slide 24: Observations
Reducing the gas flow rate resulted in a much smaller flame with smaller footprint, making it easier to observe flame propagation from the ignition point
Under these test conditions, 16 ply ACF1 still burned more than the foam block tests indicated
Panel heat flux should be changed to get closer to measured foam block heat flux

## Slide 26: Multiple Flamelet Burner

## Slide 27: 16 ply ACF1 – smaller flame, lower heat flux

## Slide 28: ACF1-HC

## Slide 31: 16 Ply ACF1
24”
12”
1 13/16”
1 13/16”

## Slide 32: 8 Ply ACF1
6”
2”
4 3/4”

## Slide 33: ACF1-HC
24”
12”
3 5/16”
8”

## Slide 34
GRP
24”
12”
8 5/16”
11 7/16 ”

## Slide 35: Observations
The smaller flame and lower heat flux settings correlate reasonably well with foam block test for the materials tested
More materials are to be tested in both foam block and VRP