## Slide 1: NexGen Burner Comparative Testing

## Slide 2: Objectives
Perform comparative burnthrough testing to determine the effect of various parameters on test results
  Use picture frame sample holder and PAN material to determine burnthrough performance
Test results will help to determine which parameters are most critical when specifying the burner in the new workbook

## Slide 3: Establish Baseline Dataset
3.43% Standard Deviation
3.17% Standard Deviation

## Slide 4: Test 1: Location of sonic choke Standard Configuration

## Slide 5: Relocated Choke

## Slide 7
Burnthrough Time
Repeatability

## Slide 8: Test Series 1 - Summary
The choke was relocated approximately 6’ from the burner and a curved, flexible hose was added between the muffler and the burner
Test results indicate no noticeable deviation from the baseline configuration

## Slide 9: Test Series 2 – Burner Cones
Objective is to determine which cone parameters have an effect on burnthrough time
  Thickness
  Flange
  Material
  Age
Besides the baseline cone, three additional cones were tested (all new)
  Baseline Cone: 0.06” thickness with recessed flange
  Cone #1: 0.048” thickness 18 gauge 310 Stainless Steel
  Cone #2: 0.061” thickness 321h Stainless Steel
  Cone #3: Same as Cone #1 with 1” flange welded on exit plane

## Slide 10: Cones
Cone #1
Cone #2
Cone #3

## Slide 11: Cone Surface Temperature Measurement
TC1
TC2
TC3
TC4
TC5

## Slide 12: FLIR Imaging

## Slide 13: Fuel Nozzle Spray Cone Angle

## Slide 14: Cone and Flame Temperature

## Slide 15: Insulated Cone

## Slide 16: Insulated Cone

## Slide 17: Cone Surface Temperature Comparison
Un-Insulated Cone
Insulated Cone

## Slide 18: Flame Temperature Comparison
Un-Insulated Cone
Insulated Cone

## Slide 19: Burnthrough Times

## Slide 20: Summary - Insulated Cone
Insulating the cone increases the average flame temperature by about 85°F
Insulation increased the cone surface temperatures by 500-600°F
The insulated cone burned through the PAN material significantly quicker than the un-insulated cone
  8579: 92 sec. quicker
  8611: 92 sec. quicker
Cone insulation used as an extreme example to determine how heat loss from cone can affect burnthrough results

## Slide 21: Installed Cone #1 0.048” thickness 18 gauge 310 Stainless Steel

## Slide 22: Installed Cone #1 0.048” thickness 18 gauge 310 Stainless Steel
Baseline Cone
Cone #1

## Slide 23: Installed Cone #1 0.048” thickness 18 gauge 310 Stainless Steel

## Slide 24: Installed Cone #2 0.061” thickness 321h Stainless Steel

## Slide 25: Installed Cone #2 0.061” thickness 321h Stainless Steel
Baseline Cone
Cone #2

## Slide 26: Installed Cone #2 0.061” thickness 321h Stainless Steel

## Slide 27: Installed Cone #3 Same as Cone #1 with 1” flange welded on exit plane

## Slide 28: Installed Cone #3 Same as Cone #1 with 1” flange welded on exit plane
Baseline Cone
Cone #3

## Slide 29: Installed Cone #3 Same as Cone #1 with 1” flange welded on exit plane

## Slide 30: Cones #1 vs. #3 – Effect of Flange

## Slide 31: Cones #1 vs. #2 – Effect of Thickness

## Slide 32: Average % Change from Baseline

## Slide 33: Cone Comparison - Summary
All cases tested reduced the burnthrough time of both 8579 and 8611 from the baseline case
In order of impact on burnthrough severity
  Insulating outer cone surface to prevent heat loss
  1” flange on end of cone
  Slightly thicker cone material
  New cone

## Slide 34: Re-run Baseline Tests
244 ± 5%
231.8<x<256.2
298 ± 5%
283<x<313

## Slide 35: Re-run Baseline Tests

## Slide 36: Test Series #3 - Stator
Definitions
“Old Stator”
Marlin Engineering CNC-machined reproduction of original Monarch H-215
“New Stator”
Marlin Engineering, symmetric, CNC-machined

## Slide 37: New Stator – External Ignition

## Slide 38: New Stator
Initially new stator was put in exact position as old stator
  4” back from nozzle tip
  Centerline between vanes aligned 35° from vertical
Ignition wires were removed from burner completely

## Slide 39: New Stator – Temperature Comparison

## Slide 40: New Stator - Burnthrough

## Slide 41: Summary of Initial New Stator Results
New Stator – Flame Temperature Measurement
  More uniform flame temperature profile
  Significant improvement on #1 T/C
  Over 50°F increase in average flame temperature
New Stator – Burnthrough Tests
  Longer overall burnthrough times for both 8579 and 8611 material
    8579 – 16.45 sec. longer
    8611 – 33.60 sec. longer

## Slide 42: Measured Flame Temperatures - Rotation

## Slide 43: Measured Flame Temperatures - Rotation

## Slide 44: Measured Flame Temperatures - Rotation

## Slide 45: Measured Flame Temperatures - Rotation

## Slide 46: Measured Flame Temperatures - Rotation

## Slide 47: Measured Flame Temperatures - Rotation

## Slide 48: Measured Flame Temperatures - Rotation

## Slide 49: Stator Rotation: ΔT=Tmax-Tmin
ΔT is used to determine the uniformity of the flame temperature measurement, smaller ΔT, more uniform profile

## Slide 50: Stator Rotation - Summary
Rotating the stator over 90° in 15° increments resulted in slightly different flame temperature profiles
The uniformity of the flame was assessed by subtracting the minimum temperature from the maximum temperature
The best uniformity was found at 0°, with a spread of 70.36°F

## Slide 51: Axial Position
4”

## Slide 52: Axial Position
5”

## Slide 53: Axial Position
6”

## Slide 54: Axial Position
3”

## Slide 55: Axial Position
2”

## Slide 56: Stator Axial Location: ΔT=Tmax-Tmin

## Slide 57: Axial Translation – Summary
Translating the stator on the axis of the burner over a range of 4 inches in 1 inch increments resulted in slightly different flame temperature profiles
The overall temperatures increased as the stator was translated closer to the fuel nozzle
The highest overall flame temperature and best uniformity was found at 2 inches back from the nozzle tip
  Tavg=1942°F
  ΔT=28°F

## Slide 58: New Stator, 0°, 2” from nozzle tip

## Slide 59: Rotation and Translation Burnthrough
The most uniform flame temperature profile and the highest overall measured flame temperature resulted in the longest burnthrough for both 8579 and 8611
  8579: 271.50
  8611: 368.25
These burnthrough times are longer than the baseline test
  8579: 27.20 sec. longer
  8611: 69.85 sec. longer

## Slide 60: Old Stator, same position as new stator, no wires

## Slide 61: Old Stator, same position as new stator, no wires

## Slide 62: Burnthrough Times

## Slide 63: Old stator @ 2” from nozzle tip - Summary
The old stator and igniters placed in the same position as the new stator resulted in lower flame temperatures with less uniformity
  New Stator: Tavg =1942°F, ΔT=28°F
  Old Stator: Tavg =1865°F, ΔT=151°F
The old stator and igniters resulted in significantly faster burnthrough times than the new stator and the original baseline
  8579: 56.75 sec. quicker than new stator
  8611: 89 sec. quicker than new stator
These tests are proof that the magnitude of the measured flame temperature is not indicative of burner severity

## Slide 64: New Stator @ 75psig sonic choke inlet pressure

## Slide 65: New Stator @ 75psig sonic choke inlet pressure

## Slide 66
New Stator @ 75psig sonic choke inlet pressure
Summary
Increasing the air pressure from 60 psig to 75 psig resulted in the 8579 being closer to the baseline, but the 8611 was still significantly longer
  8579: 5.95 sec longer
  8611: 44.6 sec longer

## Slide 67
Flame Retention Heads (FRH)
Beckett flame retention heads were purchased from local supply store
These heads are used on modern oil burners for more efficient burning
The heads can be used to create inefficient fuel rich burning that we are looking for by mismatching the air flow and the fuel firing rate
Benefits of Flame Retention Heads
  One component replaces both the stator and turbulator
  Reduces the amount of specification required for burner
  Rotationally symmetric
F-12
F-22
F-31

## Slide 68
Nozzle Depth
Note: All FRH tests were run without
Igniters or wires in the draft tube

## Slide 69: Flame Retention Heads

## Slide 70: Flame Retention Heads

## Slide 71: Flame Retention Heads - Summary
The flame retention heads give different temperature profiles depending on the size of the coflow air passages
Overall the flame temperatures were higher with flame retention heads than with stator and turbulator
A wide range of burnthrough times were obtained for the different heads, generally the larger the coflow air passages, the longer the burnthrough time
The F-22 head seems to give the closest burnthrough time to the baseline nexgen burner configuration

## Slide 72: FRH for Cargo Liner and Seat Burners

## Slide 73: Flame Retention Head: Description
Eliminates the need for a stator or turbulator
Fits on end of burner draft tube
Initial testing shows good potential

## Slide 74: Flame Retention Head: Calibration
Chart: Comparison of Average Temperatures During Calibration
| TC 1 | TC 2 | TC 3 | TC 4 | TC 5 | TC 6 | TC 7 | AVG
Flame Retention Head | 1664.375 | 1758.875 | 1807.875 | 1796.125 | 1791.5 | 1763.125 | 1694.75 | 1753.75
Sonic Burner | 1638 | 1621.2667 | 1608.6667 | 1642.1333 | 1665.0667 | 1618.1333 | 1485 | 1611.1333
Park Burner | 1694.47 | 1726.13 | 1718.45 | 1725.65 | 1751.14 | 1734.04 | 1650.9 | 1715.18
Calibration readings are significantly higher using the flame retention head compared to sonic readings using the standard stator
Readings also seemed more consistant from one calibration to the next

## Slide 75: Flame Retention Head: Test Results
Chart: Burner Comparison of Thick Cargo Liner Results

## Slide 76: Flame Retention Head: Test Results
Chart: Burner Test Result Comparison: TexTech PAN 8579
Park Burner | 344.5455
Sonic Burner | 345.8684
Flame Retention Head | 326.375

## Slide 77: Cargo Liner Flame Retention Head: Conclusion
Simplify setup and adjustments by eliminating stator and turbulator
Capable of producing higher temperatures
Flame temperature can be tailored by changing size of holes in flame retention head
Head tested produced temperatures higher than the Park or sonic burner, as well as decreased burn-through time

## Slide 78: FRH for Seat Cushion Burner
78
Chart: Calibration Temperatures using Flame Retention Head F31
| TC 1 | TC 2 | TC 3 | TC 4 | TC 5 | TC 6 | TC 7 | AVG
Calibration 1 | 1703.1 | 1788.8 | 1875.4 | 1904 | 1867.7 | 1812.8 | 1754.3 | 1815.1
Calibration 2 | 1700.9 | 1782.8 | 1870.7 | 1909.2 | 1875.1 | 1821.8 | 1745.9 | 1815.2
Calibration 3 | 1703.8 | 1780.3 | 1867.2 | 1902.3 | 1873.7 | 1821.1 | 1760.6 | 1815.6
Extremely low variation of temperature
Less than 1°F variation of averaged temperatures

## Slide 79: FRH for Seat Cushion Burner
Chart: Comparison of Park and Flame Retention Head F31 Test Results
| AirFlex | Fireblock | Dax
Park | 0.075908 | 0.070302 | 0.08164
Sonic F31 | 0.069598 | 0.070233 | 0.089436