## Slide 1: International Aircraft Materials Fire Test Working Group Meeting
Development of a New Flammability Test for Magnesium-Alloy Seat Structure
International Aircraft Materials Fire Test Working Group, Manchester, England
Tim Marker, FAA Technical Center
June 19-20, 2013

## Slide 2
Evolution of the Test Configuration
Spring 2007
Spring 2011
Horizontal Bar
Vertical Cone
Various Shapes
Summer 2011
Hollow Cylinder
Horizontal Bar
Spring 2012
Shorter cones
Taller cones
Stepped cones
Rectangular stepped shape
Horizontal cylinders
Rectangular tubing horizontal
Rectangular tubing vertical
I-Webs horizontal
T-Webs horizontal
Inverted cones
Cylindrical tubes horizontal
Cylindrical tubes vertical

## Slide 3
Which Configuration?
Hollow Cylinders (vertical): 59 Tests
Rectangular Bars (horizontal): 137 Tests

## Slide 4
Bars
Cylinders
Comparison of %RSD of Cylinder and Bar Tests

## Slide 5
Vertical Cylinder vs. Horizontal Bar Summary
Bar samples easier/less expensive to produce!
Data indicates horizontal bar configuration more repeatable

## Slide 6
Updated Horizontal Bar Testing Rig

## Slide 7
Updated Horizontal Bar Testing Rig

## Slide 8
Updated Horizontal Bar Testing Rig

## Slide 9
Eliminate measurement of residue ignition & extinguishment time
When is it “Out”?

## Slide 10
Chart: Burn Duration vs. Weight Loss .250-Inch Thickness Bars

## Slide 11
What has been done since last meeting?
√ Draft test method completed
√ Additional tests conducted
Ran an additional 99 tests for grand total of 521 tests
-Minimum time for sample to burn: 2 minutes
-Maximum weight loss: 6% to 10% (replaces time measurement of residue burning)
-Maximum time for sample to self extinguish: 3 minutes after burner off
-Sample thickness: 0.250 inches
-Burner exposure time: 4 minutes
√ Round Robin II completed

## Slide 12
How Repeatable is the Data?
Example of some of the data recorded during tests
Zeros inserted when sample does not burn

## Slide 13
Original Data with Zeros when bar doesn’t burn (107 Tests)
Modified Data with Zeros removed (67 Tests)
How Repeatable is the Data?

## Slide 14
Determine basic configuration: solid cone, vertical cylinder, horizontal bar
Make improvements to test apparatus: mounting mechanism, depth of talc
Determine which parameters to measure: e.g., time to melt, time to ignite sample, time residue burns, time
sample self-extinguishes, time residue self-extinguishes, weight loss
Select appropriate thickness of sample
Select appropriate test parameters
Determine if weight loss is good predictor of residue burn duration
Systematic Development of Lab-Scale Test
Determine interlab repeatability via Round Robins
Determine influence of exhaust ventilation on test results
Finalize all test parameters and details
Determine other sources of error and correct

## Slide 15
What is Left to Do??
Determine Influence of Catch Pan Material on Residue Burn Duration
Impact of Pre-loading a Curved Sample on Test Results
What is the Impact of Ventilation in the Testing Area?

## Slide 16
Determine Influence of Catch Pan on Residue Burn Duration

## Slide 17
Burned Sample Residue on Rigid Kaowool Board
ZE-41 Sample

## Slide 19
Impact of Talc Versus Rigid Kaowool in Catch Pan
The use of rigid Kaowool board had no apparent impact on test results compared to
a 0.25-inch layer of talc in catch pan.
During test method development, a 1-inch layer of talc was used. This depth
allowed molten residue to bury below the surface and continue to burn (insulated).
If the 0.25-inch talc depth is adhered to, results will not be impacted.
Recommend using a “screed” device to set proper talc depth.

## Slide 20
Screed Device for Leveling Talc and Setting Depth

## Slide 21
Impact of Curved Sample on Test Results
Not all samples perfectly straight!

## Slide 22
Impact of Curved Sample on Test Results

## Slide 23
Curved sample prior
to clamping
Impact of Curved Sample on Test Results

## Slide 24
Pre-Loaded Sample
What is influence of
preloading sample?

## Slide 26
Impact of Pre-Loading Curved Samples vs. Straight Samples
Slight impact on melt time?
Average melt time for straight sample: 143.7 seconds
Average melt time for curved sample: 127.9 seconds
No impact on time to begin burning
Average time to begin burning for straight sample: 163.8 seconds
Average time to begin burning for curved sample: 164.2 seconds

## Slide 27
What is the Impact of Ventilation in the Testing Area?

## Slide 28
Lab A Ventilation Configuration

## Slide 29
Lab B Ventilation Configuration

## Slide 31
Lab B Ventilation Issue Resolved

## Slide 34
RRII Statistics
7 Labs, 140 tests

## Slide 35
RRI Statistics (for comparison…)
3 Labs, 60 tests

## Slide 36
Comparison of RRI and RRII
Additional labs = more data = greater ability to determine problem areas
% RSD of time for sample to burn decreased
% RSD of time for sample to self-extinguish decreased
% RSD of weight loss increased

## Slide 37
1. Weigh the sample prior to test
Measuring Weight Loss of Bar Sample

## Slide 38
2. After test, weigh the remaining bar sample pieces
Measuring Weight Loss of Bar Sample

## Slide 39
Measuring Weight Loss of Bar Sample
3. Remove and weigh re-solidified material from catch pan
*Use compressed air
to blow off oxidation and
talc from retrieved residue

## Slide 40
Measuring Weight Loss of Bar Sample
Wt Loss % =
Initial Wt of Sample – (Final Wt of Sample + Residue)
Initial Wt of Sample
X 100

## Slide 41
Planned Activities and Next Steps?
Complete analysis of Round Robin II
Finalize draft test method
Complete report on test method development
Insert new test method into Handbook?
Refine method of determining when sample begins to burn
Refine method of determining when sample self-extinguishes
Refine method of measuring post-test weights

## Slide 42
http://www.fire.tc.faa.gov/pdf/AR11-13.pdf

## Slide 43
Questions?

## Slide 44
Determining Time Sample Begins to Burn & Self Extinguishment