## Slide 1: 2013/2014 OSU Round Robin Update
Project Leaders
Yaw Agyei – BR&T Flammability
Mike Burns – FAA Tech Center

## Slide 2: Agenda
Acknowledgements
Background
  Purpose
  Strategy
Test Results
Trends
  Preliminary analysis
Next Steps
Analysis of 80% pass criterion on sidewall coupons

## Slide 3: Acknowledgements
Support within Boeing
  BR&T Flammability (Puget Sound, SC)
  BCA Flammability
  BCA Production
  BR&T Math Group
FAA Tech Center
Participants
  40 participating labs
  46 participating units

## Slide 4: Background
Purpose: Pinpoint major sources of variability in OSU Heat Release testing
Unique Round Robin
Strategy
  Set all units in similar conditions
  Record all operating parameters
  Test more samples
  In-depth analysis of gathered data/results
Notes: Focused on inputs rather than ouput
Previous round robins more of a survey of units, this focuses on determining why results are so different from unit to unit.

## Slide 5: Pressure Measurements
Notes: Measure lower plenum and interspace pressure to try to understand air flow influence on variation

## Slide 6: Test Coupons
  Baseline – noise in system
  Honeycomb panel with decorative – representative of aircraft interiors (10)
  4 Ply pre-preg laminate – phenolic resin pre-impregnated glass fabric (10)
  Aluminum with tape – standardized coupons from Lufthansa Technik (5)
2
3
4

## Slide 7: Test Results
Chart: Honeycomb Panel with Decorative
 | Peak (kW/m2) | THR (kW- min/m2)
Avg | 58.83 | 59.90
Min | 37.43 | 42.61
Max | 71.54 | 81.07
Range | 34.12 | 42.61
% St Dev | 23% | 20%
Notes: Every line represents a unit. Average of ten coupons per unit.

## Slide 8: Test Results
Chart: Honeycomb Panel with Decorative
| A01 | A02 | A03 | A04 | A05 | A06 | A07 | A08 | A09 | A10 | A11 | A12 | A13 | A14 | A15 | A16 | A17 | A18 | A19 | A20 | A21 | A22 | A23 | A24 | A25 | A26 | A27 | B01 | B02 | B03 | B20 | B05 | B04 | B06 | B07 | B08 | B09 | B10 | B11 | B12 | B13 | B14 | B15 | B16 | B17 | B18 | B19 | B07
Peak Heat Release Rate (kW/m2) | 60.9432 | 63.1603 | 65.456 | 53.877 | 51.3681 | 71.5434 | 50.468 | 60.886 | 54.8312 | 63.5911 | 37.427 | 58.4549 | 53.911 | 53.5204 | 59.9256 | 55.437 | 69.3125 | 53.47 | 62.4 | 62.3242 | 47.813 | 63.9604 | 69.7625 | 68.1281
Total Heat Release (kW-min/m2) | 62.3421 | 64.4636 | 65.9774 | 53.877 | 52.3725 | 81.0699 | 54.3819 | 61.3885 | 63.9263 | 65.92 | 52.8543 | 57.9894 | 38.4601 | 60.1519 | 49.7445 | 65.7042 | 70.3178 | 53.47 | 56.05 | 62.1232 | 52.2212 | 69.0933 | 58.9544 | 64.6335

## Slide 9: Test Results
Chart: 4-Ply Pre-Preg Laminate
 | Peak (kW/m2) | THR (kW- min/m2)
Avg | 30.27 | 31.46
Min | 18.10 | 17.43
Max | 53.97 | 53.22
Range | 35.87 | 35.79
% St Dev | 30% | 27%

## Slide 10: Test Results
Chart: 4-Ply Pre-preg Laminate
| A01 | A02 | A03 | A04 | A05 | A06 | A07 | A08 | A09 | A10 | A11 | A12 | A13 | A14 | A15 | A16 | A17 | A18 | A19 | A20 | A21 | A22 | A23 | A24 | A25 | A26 | A27 | B01 | B02 | B03 | B20 | B05 | B04 | B06 | B07 | B08 | B09 | B10 | B11 | B12 | B13 | B14 | B15 | B16 | B17 | B18 | B19 | B07
Peak Heat Release Rate (kW/m2) | 20.9563 | 32.604 | 53.97 | 31.71 | 51.407 | 31.1406 | 22.6 | 23.45 | 33.3004 | 30.3537 | 23.35 | 43.1392 | 19.33 | 43.0725 | 25.7449 | 53.54 | 26.4484 | 19.19 | 18.0985 | 27.7216 | 20.74 | 26.7501 | 26.555 | 21.2813
Total Heat Release (kW-min/m2) | 28.8923 | 42.0782 | 48.6061 | 32.765 | 33.8163 | 43.4591 | 19.6737 | 31.1072 | 35.9827 | 29.8052 | 26.5905 | 42.5552 | 17.4263 | 32.6913 | 36.4642 | 53.2202 | 37.6009 | 28.5685 | 19.0969 | 24.2255 | 23.257 | 23.5834 | 18.0285 | 25.6246

## Slide 11: Test Results
Chart: Aluminum with Tape
 | Peak (kW/m2) | THR (kW- min/m2)
Avg | 74.69 | 26.84
Min | 61.96 | 12.78
Max | 97.06 | 43.77
Range | 35.10 | 30.99
% St Dev | 23% | 21%

## Slide 12: Test Results
Chart: Aluminum with Tape
| A01 | A02 | A03 | A04 | A05 | A06 | A07 | A08 | A09 | A10 | A11 | A12 | A13 | A14 | A15 | A16 | A17 | A18 | A19 | A20 | A21 | A22 | A23 | A24 | A25 | A26 | A27 | B01 | B02 | B03 | B20 | B05 | B04 | B06 | B07 | B08 | B09 | B10 | B11 | B12 | B13 | B14 | B15 | B16 | B17 | B18 | B19 | B07
Peak Heat Release rate (kw/m2) | 72.5651 | 79.7082 | 83.972 | 77.372 | 77.3296 | 81.9549 | 67.972 | 61.962 | 68.3926 | 81.7197 | 83.796 | 67.6439 | 65.818 | 78.1985 | 79.5113 | 97.058 | 70.7812 | 67.886 | 68.1039 | 75.9396 | 63.36 | 74.1223 | 80.7007 | 66.7401
Total Heat Release (kw-min/m2) | 31.6211 | 21.3559 | 27.4989 | 28.7917 | 30.5801 | 26.6606 | 37.4159 | 20.2897 | 26.419 | 28.8817 | 34.51 | 28.6859 | 12.7798 | 28.9832 | 28.2777 | 43.7729 | 29.9386 | 28.1025 | 18.1203 | 27.254 | 17.7661 | 23.2055 | 20.1278 | 23.0444

## Slide 13: Trends
Possible correlation between Interspace Pressure and Calibration Constant
Outliers Removed
Notes: Outlier – one or more parameters out of Mike Burns suggested range
Weak or no correlation seen with other parameters

## Slide 14: Calibration Constant (kh)
Primary factors
  Change in flow rates
  Thermopile voltage
Ratio of Delta =
Constant

## Slide 15: Ratio of Delta
Consistent within unit
Varies from unit to unit
Outliers Removed

## Slide 16: Ratio of Delta
Flow rates are consistent for all units
  Flow rates are accurate for most units
  Flow rates are proportional
 | ∆ Flow Rates (L/min) |  | 
 | 1-4 | 1-6 | 1-8
Avg | 2.99 | 4.98 | 6.98
% St Dev | 3% | 2% | 3%
% Error | 0.41% | 0.36% | 0.64%
 | ∆ Thermopile Voltage (mV) |  | 
 | 1-4 | 1-6 | 1-8
Avg | 6.18 | 10.20 | 14.28
% St Dev | 13% | 11% | 10%
% Error | ? | ? | ?
Variations observed for change in thermopile voltage for all units
  Possibly due to air flow split
Notes: Add % Error for flow meter difference
Unable to determine %error for change in thermopile voltage because actual change in thermopile voltage values are unknown – currently no measurements have been done for a unit that achieves a 3:1 air flow split
Change in thermopile voltages varies, but proportional within a unit.
Add number of data sets for interspace calibration values

## Slide 17: OSU Air Flow
75% of Air
25% of Air
3:1 Ratio

## Slide 18: Next Steps
Continue to gather round robin data
Determine change in thermopile voltage for a unit with an air flow split ratio of 3:1
  Further research to replicate observed variances in thermopile voltage
Discussion at FTWG Meetings

## Slide 19: 80% Criterion on Sidewall Panels
Dan Slaton

## Slide 20: 80% Pass Criterion
Heat Release (OSU) Round Robin data (set 1: sidewall panels)
  As of May 2014, engineering data from 17 labs (10 measurements per lab)
  “Pretend” the data are certification data
    Initially test 3 samples -> evaluate results
    Test additional 2 samples -> evaluate results
Peak Heat Release Rate

## Slide 21: 80% Pass Criterion
Heat Release (OSU) Round Robin data (set 1: sidewall panels)
  As of May 2014, engineering data from 17 labs (10 measurements per lab)
  “Pretend” the data are certification data
    Initially test 3 samples -> evaluate results
    Test additional 2 samples -> evaluate results
Total Heat Release

## Slide 22: 80% Pass Criterion
Summary
  80% pass criterion provides no benefit for either Peak or Total HR
    No “rogue” failures -> failures a result of normal statistical variation in OSU
    Existing “averaging” criterion better suited to account for statistical variation
  Use of 80% pass criterion actually a more stringent certification requirement
Recommendation
  Adopt ARAC Report “alternate proposal” (Sec. 6.2.9)
    Maintain present certification pass/fail requirements
    Add 80% pass criterion as an optional pass/requirement methodology