## Slide 1: International Aircraft Materials Fire Test Working Group Meeting
Development of a New Flammability Test for Magnesium-Alloy Seat Structure
International Aircraft Materials Fire Test Working Group, Solothurn, Switzerland
Tim Marker, FAA Technical Center
June 25, 2014

## Slide 2
Activities Since Last Meeting
Insert new test method into Handbook
Refined method of determining when sample begins to burn (10-sec dwell)
Refined method of determining when sample self-extinguishes (video)
Investigated various techniques when measuring post-test weights
Experimentation with not moving sample away from burner after test
Experimentation with new sample holder that allows elongation during heating
Investigated use of igniterless stator for more consistent flame

## Slide 4
Measurement of Bar and Residue Weight
After 1 hour
After 4 hours
After 24 hours
After wire-brushing
After hammering!

## Slide 6
Use of Flame Retention Head yields only 24% passing
Refinement of Burner Flame for Increased Repeatability
Use of Modified Flame Retention Head yields only 79% passing
Use of Stator/Turbulator (baseline) 90% passing
Igniterless Stator 85% passing
(using Elektron-43 as the testing material)

## Slide 8
Igniterless Stator Testing

## Slide 10
Translation of Sample Away from Burner

## Slide 11
Vibration or Momentum Can Cause Burning Sample to Fall

## Slide 12
Steel Cover for Cone

## Slide 14
Super Wool Cover for Cone

## Slide 16
Warped Sample Restrained in Fixture

## Slide 17
Sample Restrained in Fixture - Locked

## Slide 18
Elongation of Restrained Sample

## Slide 19
Alternate Sample Holder Allows Elongation

## Slide 20
Alternate Sample Holder Allows Elongation

## Slide 28
Other Areas of Use?

## Slide 30
Possible Areas of Mag-Alloy Use

## Slide 31
Possible Areas of Mag-Alloy Use

## Slide 32
How Can We Certify?

## Slide 33
Surface Area to Volume Ratio

## Slide 34
For truncated cone test sample: (l = 10, Db = 1.57, Dh = 0.40)
Surface Area = 33.0592 in2
Volume = 8.5161 in3
SAV Ratio = 33.0592 ÷ 8.5161 = 3.88 in-1
Surface Area to Volume Ratio
SAV Ratio = 3.88

## Slide 35
For rectangular bar test sample:
Surface Area = (2 x 0.25 x 20) + (2 x 1.5 x 20) + (2 x 0.25 x 1.5)
Surface Area = (10) + (60) + (0.75) = 70.75 in2
Volume = (0.25 x 1.5 x 20) = 7.5 in3
SAV Ratio = 70.75 ÷ 7.5 = 9.42 in-1
Surface Area to Volume Ratio
SAV Ratio = 9.42

## Slide 36
For hollow cylinder test sample (1.75 OD, wall thickness = 0.094):
Surface Area = 84.22782 in2
SAV Ratio = 84.22782 ÷ 3.90248 = 21.58 in-1
Surface Area to Volume Ratio
SAV Ratio = 21.58

## Slide 37
For thin sheet test sample: (10 inch square, thickness = 0.0625)
Surface Area = (2 x 10 x 10) + (4 x 0.0625 x 10)
Surface Area = (200) + (2.5) = 202.5 in2
Volume = (l x w x t)
Volume = (10 x 10 x .0625) = 6.25 in3
SAV Ratio = 202.5 ÷ 6.25 = 32.4 in-1
Surface Area to Volume Ratio
SAV Ratio = 32.4

## Slide 38
For solid basketball-sized test sample: (9.5-inch diameter)
Surface Area = 4 pr2
Surface Area = (4 x 3.14 x 22.5625) = 283.53 in2
Volume = 4/3pr3
Volume = (4 ÷ 3 x 3.14 x 107.17) = 448.92 in3
SAV Ratio = 283.53 ÷ 448.92 = 0.632 in-1
Surface Area to Volume Ratio
SAV Ratio = 0.632

## Slide 40
Considerations for Qualifying Other Mag-Alloy Components
Possible to define a maximum SAV ratio + use oil burner test
If SAV ratio is less than xx, use oil burner test
If SAV ratio is greater than xx, use suitable electrical arc test
For Example:

## Slide 41
Questions?

## Slide 42
http://www.fire.tc.faa.gov/pdf/AR11-13.pdf

## Slide 43
http://www.fire.tc.faa.gov/pdf/TC-13-52.pdf

## Slide 44
Discussion Items for Inclusion in Advisory Circular
Testing of coatings (powder coatings, anodizing, paints)
Can other seat components also be made of magnesium alloy?
Can “Equivalent Geometry” be defined using SAV ratio?