## Slide 1: International Aircraft Materials Fire Test Working Group Meeting
Seat Cushion Oil Burner Round Robin Update
International Aircraft Materials Fire Test Working Group
Tim Salter, FAA Technical Center
June 25-26, 2014, Solothurn, Switzerland

## Slide 2: Introduction
Previous interlab studies had shown the NexGen burner test results to be less repeatable than originally thought
  Within a single lab, as well as among multiple test labs
In the case of the Park burner, the stator and turbulator inside the burner draft tube could be adjusted to compensate for any irregularities in burner performance which might impact test results
The NexGen burner was designed to be setup in a standardized configuration, meaning that there are no adjustments to be made in order to simplify NexGen burner test rig setup
Flames coming from the NexGen burner cone were often bias to the left or right side, rather than exiting evenly from the cone
It was thought that redesigning the internal components of the NexGen burner may help reduce flame bias and increase test repeatability

## Slide 3: Old Vs. New Burner Internals
The original concept was to retain the same internals from the Park burner for use in the NexGen burner in order to keep burner performance similar
After trialing the igniterless stator design with no success, other options were considered
Oil burners on the market today no longer use stators and turbulators to direct the flow of air through the burner
Flame retentions heads (FRH) are now used in their place
  Generate a more efficient and complete combustion
  Simpler in design
  Relatively easier to produce
Turbulator
Static Plate
Stator
Flame Retention Head

## Slide 4: FRH vs. Stator and Turbulator
Flame Retention Head
Stator and Turbulator

## Slide 5: NexGen Burner Settings for 2013 Seat Cushion Flammability Round Robin
Face of FRH to nozzle tip: 1-1/8”
Fuel nozzle adapter to static plate: 2-3/8”
Static Plate Angle: centerline of igniters at 0°
  Looking into the cone of the burner, the centerline between the igniters will be at 0° on the burner reference
Fuel pressure: 108 psi (+/- 4 psi)
  This pressure is to be used as a starting point when flow checking the fuel flow rate
Air pressure: 45 psi
Air Temperature: 40-60°F
Fuel Temperature: 32-52°F

## Slide 6: Test Materials
All participating labs provided with cushions for testing purposes
3 different foam cushion types will be provided
  Airflex fire hardened foam
  Dax fire hardened foam
  Fire retarded polyurethane foam with a fire blocking layer
There will be 3 cushion sets of each cushion type provided
  9 samples total
Testing should be performed as described in the Rule or Fire Test Handbook

## Slide 7: FAA Initial Test Results using the FRH with the NexGen Burner
% Weight Loss for each Cushion Sample Set Tested using Delavan W nozzle and 45 psi air pressure
 | Airflex | Fireblock | Dax
Sample #1 | 7.50% | 7.42% | 6.58%
Sample #2 | 7.25% | 7.64% | 7.43%
Sample #3 | 6.93% | 6.12% | 7.72%
Average | 7.22% | 7.06% | 7.24%
Stdev | 0.287 | 0.82 | 0.594
%Stdev | 3.97 | 11.67 | 8.20
Chart: Weight Loss %
| Airflex #1 | Airflex #2 | Airflex #3 | Fireblock #1 | Fireblock #2 | Fireblock #3 | Dax #1 | Dax #2 | Dax #3
 | 0.075 | 0.072464 | 0.069272 | 0.074205 | 0.076389 | 0.061151 | 0.065767 | 0.074324 | 0.077181

## Slide 8: 2013 Round Robin Test Results
Chart: Round Robin 2013 Average Weight Loss % and Burn Lengths for Fireblocked Cushions
| Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL %
 | 8.934 | 8.292 | 12.167 | 0 | 7.06 | 5.4333 | 7.1333 | 8.9667 | 0 | 7.3518 | 6.1333 | 1.0333 | 7.5333 | 0 | 3.6267 | 7.1667 | 6.375 | 9.6667 | 0 | 5.5967 | 8.6 | 9.9 | 13.2 | 0 | 7.57 | 5.8333 | 6 | 9.1667 | 0 | 7.2333 | 7.2 | 7.425 | 10.6778 | 0 | 6.3466

## Slide 9: 2013 Round Robin Test Results
Chart: Round Robin 2013 Average Weight Loss % and Burn Lengths for Dax Cushions
| Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL %
 | 8.958 | 9.833 | 10.5 | 0 | 7.24 | 7.4667 | 9.3667 | 8.2333 | 0 | 8.38 | 5.8 | 1.0667 | 7.3 | 0 | 4.25 | 10 | 6.3333 | 10.7917 | 0 | 7.58 | 10.6 | 9.9 | 11.5 | 0 | 9.36 | 8.5 | 5.8333 | 10.3333 | 0 | 8.6 | 7.4803 | 5.643 | 8.2677 | 0 | 6.6269

## Slide 10: 2013 Round Robin Test Results
Chart: Round Robin 2013 Average Weight Loss % and Burn Lengths for Airflex Cushions
| Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL %
 | 7.375 | 10.417 | 8.792 | 0 | 7.22 | 4.9333 | 6.5667 | 6.6 | 0 | 7.35 | 5.8 | 1.0667 | 7.7333 | 0 | 5.5467 | 7.5208 | 5.4583 | 8.4167 | 0 | 8.3167 | 7.7 | 10 | 10.6 | 0 | 8.87 | 5.3333 | 6.1667 | 7.8333 | 0 | 5.7333 | 6.4304 | 6.5617 | 8.2677 | 0 | 7.0026

## Slide 11: 2013 Round Robin Test Results
Chart: Round Robin 2013 Average Weight Loss %
| Fireblock | Dax | Airflex
Lab A | 7.06 | 7.24 | 7.22
Lab B | 7.3518 | 8.38 | 7.35
Lab C | 3.6267 | 4.25 | 5.5467
Lab D | 5.5967 | 7.58 | 8.3167
Lab E | 7.57 | 9.36 | 8.87
Lab F | 7.2333 | 7.7 | 5.7333
Lab G | 6.42 | 6.6267 | 7
Lab H
Lab I
Lab J

## Slide 12: 2013 Round Robin Test Results
No average weight loss % failures have been experienced in a lab for the 2013 round robin
%Stdev results are above the preferred 10% limit when comparing all lab’s results
Average Weight Loss % Results
 | Fireblock | Dax | Airflex
Lab A | 7.06 | 7.24 | 7.22
Lab B | 7.35 | 8.38 | 7.35
Lab C | 3.63 | 4.25 | 5.55
Lab D | 5.60 | 7.58 | 8.32
Lab E | 7.57 | 9.36 | 8.87
Lab F | 7.23 | 7.70 | 5.73
Lab G | 6.42 | 6.63 | 7.00
Lab H |  |  | 
Lab I |  |  | 
Lab J |  |  | 
Avg | 6.41 | 7.31 | 7.15
Stdev | 1.40 | 1.60 | 1.22
%Stdev | 21.83 | 21.94 | 17.10
Chart: Round Robin 2013 Average Weight Loss %
| Fireblock | Dax | Airflex
Lab A | 7.06 | 7.24 | 7.22
Lab B | 7.3518 | 8.38 | 7.35
Lab C | 3.6267 | 4.25 | 5.5467
Lab D | 5.5967 | 7.58 | 8.3167
Lab E | 7.57 | 9.36 | 8.87
Lab F | 7.2333 | 7.7 | 5.7333
Lab G | 6.42 | 6.6267 | 7
Lab H
Lab I
Lab J

## Slide 13: 2013 Round Robin Test Results
The data on the previous slide shows the %Stdev among the participating labs to be elevated
Results are likely due to different configurations of labs (test area size, ventilation, etc.)
However, when examining the results of one lab at a time, there appears to be much higher consistency
The graph shown (right) shows the %Stdev for weight loss percent within each particular lab
Variations in test results not likely caused by burner
Chart: Round Robin 2013 Total % Standard Deviation within Labs for All Cushion Types
| % Standard Deviation
Lab A | 7.9494
Lab B | 12.7642
Lab C | 5.6573
Lab D | 5.5461
Lab E | 7.646
Lab F | 13.9924
Lab G | 10.1175
Lab H
Lab I
Lab J

## Slide 14: Conclusion of 2013 Seat Cushion Round Robin
Turbulator
Static Plate
Stator
Flame Retention Head

## Slide 15
Questions?

## Slide 16: 2012 Round Robin Test Results
 | Fireblock | Dax | Airflex
Lab A | 7.55 | 7.00 | 7.55
Lab B | 11.02 | 5.85 | 8.52
Lab C | 4.69 | 6.60 | 6.66
Lab D | 6.50 | 8.97 | 7.93
Lab E | 8.97 | 7.55 | 5.94
Lab F | 10.18 | 7.10 | 6.45
Lab G |  |  | 
Lab H |  |  | 
Avg | 8.15 | 7.18 | 7.17
stdev | 2.37 | 1.05 | 0.98
%stdev | 29.09 | 14.57 | 13.72
FAA is Lab A
Chart: Round Robin 2012 Average Weight Loss Percent
| Fireblock | Dax | Airflex
Lab A | 7.55 | 7 | 7.55
Lab B | 11.02 | 5.8533 | 8.5233
Lab C | 4.6867 | 6.6033 | 6.6567
Lab D | 6.5 | 8.97 | 7.9267
Lab E | 8.97 | 7.55 | 5.94
Lab F | 10.18 | 7.1 | 6.45
Lab G
Lab H

## Slide 17: 2012 Round Robin Test Results
Lab at far left is FAA Technical Center
Chart: Fireblock Cushion Burn Lengths and Weight Loss Percent
| Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL % | Top | Bottom | Front | Back | WL %
 | 5.44 | 12.73 | 8.04 | 0 | 7.55 | 9.252 | 16.4698 | 7.0472 | 5.2493 | 11.02 | 6.5333 | 4.6667 | 10.2 | 0 | 4.6867 | 5.4333 | 15.8333 | 8.0667 | 0 | 6.5 | 5.75 | 12.5 | 7.9167 | 0 | 8.97 | 6.8333 | 15.1667 | 8.2333 | 0 | 10.18