## Slide 1: International Aircraft Materials Fire Test Working Group Meeting
Development of a New Flammability Test for Magnesium-Alloy Seat Structure
International Aircraft Materials Fire Test Working Group, Bremen, Germany
Tim Marker, FAA Technical Center
June 3-4, 2015

## Slide 2
Coatings: summary of recent testing and recommendations
Air regulators: recent findings
Round Robin III: results obtained so far
Full scale testing/weight of components
Arc testing: recent test results
Miscellaneous Items/Future
Magnesium Alloy Flammability Highlights
Availability: Test method is currently in the Materials Fire Test Handbook
Mag Use in Other Areas: What is the appropriate method of testing?

## Slide 3
Magnesium Alloy Flammability Highlights
826 tests completed to date

## Slide 4
Magnesium Alloy Flammability Test Method is
now in the Aircraft Materials Fire Test Handbook!
Availability of Test

## Slide 8
First 2 test labs officially set up to run mag test

## Slide 9
Testing of Coated Magnesium Samples
-Chromium-free pre-treatment conversion coatings
-Polyester
-Polyester/Epoxy blend
25.4 Test Samples
In the Handbook test method…
25.4.6 Sample Coatings
If a finish coating, anodizing, or other surface treatment is used on the alloy in service, additional test samples must also be prepared and tested with this treatment to ensure it does not adversely affect sample performance.
December 2014: Various coated samples tested at FAATC…

## Slide 11
Argument Against Burner Testing of Coatings
- Currently, aluminum alloy seat structure is not oil-burner tested
- Oil-burner testing of mag-alloy seat structure “over and above”
- Suggestion was made to coat EL43 samples with “undesirable” coatings
Recent Testing of Coatings
- If undesirable coatings do not cause EL43 to fail, it can be assumed there are
no typical aircraft coatings that would cause the underlying magnesium alloy to fail
Testing of Coated Magnesium Samples

## Slide 12
Testing of Coated Magnesium Samples

## Slide 13
Testing of Coated Magnesium Samples

## Slide 14
Testing of Coated Magnesium Samples

## Slide 15
Bare Sample
Testing of Coated Magnesium Samples
Coated Sample

## Slide 16
Chart: Melt Time of Samples Coated with Non-FR Epoxy/Film
| EL-43 | EL-43 | EL-43 | EL-43 | EL-43 | EL-43 | EL-43 | EL-43 | EL-43 | EL-43 | EL-43
Melt (Seconds) | 140 | 99 | 107 | 117 | 110 | 107 | 121 | 120 | 115 | 108 | 115

## Slide 17
Chart: Results of Samples Coated with Non-FR Epoxy/Films
| EL-43 | EL-43 | EL-43 | EL-43 | EL-43 | EL-43 | EL-43 | EL-43 | EL-43 | EL-43 | EL-43
Melt (Seconds) | 140 | 99 | 107 | 117 | 110 | 107 | 121 | 120 | 115 | 108 | 115
Bar Begins to Burn (Seconds) | 140 | 146 | 186 | 0 | 0 | 107 | 217 | 253 | 115 | 156 | 122
Bar Out (Seconds) | 247 | 276 | 366 | 0 | 0 | 389 | 384 | 277 | 363 | 290 | 331

## Slide 18
Coatings caused accelerated melt times in all cases
80% of coated samples resulted in magnesium ignition after 2 minutes (80% pass)
Coatings not causing underlying magnesium alloy to become more hazardous
Recommendation 1: Continue testing mag alloy using oil burner (non-coated)
Recommendation 2: Test coatings using 12-sec VBB over mag alloy substrate
Testing of Coated Magnesium Samples

## Slide 19
Testing of Various Air Regulators
Originally-supplied unit (Norgren) caused fluttering, “trumpeting” on cargo liner rig

## Slide 20
Testing of Various Air Regulators
Norgren
Speedaire

## Slide 21
Testing of Various Air Regulators

## Slide 22
Testing of Various Air Regulators
Purchased brass/chrome units
Part number 49305K23
Manufactured by REGO
Supplied by McMaster-Carr
Operating range of 0-55 psi

## Slide 23
Testing of Various Air Regulators
Unit installed on mag test burner
Noticeable elevated level of smoke
during calibration
Suspected reduced airflow through
burner, causing elevated smoke

## Slide 24
Testing of Various Air Regulators
Manufactured by Parker
Part number 73535627
Supplied by MSC Industrial
Model R119-08CG/M2

## Slide 25
Measurement of Intake Pressure vs Exit Air Velocity

## Slide 26
Measurement of Exit Air Velocity Using Omega Velocity Meter

## Slide 27
Measurement of Exit Air Velocity Using Omega Velocity Meter

## Slide 28
Measurement of Intake Pressure vs Exit Air Velocity
Chart: Pressure (psi)
Pressure at Regulator (psi) | 40 | 45 | 50 | 55 | 60 | 40 | 45 | 50 | 55 | 60 | 40 | 45 | 50 | 52.6 | 55 | 60
Pressure Before Sonic Choke (psi) | 40 | 45.1 | 50.2 | 55.2 | 60.2 | 40.1 | 45.1 | 50.1 | 55.1 | 60.1 | 33 | 37.9 | 42.5 | 45 | 47.4 | 52.1
Exit velocity (ft/min) | 1260 | 1390 | 1510 | 1610 | 1715 | 1270 | 1385 | 1500 | 1610 | 1710 | 1110 | 1225 | 1320 | 1380 | 1440 | 1545

## Slide 29
Chart: Intake Pressure vs Exit Velocity Relationship
| 40 | 45 | 50 | 55 | 60
Speedaire Exit velocity (ft/min) | 1260 | 1390 | 1510 | 1610 | 1715
Parker Exit Velocity (ft/min) | 1270 | 1385 | 1500 | 1610 | 1710

## Slide 30
Testing of Various Air Regulators
Findings:
Intake pressure vs. exit velocity relationship linear
Brass/chrome REGO regulator not suitable for NexGen burner application
Speedaire 4ZM10 acceptable for NexGen burner use
Parker R119-08CG/M2 acceptable for NexGen burner use
Accurate control of pressure/exit velocity is essential in proper calibration

## Slide 31
Purpose: To help identify differences in labs. Results will help in the
development of a repeatable test.
Technique: Test identically-prepared samples under controlled conditions
Participants: FAA, Accufleet, Airbus, Magnesium Elektron
Equipment: Igniterless stator, spark plug, new clamp-style
sample holder, 20 samples of EL43, 1 sample AZ31
Magnesium Alloy Flammability Test Round Robin III

## Slide 32
Chart: Burner Flame Temperature Check
Pre-Test Temperature Check | 1715 | 1706 | 1690 | 1687 | 1683 | 1658 | 1642 | 1644.6202 | 1669.5708 | 1657.0925 | 1640.9041 | 1617.9175 | 1633.5194 | 1616.5083 | 50 | 50 | 50 | 50 | 50 | 50 | 50 | 1643 | 1660 | 1681 | 1671 | 1668 | 1685 | 1692
Post-Test Temperature Check | 1693 | 1678 | 1651 | 1643 | 1633 | 1621 | 1625 | 1633.2893 | 1668.1505 | 1657.4508 | 1638.1233 | 1607.8637 | 1609.4657 | 1616.0966 | 50 | 50 | 50 | 50 | 50 | 50 | 50 | 1624 | 1656 | 1680 | 1671 | 1664 | 1674 | 1670

## Slide 33
Chart: Round Robin III Using EL43 Samples

## Slide 34
Chart: Round Robin III Using EL43 Samples

## Slide 35
Chart: Round Robin III Using EL43 Samples

## Slide 36
Chart: Round Robin III Using EL43 Samples

## Slide 37
Chart: Round Robin III Using EL43 Samples

## Slide 38
Chart: Average Weight Loss of 20 Samples
Average Weight Loss, Including Zeros | 2.0317 | 6.4788 | 0.01 | 1.0205
Average Weight Loss, Excluding Zeros | 2.9024 | 6.4788 | 0.01 | 1.4578

## Slide 39
Magnesium Alloy Flammability Test Round Robin III
Preliminary Findings:
Melt times consistent between labs, indicating samples being exposed similarly
Time when sample begins to burn also consistent between labs
Time for sample to self extinguish remains inconsistent
Weight Loss results still an issue, with excessive scatter
Temperature Check shows burner flame agreement using igniterless stator
Further analysis to follow when all data received

## Slide 40
The Use of Magnesium Alloy in Other Cabin Areas
Use in 5 primary
seat components
Use in other
cabin components
accessible
inaccessible
Use in other non-
primary seat
components
Which Test?
Oil Burner
Oil Burner ?
Oil Burner ?
Elec Arc ?

## Slide 41
The Use of Magnesium Alloy in Other Cabin Areas
Can Surface Area-to-Volume (SAV) Ratio be used?
BE 990 Coach seat cross tube = 22.6
Typical Leg Surface Area-to-Volume Ratio = 13
Typical Spreader Surface Area-to-Volume Ratio = 12
Other seat cross tubes as high as 31.8
Test Method Rectangular Bar Sample = 9.4
Can “Equivalent Geometry” be defined using SAV ratio?

## Slide 42
Is full-scale testing necessary to determine max allowable % of magnesium?
What is typical maximum % of magnesium in seat (target)?
The Use of Magnesium Alloy in Other Cabin Areas
How could full-scale tests be conducted?
Is the goal a strict limit, or simply guidance material in future Advisory Circular?

## Slide 43
Update on electrical arc testing
electrode
Thin sample

## Slide 44
Update on electrical arc testing
electrode
Thin sample
plot amps vs thickness
.046875 and 11 amps
.0625 and 11 amps

## Slide 45
Update on electrical arc testing

## Slide 46
Update on electrical arc testing

## Slide 47
Questions?