## Slide 1: VFP Update

## Slide 2: Introduction
Carbon fiber composites are being used more frequently in aerospace applications
  Increased strength
  Lower density
  Better corrosion resistance
New designs of commercial transport airplanes include primary and secondary structure constructed from carbon fiber composites
Current FAR’s do not require flammability testing for fuselage skins or structures, as traditional designs are inherently non-flammable
  Special Conditions for certification of fire resistance of composite fuselage
  Must demonstrate level of safety equivalent to or better than traditional constructions
To continue with the FAA’s efforts to enhance in-flight fire safety, materials in inaccessible areas of the cabin should meet a flammability test based on the “block of foam” fire source

## Slide 3: Introducing VFP 3.0
New and improved VFP
Features:
  Smaller footprint
  Controlled air inlet
  Double-door system to keep backside smoke out of lab
  Larger viewing windows

## Slide 4: VFP 3.0 Features
Panel mounted flow meters
Traversing pilot flame mechanism
Larger windows on both sides

## Slide 5: VFP 3.0 Features
Outer door
Inner door

## Slide 6: VFP 3.0 Features
Fixed Furnace
Fixed Air Inlet
Honeycomb
3003 Aluminum
¾” thick
½” cell size
Perforated Steel Sheet
304 Stainless Steel
0.024” thick
24 gauge
0.045” hole diameter
37% open area
0.066” hole center-to-center

## Slide 7: New Power Supply
Keysight Technologies 6802A Basic AC Power Source
  Max output power 1000 W
  Max voltage 270 V
  Max current 10 A
  VFP requires 706 W, 112 V, 6.3 A
Built-in accurate measurement of Voltage, Current, and Power
  Accuracy:
    Voltage ±0.25% of reading + 0.15V (typical)
    Current ±0.25% of reading + 0.04A (typical)
    AC Power ±01% of reading + 1W (typical)
  Uses SCPI commands (Standard Commands for Programmable Instruments) to control and query measurements of voltage, current, and power

## Slide 8: New Power Supply
Keysight 6802A
  $4300
Variac
  $1077
Keithley digital multimeter
  $1940
Keithley expansion board
  $500
Current transducer
  $100
Total Cost
  $3617
OR

## Slide 9: VFP 3 Demonstration Test

## Slide 10: Propane vs Methane
It was requested to determine if methane could be used instead of propane
3 K-type exposed junction thermocouples used to quantify flame temperature
Ceramic fiberboard used behind thermocouples to simulate test sample impingement
TCs mounted 1” above burner face

## Slide 11: Flame Profile Comparison
Methane 80/80
Methane 100/100
Propane 45/90

## Slide 12: Propane vs Methane
Initial test results indicate that similar temperatures and profiles can be achieved by increasing the flow rate when using methane
Can not be certain that both gases are equivalent until burn tests are performed with both gases on the same materials

## Slide 13
A
C
B
Recently received 3 new ribbon burners
Will loan one to Boeing, one to Airbus for installation in their current VFP 2 machines
New Ribbon Burners

## Slide 14: PIV Setup
Ribbon Burner
Camera
Laser

## Slide 15: Mean Velocity Fields
Current VFP Burner
Marlin Burner

## Slide 16: Streamlines
Current VFP Burner
Marlin Burner

## Slide 17: Vertical Velocity Profiles*
Current VFP Burner
Marlin Burner
*At various heights from the burner exit plane

## Slide 18: Visual Comparison
Current VFP Burner
Marlin Burner

## Slide 19: Impingement Comparison
Current VFP Burner
Marlin Burner

## Slide 20: Summary
Develop better sample holding methods for panels, wires, and ducts
Standardize test method procedure
Find materials for comparative testing with new machines
Continue development and testing of VFP 3
  Work with equipment manufacturers to build commercial versions
  Develop detailed drawings for VFP 3
  Comparison testing with commercial versions once complete