## Slide 1: International Aircraft Materials Fire Test Working Group Meeting
Study of Reinforced Cone for use with Oil Burners
International Aircraft Materials Fire Test Working Group
Tim Salter, FAA Technical Center
June 6-7, 2018, Montargis, France

## Slide 2: Presentation Outline
Background Information
Standardized Cone Design
Cone Warpage Issues
Reinforced Cone Vs. Standard Cone Study
Test Result Comparison and Outcome
Additional Item
  Burner Flame High Speed Video

## Slide 3: Burner Cone Background
Burner cone dimensions and diagrams have been standardized since burner conception
Cones subject to warpage due to heat cycling
Various designs or frames, clamps, and rings have been used by labs to reduce warpage
No standardized design for cone reinforcement
FAA study revealed cone reinforcements influence airflow emitted from burner cone exit plane
Alterations to cone design discouraged due to unknown influence on test results

## Slide 4: Defined Cone Specifications
Alloy type
Sheet metal gage (thickness)
Placement of bends, welds, and small features
Tolerance for cone exit plane dimensions
  Replace or repair cone if out of tolerance
  Cone dimensions should be checked at the beginning and end of test day
  Test results may be void if cone is found to be out of tolerance after testing

## Slide 5: Cone Warpage Study
Cone exit plane may expand or contract out of tolerance
Some labs experiencing excessive cone warpage and frequently repairing or replacing cones
  Costly and time consuming
Allow cone reinforcement?
Conduct study to determine if cone reinforcement may be permitted
  Are the test results the same? More or less severe?

## Slide 6: Cone Comparison Study
Study involving two labs
  FAA T.C. and outside test lab
Run tests with standard and reinforced cones
  Same reinforced cone used by both labs
Seat cushion test method used for study
  Seat test samples more sensitive than other burner test samples
  Tests results most likely to show influence of cone reinforcement frame

## Slide 7: Cone Comparison Study
Identical seat test sample used for both cone designs
  Fire hardened foam
  Same manufacturer
  No dress covering
9 samples per cone
  3 different foam densities
  3 samples of each density
    3 + 3 + 3 = 9
FAA T.C. results showed excessive burning on bottom of sample due to burner misalignment

## Slide 8: Low Density Foam Results
FAA T.C. Test Lab
Chart: Low Density Foam Average Results
| % Weight Loss | Vertical Front Burn (in) | Vertical Back Burn (in) | Horz Top Burn (in) | Horz Bottom Burn (in)
No Frame | 10.3696 | 12 | 0 | 7.8333 | 17
With Frame | 11.4874 | 12.1667 | 0 | 11.6667 | 17
Outside Test Lab
Chart: Low Density Foam Average Results
| % Weight Loss | Vertical Front Burn (in) | Vertical Back Burn (in) | Horz Top Burn (in) | Horz Bottom Burn (in)
No Frame | 5.73 | 10 | 0 | 9.4 | 7.4
With Frame | 6.7 | 11.5 | 0 | 10.6 | 7.3

## Slide 9: Medium Density Foam Results
FAA T.C. Test Lab
Chart: Medium Density Foam Average Results
| % Weight Loss | Vertical Front Burn (in) | Vertical Back Burn (in) | Horz Top Burn (in) | Horz Bottom Burn (in)
No Frame | 8.5796 | 10.5 | 0 | 8 | 17
With Frame | 8.9553 | 10.6667 | 0 | 10.1667 | 17
Outside Test Lab
Chart: Medium Density Foam Average Results
| % Weight Loss | Vertical Front Burn (in) | Vertical Back Burn (in) | Horz Top Burn (in) | Horz Bottom Burn (in)
No Frame | 9.61 | 14.6 | 0 | 14.2 | 5.4
With Frame | 9.9 | 15.5 | 0 | 14.5 | 4.6

## Slide 10: High Density Foam Results
FAA T.C. Test Lab
Chart: High Density Foam Average Results
| % Weight Loss | Vertical Front Burn (in) | Vertical Back Burn (in) | Horz Top Burn (in) | Horz Bottom Burn (in)
No Frame | 5.3527 | 9.8333 | 0 | 6.5 | 17
With Frame | 5.7973 | 10.3333 | 0 | 8.3333 | 17
Outside Test Lab
Chart: High Density Foam Average Results
| % Weight Loss | Vertical Front Burn (in) | Vertical Back Burn (in) | Horz Top Burn (in) | Horz Bottom Burn (in)
No Frame | 4.06 | 10.4 | 0 | 9.9 | 5.5
With Frame | 4.31 | 11.9 | 0 | 11.4 | 5.5

## Slide 11: Outcome of Study
Average percent weight loss and burn lengths differed between labs
  Burner configuration issue
Reinforced cone results more conservative for nearly all test parameters at both labs
  More severe burning of samples
Frame successfully prevented warpage
Study results show reinforced cone design may be acceptable for certification testing

## Slide 12: Handbook Updates
Dimensions and drawings of cone frame will be added to Fire Test Handbook
  Chapter 7
Frame is optional
  Conventional or reinforced cone permitted for testing
No other reinforcement designs tested
  Use the frame design provided in Handbook

## Slide 13: Burner Flame Video
High speed video TCs in burner flame
  Cargo burner flame shown
Demonstrates transient flame
  TCs not continuously immersed in flame
Thermocouples with a high number of heat cycles do not respond to temperature as rapidly as new thermocouples
Reason why lower temperatures are seen when using worn thermocouples

## Slide 14: Thermocouples in Burner Flame

## Slide 15
Questions?
timothy.salter@faa.gov
(1)-609-485-6952