## Slide 1: Vertical Bunsen Burner Testing of 3-D Printed Material

## Slide 2: Introduction
Test solid 3-D printed material in Vertical Bunsen Burner
Ultem Support material
0.060 inch thick Samples
Printed in 3 orientations
  Flat (XY), Sideways (YZ), and Standing (ZX)
Attempting to find worst-case scenario in order to simplify future testing

## Slide 3: Printing Orientations
XY-Direction
YZ-Direction
ZX Direction
3 orientations
0.10” slice height
0.20” printing width

## Slide 4: Ultem Support Material
XY Direction
YZ Direction
ZX Direction
(Used as support material when printer is building with Ultem 9085)

## Slide 5
Chart: 0.060 Ultem Support Material
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9
Flame Time | 16.5 | 14.8 | 17.7 | 16.1 | 15 | 18.2 | 13.9 | 18.5 | 18.1 | 11 | 8.6 | 130 | 6.5 | 5.9 | 11.3 | 19.1 | 17.4 | 33 | 110 | 95 | 14.8 | 184 | 134 | 20.4 | 14.5 | 18.1 | 15.1



Burn Length | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 2.9 | 0.2 | 0.2 | 0.2 | 0.3 | 0.3 | 0.4 | 1.6 | 1.4 | 0.2 | 2.6 | 1.7 | 0.3 | 0.2 | 0.2 | 0.2
Drip Flame Time | 4.4 | 4.3 | 3.6 | 5 | 3.6 | 3.2 | 3.5 | 5.6 | 4.7 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 5.8 | 0 | 2.3 | 3.1 | 4.8 | 4 | 4.3 | 5.8 | 3.7 | 5.8 | 6

## Slide 6
Chart: 0.060 inch Ultem Support Flame Time
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9
 | 16.5 | 14.8 | 17.7 | 16.1 | 15 | 18.2 | 13.9 | 18.5 | 18.1 | 11 | 8.6 | 130 | 6.5 | 5.9 | 11.3 | 19.1 | 17.4 | 33 | 110 | 95 | 14.8 | 184 | 134 | 20.4 | 14.5 | 18.1 | 15.1

## Slide 7
Chart: 0.060 Ultem Support Burn Length
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9
Burn Length | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 0.2 | 2.9 | 0.2 | 0.2 | 0.2 | 0.3 | 0.3 | 0.4 | 1.6 | 1.4 | 0.2 | 2.6 | 1.7 | 0.3 | 0.2 | 0.2 | 0.2

## Slide 8
Chart: 0.060 inch Ultem Support Drip Flame Time
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9
Drip Flame Time | 4.4 | 4.3 | 3.6 | 5 | 3.6 | 3.2 | 3.5 | 5.6 | 4.7 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 5.8 | 0 | 2.3 | 3.1 | 4.8 | 4 | 4.3 | 5.8 | 3.7 | 5.8 | 6

## Slide 9
Chart: % Did Not Self-Extinguish - 0.060 inch Ultem Support
| XY Direction | YZ Direction | ZX Direction
 | 0 | 0.11111 | 0.44444
Chart: % Did Not Self-Extinguish - 0.060 inch Nylon-12
| XY Direction | YZ Direction | ZX Direction
% Did Not Self-Extinguish | 0.66667 | 0.18182 | 0.36364
Chart: % Did Not Self-Extinguish - 0.10 inch Nylon-12
| XY Direction | YZ Direction | ZX Direction
% Did Not Self-Extinguish | 1 | 0.55556 | 0.22222
*All Ultem Support samples were allowed to self extinguish – above graph is percentage of samples with flame time > 60 seconds

## Slide 10: Ultem Support vs. Nylon-12 Dripping
Ultem Support
Nylon-12
Nylon-12 continuously drips while Ultem Support had one big drip at most

## Slide 11: Summary of Results and Future Work
Ultem Support showed some difference in printing orientation
  YZ-direction only dripped on one sample vs every sample for the other print orientations
  ZX-direction was most severe case for Ultem Support
  XY-direction was most severe case for Nylon-12
Ultem Support seems to be a good candidate for a “borderline” material
Will test different thicknesses and infill percentage next

## Slide 12
Contact:
Steven Rehn
Federal Aviation Administration
William J. Hughes Technical Center
Fire Safety Branch, Bldg. 203
Atlantic City Int’l Airport, NJ 08405
(609) 485-5587
steven.rehn@faa.gov
Questions?