## Slide 1: International Aircraft Materials Fire Test Working Group Meeting
Development of a New Flammability Test for Magnesium-Alloy Seat Structure
International Aircraft Materials Fire Test Working Group, Bordeaux, France
Tim Marker, FAA Technical Center
March 16-17, 2016

## Slide 2
Oil Burner Testing of Solid Components Exceeding the SAV Ratio of 20
Discussion Items for Task Group
Magnesium Alloy Task Discussion Items
Mag Use in Other Cabin Components: What is the appropriate method of testing?
Radiant Panel Testing (58 Tests Conducted)
Video of Radiant Panel Test (time permitting)

## Slide 3
Surface Area-to-Volume (SAV) Ratios of Seat Components
Low SAV ratio = low probability of ignition
High SAV ratio = high probability of ignition

## Slide 4
Surface Area-to-Volume (SAV) Ratios of Seat Components
SAV ratio solid ≤ 20
SAV ratio hollow ≤ 40

## Slide 5
The Use of Magnesium Alloy in Other Cabin Areas
Use in 5 primary
seat components
Use in other
cabin components
Accessible
Below seat height
inaccessible
Use in other non-
primary seat
components
What is the appropriate method of test?
Oil Burner
Ignition/Self
Extinguishment
Oil Burner
Oil Burner
Accessible
Above seat height
Oil Burner

## Slide 6
Possible Criteria for Allowing Substantiation of non-Seat
Components Using the Oil Burner per Chapter 25
2. Surface Area-to-Volume (SAV) Ratios (≤ 20 solids, ≤ 40 hollow)
1. Component is accessible
3. Component is Located at Height Comparable to Seat Height
4. Proximity to Electrical Components is Minimized

## Slide 7
The Use of Magnesium Alloy in Other Cabin Areas
Use in 5 primary
seat components
Use in other
cabin components
Accessible
Below seat height
inaccessible
Use in other non-
primary seat
components
What is the appropriate method of test?
Oil Burner
Ignition/Self
Extinguishment
?
Oil Burner
Oil Burner
Accessible
Above seat height
Oil Burner
?

## Slide 8
Possible Methodology for SAV Ratio > 20
Solve for t
Minimum Burn Time > (t / .25) x 2 Min

## Slide 9
Testing of Thin Magnesium Sheet in Radiant Panel

## Slide 10
Testing of Thin Magnesium Sheet in Radiant Panel
Initial Testing using 3- by 4-inch
sample size

## Slide 11
Chart: Ignition of Thin Magnesium Samples Using Radiant Panel
EL43 Time of Ignition | 247 | 600 | 600
AZ31 Time of Ignition | 42 | 94 | 288

## Slide 12
Chart: Testing 0.025-inch Thick Mag Samples in Radiant Panel
| EL43 (3 by 4) | EL43 (3 by 4) | EL43 (3 by 4) | AZ31 (3 by 4) | AZ31 (3 by 4) | AZ31 (3 by 4) | EL43 (4 by 4) | EL43 (4 by 4) | EL43 (4 by 4)
Time of Ignition | 361 | 287 | 241 | 38 | 48 | 42 | 300 | 97 | 180

weight loss (%) | 36.3636 | 9.0909 | 40 | 100 | 100 | 100 | 0 | 0 | 33.3333

## Slide 13
Preliminary Testing of Thin Magnesium Samples in Radiant Panel
Greater thickness proportional to increased time to ignite
Weight loss proportional to amount of burning (burn length)
Pilot light on edge of sample resulted in earlier time of ignition vs. pilot in center
AZ31 ignited very easily and burned completely compared to EL43
1 minute preheat did not result in earlier ignition

## Slide 14
Machining Thin Magnesium Samples
Jig used for machining
Mag plate glued to jig

## Slide 15
Machining Thin Magnesium Samples
Thermoset adhesive
Underside of jig

## Slide 16
Machining Thin Magnesium Samples
Machined sample

## Slide 17
Machining Thin Magnesium Samples
Thicker plate of mag
Area machined out

## Slide 18
6- by 6-inch Machined Area Removed from Box

## Slide 19
Testing of 3- by 3-Inch Thin Magnesium Sample
3
3

## Slide 20
Testing of 3- by 3-Inch Thin Magnesium Sample
Pilot light in geometric center of sample

## Slide 21
Chart: Testing of 3- by 3-inch Samples
Time of Ignition (Seconds) | 194 | 79 | 240 | 240 | 37 | 48 | 43 | 52 | 204 | 0 | 157 | 0 | 103 | 111 | 123 | 141 | 103 | 126 | 114

Weight Loss (%) | 0 | 57.1429 | 42.8571 | 28.5714 | 100 | 66.6667 | 66.6667 | 66.6667 | 40 | 0 | 86.6667 | 0 | 92.8571 | 100 | 100 | 96.4286 | 85.7143 | 100 | 100

## Slide 22
Preliminary Findings of 3- by 3-inch Magnesium Sample Testing
When using 3- by 3-inch sample size, large % of coupon is covered in flame
Propose forcing ignition of sample, and determining it’s ability to self extinguish
Propose increased sample length to allow sample the opportunity to self extinguish
Propose moving pilot light to end of sample
EL21 ignited more easily than EL43
Some of EL21 samples burned completely under this configuration (100% weight loss)
3- by 3-inch sample size may be too small (not scaled for the apparatus)

## Slide 23
3- by 6-inch Thin Magnesium Sample
Initial piloted ignition
Burn

## Slide 24
3- by 6-inch Thin Magnesium Sample

## Slide 25
3- by 6-inch Sample of AZ-31

## Slide 26
3- by 6-inch Sample of AZ-31

## Slide 27
3- by 6-inch Sample of AZ-31
Sample completely consumed (100% weight loss)

## Slide 28
Chart: Tests Using 3- by 6-inch Sample Size
Time of Ignition | 240 | 120 | 121 | 122 | 158 | 133 | 47 | 73 | 35 | 36 | 39 | 39 | 240 | 240 | 144 | 146 | 163 | 87 | 99 | 114 | 113 | 73 | 88

weight loss (%) | 7.1429 | 7.1429 | 7.6923 | 7.6923 | 21.4286 | 21.4286 | 21.4286 | 21.4286 | 23.0769 | 23.0769 | 23.0769 | 23.0769 | 3.3333 | 13.7931 | 0 | 3.4483 | 24.1379 | 20.6897 | 20.6897 | 24.1379 | 27.5862 | 27.5862 | 100 | 100

## Slide 29
Preliminary Findings of 3- by 6-inch Magnesium Sample Testing
When using 3- by 6-inch sample size, better separation between good and poor alloys
Time of ignition may not be important, provided the sample demonstrates ability to
self-extinguish
Increased sample length allows sample the opportunity to self extinguish
Pilot light repositioned to ½-inch from end of sample
EL21 ignited more easily than EL43
Neither EL21 or EL43 samples burned completely (100% weight loss)
3- by 6-inch sample size scaled more appropriate for the apparatus

## Slide 30
Test Results of 3- by 6-inch Thin Magnesium Samples

## Slide 31
Questions on Radiant Panel Testing of Thin Samples?

## Slide 32
Proposed SAV ratio limit of 20 for “solid” seat components
Testing of Thinner Bar Samples Using Oil Burner
What if solid seat component exceeds SAV ratio? example: tray table arm
2 SAV ratios studied: 23 and 26

## Slide 33
For rectangular bar test sample:
Surface Area = (2 x 0.25 x 20) + (2 x 1.5 x 20) + (2 x 0.25 x 1.5)
Surface Area = (10) + (60) + (0.75) = 70.75 in2
Volume = (0.25 x 1.5 x 20) = 7.5 in3
SAV Ratio = 70.75 ÷ 7.5 = 9.43 in-1
Surface Area to Volume Ratio
SAV Ratio = 9.43

## Slide 34
Testing of Thinner Bar Samples Using Oil Burner

## Slide 35
Testing of Thinner Bar Samples Using Oil Burner

## Slide 36
Machining Thin Magnesium Bar Samples

## Slide 37
Testing Thin Magnesium Bar Samples

## Slide 38
Testing Thin Magnesium Bar Samples

## Slide 39
Chart: Testing Thin Samples Using Oil Burner
Melt (Sec) | 54 | 48 | 141.55
Bar Begins to Burn (Seconds) | 71 | 48 | 176.15
Bar Out (Sec) | 277 | 322 | 313.55
Weight Loss (%) | 5.3763 | 16.6667 | 2.0317

## Slide 40
Discussion Items for Task Group
Continue the development of acceptance criteria for allowing the use of the
oil burner for:
non-primary seat components (ex: tray table arms). Discuss recent
oil burner tests on thin bar samples.
non-seat components (ex. galley carts).
Continue radiant panel testing of thin magnesium alloy samples, develop
pass/fail criteria for inaccessible area components.
Discuss use of magnesium alloy components located in accessible areas that are
situated higher than seat back height.

## Slide 41
Video of Thin Magnesium Sample in Radiant Panel