## Slide 1: CFRP Flammability Tests
Test Configuration Influence on Flame Propagation

## Slide 2: Introduction
Tests were performed to determine the influence of a variety of configurational factors on inboard flame propagation of composite fuselage panels
  Insulation-panel spacing
  Heat retention near panel surface
  Outboard surface heat loss
The original foam block fire source and test rig were used
CFRP panels were procured for this testing
  0.1” thickness
  Quasi-isotropic tape layup, single outer ply of woven fabric
  350°F cure toughened epoxy

## Slide 3: Test Series
Flat Panel Tests
  Baseline
  Thermal-Acoustic insulation blanket between inboard face of test panel and test rig shroud
    Vary gap from tightly pressed up to panel  1” gap
  If significant flame propagation is found,
    Determine if increasing the rate of heat transfer from the outboard surface influences inboard flame propagation
Simulated Structure and Panel Tests
  Determine if both the structure and panel will propagate flames under conditions found previously
  Determine if increasing the rate of heat transfer from the outboard surface influences inboard flame propagation
Simulated Primary Lithium Battery Powered Electronic Locator Transmitter (ELT) failure adjacent to CFRP panel
  Higher intensity fire source
  Determine if this fire source will cause CFRP panel to propagate flames similar to foam block
  Will more intense fire source overcome increased rate of heat transfer from the outboard surface?

## Slide 4: Foam Block Test Configuration

## Slide 5
Date | Test Name | Configuration | Insul. Dist. | Burn Length | Burn Width
1/22/2015 | Baseline | Std. Config. | n/a | 6.5625 | 6.6875
1/22/2015 | Insulation 1 | Insul Pressed Tightly to Skin | 0 | 0 | 0
1/26/2015 | Insulation 2 | Insul Pressed Tightly to Skin | 0 | 7.5 | 15.25
1/27/2015 | Insulation 3 | Insul slightly further from skin | 0.5 | 10 | 15
1/27/2015 | Insulation 4 | Insul further from skin | 1 | 9.25 | 6.25
1/28/2015 | Insulation 5 | Insul closer, added gasket | 0.5 | 46 | 12
3/4/2015 | Insulation 6 | Insulation 5 w/water cooling | 0.5 | 0 | 0
3/9/2015 | Insulation 7 | repeat of insulation 6 | 0.5 | 0 | 0
3/17/2015 | Insulation 8 | CFRP with frames | 0.5 | 46 | 12
3/19/2015 | Insulation 9 | CFRP with frames & water cooling | 0.5 | 3 | 3
3/24/2015 | Insulation 10 | CFRP frames & stringers | 0.5 | 16 | 14
3/27/2015 | Insulation 11 | CFRP frames & stringers (flipped panel) | 1 | 2 | 5
4/2/2015 | Insulation 12 | CFRP frames & stringers | 1 | 8 | 7
4/2/2015 | Insulation 13 | CFRP frames & stringers (flipped panel) | 1 | 9 | 8
4/2/2015 | Insulation 14 | CFRP frames & stringers (sealed w/RTV) | 1 | 7 | 4
4/30/2015 | Insulation 15 | CFRP frames & stringers (flipped panel+RTV) | 0.5 | 8 | 5
4/30/2015 | Insulation 16 | CFRP frames & stringers (sealed w/RTV) | 0.5 | 33.5 | 14
5/28/2015 | Insulation 17 | Insulation 16 w/water cooling | 0.5 | 9 | 9.75
Test Matrix: Foam Block Ignition Source

## Slide 6: Lithium Battery Ignition Source Test Configuration
Lithium Battery Test Configuration
  5 D-Cell Lithium batteries (non-rechargeable)
  Battery box insulated w/ ½” ceramic fiberboard
  Battery box surface within ½” of CFRP inboard panel surface
  Insulation blanket placed between shroud and inboard face of CFRP panel
  Thermocouples penetrate through insulation blanket, within ¼” of CFRP panel surface
  Thermocouples on each battery cell and on cartridge heater

## Slide 7
Battery Configuration

## Slide 8: Gas Analyzers
Non-dispersive IR Measurement of CO and CO2
Paramagnetic Measurement of O2
Single stream sample plumbed in series
Filtered and dried to 1 micron & 5°C dew point
6 Lpm flowrate
Approx 20’ of ¼” sample line
Gas Measurement Location

## Slide 11
10 Ply CFRP, Battery Ignition Source
Inboard Panel Temperatures
Measured Gas Concentrations

## Slide 12
Comparison: Static Ambient vs. Cooled Backside
Inboard Panel Temperatures
Static Ambient
Cooled Backside

## Slide 13
Date | Test Name | Configuration | Panel Thickness (in.) | Insul. Dist. (in.) | Burn Length (in.) | Burn Width (in.)
7/9/2015 | ELT 1 | Simulated ELT, insulation, no cooling | 0.098 | 0.5 | 46 | 15
7/16/2015 | ELT 2 | Simulated ELT, insulation, w/cooling | 0.098 | 0.5 | 3 | 6
8/6/2015 | ELT 3 | Simulated ELT, insulation, no cooling, 32 Ply | 0.366 | 0.5 | 17 | 10.5
8/13/2015 | ELT 4 | Simulated ELT, insulation, no cooling, 24 Ply | 0.275 | 0.5 | 24 | 10
8/25/2015 | ELT 5 | Simulated ELT, insulation, no cooling, 16 Ply | 0.13 | 0.5 | 43.5 | 15.5
Test Matrix: Lithium Battery Ignition Source
24 Ply CFRP

## Slide 14: 24 Ply CFRP, Battery Ignition Source
Inboard Panel Temperatures
Measured Gas Concentrations

## Slide 15: Next Steps
Increase measurement range of CO analyzer to 30%
  Re-test CFRP 10 ply w/foam block
Quantify cooling efficiency
  Compare to calculated and/or measured in-flight heat loss rates for CFRP airplanes
Once cooling rate is fixed, re-test foam block and Lithium battery configurations w/new cooling rate

## Slide 16: Foam Block Baseline – 8x
Fabric Overlap Seam

## Slide 17: Foam Block Baseline Observations
The seam created where two pieces of prepreg fabric overlap is a significant barrier for flame propagation
  If the fire is unable to develop fully, it will not propagate
The gas sampling system clogged, resulting in no gas data. A new method is required

## Slide 18: Gas Sampling Modifications

## Slide 19: 10 ply CFRP Foam Block 8x – Expanded CO Range 0-30%

## Slide 20: 10 ply CFRP Foam Block – Expanded CO Range 0-30%

## Slide 21: Foam Block Baseline 2 Observations
Heat escaped from back of fire box area resulting in a stalled flame propagation
  A better method of closing fire box area is required
Igniting a second foam block was able to produce a full-length flame propagation
Although the CO measurement range was expanded to 30%, peak CO measurements of only 2-3% were observed
  This is most likely due to an over-ventilated configuration with the foam block source
  Previous measurements of 10% or greater CO were obtained using the lithium battery source, which has significantly less available air for combustion
A battery source baseline will be run with the expanded CO measurement range to validate this

## Slide 22: Large Scale CFRP Skin & Structure Tests
Large scale CFRP skin and structure test fixture
Study propagation of fire from bay-to-bay with and without cooling

## Slide 23: CFRP Structure Tests

## Slide 24: Simulated CFRP Aircraft Structure
8’
4’

## Slide 28: Large Scale Test Plan
Continue evaluating backside heat transfer methods to accurately represent in-flight cooling
Begin planning baseline tests
  Construct rig to hold test panel at variable angles
  Static ambient conditions on backside
    Foam block
    Simulated ELT
Test configuration guidance or suggestions welcome and encouraged