## Slide 1: Development of a Lab-Scale Fire Test Method for Composite Structure

## Slide 2: Objective
Develop a lab-scale test method for composite structure
  Representative of the threat
    Moderate fire about the size of the block of foam fire
  Relatively simple
    Radiant heat source + Pilot ignition
  Low cost
    Small sample size
  Can be adapted to other inaccessible area materials
    Ducts
    Wire Insulation
    Other composites that are not small parts as defined in regulations

## Slide 3: Lab-Scale Test Method Development
The foam block fire source was characterized by measuring the heat flux gradient along an insulated board for the duration of the foam burning event
This heat flux gradient will then be used to impose a similar heat flux on a smaller sample in a lab-scale test apparatus

## Slide 4: Foam Block Heat Flux Gradient

## Slide 5: Vertical Radiant Panel (VRP) Development
Objective: to develop a “new” radiant panel type test that will:
  Simulate conditions of a foam block test
    Incident heat flux on sample
    Duration
    Geometry
  Correlate results from foam block test
    Use current database of materials already tested
      Aerospace/non-aerospace grade composites (1/8” thick)
      Aerospace grade carbon epoxy, varying thicknesses
      Cargo liners and floor panels, varying thicknesses

## Slide 6
VRP Configuration
Heat flux gradient
  A tilted panel was used to attempt to achieve the same measured gradient as the foam block test
  Furthest backward tilt (70°) could not achieve steep enough gradient
  Zero position heat flux too low
Next attempt:
  Separate emitter strips into 3 individually controlled pairs to control the heat flux gradient

## Slide 7
Bottom 2 Strips Only

## Slide 8: Modifications to VRP
Swivel doors added to make switching between calibration and testing quick and easy

## Slide 9: Unidirectional NBS Chamber Pilot Burner
2”
50 ccm @ 20 psig propane

## Slide 10: Multiple Flamelet Burner

## Slide 11: Recent Modifications
NBS furnace is widely used in FAA fire test community
  Smoke chamber
  Slide test
Provides steady, intense thermal radiation
Runs on 110V ac, no special power requirements
Controlled with variable AC transformer instead of backside TC and temp controller

## Slide 12
6” x 12” sample holder
Furnace
Pilot Burner
Schmidt-Boelter
Gauges
Recent Modifications

## Slide 13
Recent Modifications

## Slide 14: Measured Heat Flux

## Slide 15: Recent Testing
Procedure | 
1 | Set Heat Flux Gradient, 5 minute average of each calorimeter
2 | Install Pilot Burner
3 | Install Sample
4 | Ignite Pilot Burner, set propane pressure and flow rate
5 | Swing away calorimeter door
6 | Swing in sample door, start timer
7 | Impinge flame and expose sample to radiant heat for 60 sec.
8 | At 60 sec., pilot burner is turned off, sample remains exposed to radiant heat and allowed to burn
9 | Test is terminated when flames extinguish, sample is removed and allowed to cool
10 | Once sample is cool, degreaser is used to wipe away sooted areas
11 | Burn length and width are measured, and after flame time is assessed from video

## Slide 17: G-10 Glass Epoxy
BLavg=3.95”
  %sd=9.11%
BWavg=2.5”
  %sd=8.66%
AFavg=28 sec.
  %sd=37.8%

## Slide 18: Fiber Reinforced Polyester
BLavg=6.208”
  %sd=16.14%
BWavg=4.125”
  %sd=0%
AFavg=334.3 sec.
  %sd=18.75%
12”
6”

## Slide 19: ACF1-HC
BLavg=5.58”
  %sd=4.23%
BWavg=2.48”
  %sd=3.85%
AFavg=91 sec.
  %sd=9.57%

## Slide 20: ACF1 16 ply
BLavg=2.125”
  %sd=40.75%
BWavg=1.375”
  %sd=9.09%
AFavg=9.5 sec.
  %sd=126.53%

## Slide 21: ACF1 4 ply
BLavg=4.395”
  %sd=2.17%
BWavg=2.375”
  %sd=2.63%
AFavg=22.67 sec.
  %sd=19.89%

## Slide 22: ACF1 8 ply
BLavg=3.625”
  %sd=8.95%
BWavg=2.125”
  %sd=0%
AFavg=64.67 sec.
  %sd=12.011%

## Slide 23: Average Results

## Slide 24: VRP vs. Foam Block Burn Length & Width

## Slide 25: VRP vs. Foam Block Burn Area

## Slide 26: VRP vs. Foam Block Burn Time

## Slide 27: Recent Testing – Summary
Fairly good repeatability was found for most sample sets
  Average %SD
    Burn Length: 13.56%
    Burn Width: 4.04%
    After Flame: 37.43%
  More tests need to be performed to standardize a procedure, environmental influences, etc.
Lab scale test results generally correlate with intermediate scale testing

## Slide 28: Effect of Drafts on Heat Flux
Three scenarios were tested to determine the effect of enclosing the apparatus on air drafts near the sample or heat flux gauge surfaces
  Baseline: Partially shrouded, no exhaust fans
  Partially shrouded, exhaust fans approximately 6’ above top of apparatus gently drafting air out of room
  Fully shrouded, no exhaust fans
SB1
SB2
SB3
SB4

## Slide 29
SB1
SB2
SB3
SB4
SB1
SB2
SB3
SB4
SB1
SB2
SB3
SB4

## Slide 31: Heat Flux Fluctuations
Bottom 2 flux gauges have less relative fluctuation than the top 2
The average measured values at each SB gauge changed little from test to test
Burn tests can be performed to determine the actual effect on test results
The final design will specify how to enclose the apparatus to standardize air currents and fluctuations

## Slide 32: Next Steps
Furnace comparison
  Spiral tubular heating elements were ordered from different manufacturers to determine the difference in measured heat output at the same power settings, distance
Calibration
  Determine if specification of power (voltage, current), distance from heat flux gauge, and furnace specifications will adequately represent the desired incident flux
    Removing HFG from calibration procedure would reduce cost of running test and eliminate uncertainty of calibration and use of HFG
  Mapping of furnace with HFG on a traverse
    Monitor input voltage and current while traversing SB gauge to map heat flux vs. input power, distance
    Determine repeatability
      Different day
      Different furnace

## Slide 33: Next Steps cont.
Version 2.0
  Once design and test parameters are confirmed, perform repeatability testing
    Will be receiving large quantity of 6” x 12” carbon fiber composite samples of varying ply thicknesses, layups, fibers, and epoxies
  Construct one or more units
    Perform comparative testing on multiple units to determine reproducibility

## Slide 34: Version 2.0

## Slide 35: Version 2.0
Furnace height adjustment
Furnace distance adjustment

## Slide 36: Version 2.0
Variable AC Transformer
Cooling fan for SB gauge water
Propane gas for
Pilot burner
Propane gas flow meter
Propane gas
pressure regulator
Pilot burner gas
on/off valve
Furnace distance adjustment

## Slide 37: Version 2.0
Variable AC Transformer
Propane gas for
Pilot burner
Propane gas flow meter
Propane gas
pressure regulator
Pilot burner gas
on/off valve
Furnace distance adjustment