## Slide 1: The aircraft hazards of flammable gasses produced by lithium batteries in thermal runaway
Fall Systems Meeting
FAA Fire Safety
10/2015

## Slide 2: Background
Lithium-metal and lithium-ion cells contain flammable electrolytes which react during thermal runaway and release flammable gasses.
The unburnt gasses can accumulate and result in an explosive environment.

## Slide 3: Background (gas composition)
Chart: State of Charge (%)
| 100 | 50 | 90 | 80 | 70 | 60 | 40 | 30 | 20 | 10
Gas Volume (liters (10psi)) | 7.85 | 2.2498 | 5.2314 | 5.0493 | 4.2391 | 2.8109 | 2.0897 | 1.4934 | 1.3239 | 1.0432
Chart: State of Charge (%)
| 100 | 50 | 90 | 80 | 70 | 60 | 40 | 30 | 20 | 10
 | 0.70338 | 0.39494 | 0.5642 | 0.51212 | 0.4557 | 0.36022 | 0.33852 | 0.23002 | 0.17794 | 0.12152
Chart: State of Charge (%)
| 100 | 50 | 90 | 80 | 70 | 60 | 40 | 30 | 20 | 10
 | 1.5301 | 0.43244 | 1.012 | 0.93084 | 0.84721 | 0.65825 | 0.4419 | 0.096131 | 0.06484 | 0.04366
Chart: State of Charge (%)
| 100 | 50 | 90 | 80 | 70 | 60 | 40 | 30 | 20 | 10
 | 2.1344 | 0.11718 | 1.6796 | 1.5103 | 1.2065 | 0.24304 | 0.099819 | 0.03472 | 0.03038 | 0.0217
Tests conducted at cabin pressure at altitude (10psia)
Tests were conducted to determine gas compositions and volumes for various states-of-charge and various chemistries.

## Slide 4: Background (combustion)
Tests were conducted at altitude to determine the pressure rise generated by combustion of battery gasses.
Chart: Battery Gas Concentration (%)
| 15 | 10 | 12.5 | 17.5 | 20 | 22.5 | 25 | 30 | 35 | 40 | 33.9
100% SOC | 55.265 | 13.205 | 36.954 | 62.04 | 67.686 | 71.208 | 72.3 | 69.834 | 61.796 | 42.35 | 66.728
50% SOC | 14.047 | 58.421 | 69.071 | 68.299 | 58.87 | 13.45 | 9.4 | 36 | 70.109 | 42.1
P initial | 10 | 10 | 10 | 10 | 10 | 10 | 10 | 10 | 10 | 10 | 10

## Slide 5: Background (halon effectiveness)
Tests were performed in a 10.8m3 chamber to evaluate the effectiveness of Halon 1301 with vent gasses.
  Runaway was initiated => Halon was introduced => Spark was activated => Pressure was recorded

## Slide 6: Background (halon effectiveness)
Test with 5.28% Halon
Test without suppression
Test with 10.43% Halon

## Slide 7: Balloon Tests
Class C cargo compartments are equipped with pressure relief panels that become dislodged during a pressure event.

## Slide 8: Introduction
Could a small collection of battery gasses accumulate within a package and combust to dislodge the panels?
  If the panels became dislodged then the halon system would lose effectiveness.
Quantitative tests were first performed in a pressure chamber followed by verification tests in a 737.

## Slide 9: Bottled Gas
Rather than collect Li-Ion vent gasses for subsequent tests, a bottle of mixed gas was purchased that matched the composition from previous analysis.
  30.1% CO2
  27.6% H2
  22.9% CO
  6.37% CH4
  4.48% C3H6
  2.21% C2H4
  1.57% C4H10
  1.17% C2H6
  .56% C4H8
  .268% C3H8

## Slide 10: Bottled Gas
We then verified that pressure rise from bottled gas was identical to pressure rise from actual gas.
  Max pressure from actual gas at altitude: 70.1 psia
  Max pressure from bottled gas at altitude: 71.4 psia
Chart: Actual Gas
Chart: Bottled Gas

## Slide 11: Setup (quantitative tests)
Tests were conducted in a 10.8m3 chamber with small pockets of gas (in a balloon) to determine how many 18650 sized cells would compromise fire suppression in a cargo compartment.

## Slide 12: Pressure Chamber Cargo Compartment Tests
Balloon pressure rise was verified with gas accumulation in a box.
  Pressure from volume of gas corresponding to 5 cells at 50% SOC in balloon: .85 psi
  Pressure from volume of gas corresponding to 5 cells at 50% SOC in box: .97 psi

## Slide 13: Results Pressure Chamber Cargo Compartment
Tests at Sea Level:
Tests at Altitude:
Chart: Altitude, 50% SOC
| 5 | 3 | 1
Pressure Rise LS | 1.33 | 0.84 | 0.27
Chart: Sea Level, 50% SOC
| 5 | 11 | 6.8109000000000002
Number of Cells | 0.85 | 1.55 | 1.1
Chart: Altitude, 100% SOC
| 1.61 | 0.96599999999999997 | 0.32200000000000001
 | 1.33 | 0.84 | 0.27
Chart: Sea Level, 100% SOC
| 1.61 | 3.5419999999999998 | 2.1930000000000001
 | 0.85 | 1.55 | 1.1

## Slide 14: Setup (verification tests)
Pressure chamber tests were repeated in fwd. cargo compartment of 737 with 70% loading.
  Total volume of compartment (documented): 370ft3
  Volume of boxes based on 70% loading: 259ft3

## Slide 15: 737 Cargo Compartment Results
5 cells at 50% SOC
1.61 cells at 100% SOC
.252 psi peak pressure

## Slide 16: 737 Cargo Compartment Results
20 cells at 50% SOC
6.44 cells at 100% SOC
1.22 psi peak pressure
Additional panel behind door (not shown) and panel on sidewall (not shown) were also compromised.

## Slide 17: 737 Cargo Compartment Results
8 cells at 50% SOC
2.6 cells at 100% SOC
.594 psi peak pressure

## Slide 18: 737 Cargo Compartment Results
Chart: Sea Level, 50% SOC
| 4.9901999999999997 | 20 | 8
 | 0.252 | 1.219 | 0.594

## Slide 19: Summary
If gasses from 8 18650 cells at 50% SOC
or
If gasses from 3 18650 cells at 100% SOC
accumulate in a loaded 737 fwd. cargo compartment and ignite, the halon suppression system would be compromised.

## Slide 20: Future Work
Test setup is underway to characterize the vent gasses from li-metal button cells.