## Slide 1: Kevlar® XF for Fire-Resistant Air Cargo Containers
Ley Richardson, Ph.D.
Principal Application Research Associate - Aerospace
DuPont Protection Technologies
International Aircraft Systems Fire Protection Working Group Meeting
21-22 October 2015
Disclaimer: This information corresponds to our current knowledge on the subject and may be subject to revision as new knowledge becomes available. It is your responsibility to investigate other sources of information on this issue that more appropriately addresses your product and its intended use. This information is not intended for use by you or others in advertising, promotion, publication or any other commercial use. DUPONT MAKES NO WARRANTIES OF ANY KIND REGARDING THIS INFORMATION AND ASSUMES NO LIABILITY WHATSOEVER IN CONNECTION WITH ANY USE OF THIS INFORMATION. This information is not a license to operate under, or intended to suggest infringement of, any existing trademarks or patents.
  The DuPont Oval Logo, The miracles of science™, and Kevlar® are registered trademarks or trademarks of E.I. du Pont de Nemours and Company or its affiliates.

## Slide 2: DuPont History in Air Cargo Systems
Blast-resistant HULD
(Kevlar®)
Ultralite® ULD
(Kevlar®)
Worked with unit load device (ULD) manufacturers over past 15+ years on application-specific developments employing Kevlar® composites
© 2015 DuPont. All rights reserved.

## Slide 3: DuPont Perspective on Fire Protection
In general, fires are unpredictable
  Intensity (temperature, duration, heat flux/energy density)
  Propagation (direction, rate)
Advocate multiple approaches and layers of protection/suppression for maximum risk mitigation
  Prevention
  Passive suppression
  Active suppression
  Combinations
Use of fire-resistant materials can reduce risks
© 2015 DuPont. All rights reserved.

## Slide 4: Flammability of Materials Employed in Cargo Containers
Existing commercial composite ULDs frequently employ polypropylene (PP) or polyethylene (PE) resins or fibers
Upon burning, PP and PE exhibit high heat release capacities and no char yield relative to many other polymers
DuPont has studied flammability of commercially available ULD panel materials via cargo liner test (14 CFR 25, Appendix F, Part III)
Table from DOT/FAA/AR-04/11 Technical Report by Zhang
© 2015 DuPont. All rights reserved.

## Slide 5
14 CFR 25 Appendix F Part III Fire Test

## Slide 6: Commercial Polypropylene / Glass ULD Panels
The three different commercially available PP / glass ULD panel types tested failed 14 CFR 25 Appendix F Part III fire test

## Slide 7
14 CFR 25 Appendix F Part III Fire Test

## Slide 8: Kevlar XF vs. Aluminum in 14 CFR 25 App F Part III Test
Material: Aluminum

## Slide 9: Kevlar® XF Fire Resistance After Simulated In-Service Abuse
14 CFR 25 App F Part III fire testing following mechanical testing and 24 hr water immersion
No flame
penetration
No flame
penetration

## Slide 10: Kevlar® XF Fire Resistance After Simulated In-Service Abuse
14 CFR 25 App F Part III fire testing following mechanical testing and 24 hr water immersion
No flame
penetration
Additional 14 CFR 25 App F Part III fire testing of sidewall-ceiling combinations of Kevlar® XF panels simulating fire in a ULD corner concluded at 15 min. without flame penetration.

## Slide 11: Summary
Kevlar® XF is a new DuPont panel material for ULDs that:
Meets technical requirements in the current SAE/ISO draft standard for Fire-Resistant Containers (FRCs), including 14 CFR 25 Appendix F Part III flame penetration requirements
Maintains Part III-compliant fire resistance following simulated in service abuse
Is lightweight compared to other commercially available ULD panels
Additional Data Available from DuPont:
Smoke Emission
Toxic Gas Emission
Heat Release Rate (OSU)
Fungus Resistance
UV and Humidity Exposure
Puncture Resistance
Abrasion Resistance
Residual Strength After Part III Fire Test Exposure
© 2015 DuPont. All rights reserved.

## Slide 12
ley.richardson@usa.dupont.com