## Slide 1: UN Battery Classification Test Method Development

## Slide 2: Introduction
Currently all lithium batteries are classified for shipping as either lithium-ion or lithium metal
All lithium-ion or lithium metal batteries are not created equal
New classifications reflect actual hazards:
  Propagation
  Fire
  Gas Hazard
  Temperature Hazard

## Slide 3: Lithium Battery Classification
By Default, no testing will be required, all hazards would be considered worst case with common chemistry
Purpose of this testing is to determine worst case as well as developing test methods for individual batteries to be classified on their own
  Gas Volume Test (all gas emitted is assumed to be toxic)
  Propagation Test
  Flammability and temperature hazard determined in one of these tests
If a battery shipper/seller can prove their battery is inherently safer, then they may be able to ship with fewer restrictions

## Slide 4: Battery Gas Volume Measurements
Single cell placed in 21.7L pressure vessel and heated until thermal runaway
Instrumented with pressure transducers and thermocouples for heater, battery, and ambient air
Chamber is evacuated with vacuum pump, then filled with nitrogen at atmospheric pressure
Battery gas volume is calculated from temperature and pressure measurements
All cells at 100% SOC

## Slide 5: Battery Gas Volume Measurements
Heating rate controlled with temperature controller
Cells heated at rates of 5°C, 10°C, and 20°C per minute
Example shows an 18650 cell heated at 20°C/min

## Slide 6: Battery Gas Volume Measurements
Chamber pressure and temperature data from same test
Calculated amount of gas (in moles) using ideal gas law
Converted to liters of gas at NIST normal temperature and pressure (NTP: 20°C and 1 atm)
This test produced 3.39L of gas
Initial pressure and temperature
Final pressure and temperature

## Slide 7: Battery Gas Volume Measurements
Tested 26 lithium-ion cells
  Size from AAA to large pouches
  LCO, NMC, LFP, LTO, LMN chemistries
Tested 11 lithium metal cells
  Button cells up to 17500
  LiFeS2, LiMnO2, LiSOCl2, LiSO2 chemistries
Lithium-ion batteries tested
Lithium metal batteries tested

## Slide 8: Battery Gas Volume Measurements

## Slide 9: Battery Gas Volume Measurements
Highest was LTO 18650 at 0.71 L/Wh
Highest LCO was 10,000 mAh pouch cell at 0.59 L/Wh
Highest LFP was AA at 0.32 L/Wh

## Slide 10: Battery Gas Volume Measurements

## Slide 11: Battery Gas Volume Measurements
Highest was LiMnO2 CR123A at 0.58L/Wh
Need larger sample size of other cells

## Slide 12: Battery Propagation Testing
6 cells placed in a line in an insulated box to determine if thermal runaway will propagate down the line
Cell #1 heated at 20°C/min until thermal runaway occurs, then heater is turned off
Thermocouple placed on each cell to measure temperature
Top of box is vented to allow gas to escape
Spark ignitor placed 3 inches above the box
  To determine if gas is flammable
  Ignitor turned off after first cell goes into thermal runaway
All cells at 100% SOC
Tested 20 Li-ions and 16 Li metals so far

## Slide 13
Notes: Video starts 12:15 after start of test

## Slide 14: Battery Propagation Testing
All LCO cells propagated except AAA size
No LFP cells fully propagated
All cells produced flammable gas

## Slide 15: Battery Propagation Testing
LiFeS2 propagated at AA size for one brand, not AAA
All cells produced flammable gas except LiSO2
Small CR2430 button cell propagated (0.855 Wh)

## Slide 16: Speed of Propagation
Calculated from the diameter (or length) of the cell and the time it takes to propagate from cell 1 to cell 6
Diameter

## Slide 17: Speed of Propagation
Cylindrical cells increased as size and energy capacity increased
Pouch cells stayed relatively constant regardless of size

## Slide 18: Speed of Propagation
LiMnO2 cells propagation speed seemed to increase with size as well, but all these cells tested were very small
Need to test larger cells to confirm

## Slide 19: Speed of Propagation
Tested LiMnO2 9V batteries in two orientations
9V batteries are 26mm x 16mm
Took 695s to propagate in 16mm direction and 658s in 26mm direction
Speed increased from 6.91 mm/min to 11.85 mm/min
16mm
26mm

## Slide 20: Conclusion and Future Work
Battery gas volume increases with battery capacity in lithium-ion and lithium metal cells
  Different chemistries produce different L/Wh measurements
Battery propagation test works well for testing propagation and flammability
  Ignitor placed above cell #1 always ignited flammable gases
  Cells must be secured in box
Propagation speed increased with cell capacity in cylindrical cells
Future work is to simplify decision tree and conduct any further testing necessary to support the changes

## Slide 21: Questions?
Contact:
Steven Rehn
Federal Aviation Administration
William J. Hughes Technical Center
Fire Safety Branch, Bldg. 203
Atlantic City Int’l Airport, NJ 08405
(609) 485-5587
steven.rehn@faa.gov