## Slide 1: Cargo Heat Release Rate Testing
Joseph Panagiotou
Office of Research & Engineering
Materials Laboratory

## Slide 2: Recent Fires in Freighter Aircraft
UPS, flight 1307, DC-8
  February 7th 2006 in Philadelphia, PA
  In-flight fire with emergency landing
  Total hull loss
  Undetermined ignition source
UPS, flight 006, B747-400F (ongoing)
  September 4th 2010 in Dubai, UAE
  In-flight fire with crash landing (total hull loss)
Asiana Cargo, flight 991, B747-400F (ongoing)
  July 28th 2011 west of Jeju island, South Korea
  In-flight fire with crash landing (total hull loss)

## Slide 3: Issues That Keep Coming Up
Lithium & lithium-ion batteries in the cargo
  Fire hazard posed by batteries?
Fire detection & suppression
Fire containment
Fire resistance of cargo liners
  Characteristics of cargo container fires?

## Slide 4: Fire Hazard Potential of Batteries
Ignition Hazard
Explosion/overpressure
Incendiary particles / fire spread
Energy release rate / total energy
Hazardous products of combustion
Propagation in low oxygen environment

## Slide 5: Cargo Container Fire Characteristics
Detectability of the fire
Container effects (depends on type)
Size of the fire at detection and growth rate
Energy release rate and total energy
Container material flammability
Cargo flammability

## Slide 6: Topics Addressed
Fire load contribution of lithium and lithium-ion batteries
  Small scale tests using single battery cells
    Cone calorimeter (FAATC)
    Li-ion, Li, Li-PO batteries tested
  Small scale tests using single boxes of batteries (100ct.)
    Medium scale oxygen consumption calorimeter hood (BATFE)
    Li-ion batteries tested
Burning characteristics of cargo container fires
  Large scale tests using main cargo deck type containers
    Large scale oxygen consumption calorimeter hood (BATFE)
    Rigid A2N (Aluminum/Lexan) construction
    Collapsible DMZ (FR PP) construction
    Fire load composed of 77 18” cube cardboard boxes with 2.5lb shredded paper inside

## Slide 7: Small Scale Battery Tests
Box of 100 Li-ion batteries subjected to propane burner fire
Batteries suspended above burner
Steady burner output of 30kW
Heat flux gauges
Thermocouples
Oxygen consumption calorimetry
Box of batteries

## Slide 8: Small Scale Battery Tests (video)

## Slide 9: Small Scale Battery Tests
Chart: Box of 100 Li-ion Batteries Suspended Over 30kW Burner
Burner output
Δ(HRR)

## Slide 10: Small Scale Battery Tests
Peak Δ(HRR) ~ 90kW above burner output of 30kW
Energy contribution from 100 batteries ~ 11237 kJ
  112 kJ per battery cell (88 kJ from cone calorimeter testing at FAATC)
Burning time 320 seconds
Maximum temperature excursion 12” above box ~ 250°C
Maximum heat flux excursion 22” from edge of box ~ 3 kW/m2

## Slide 11: Small Scale Battery Tests
Chart: Energy Release Rate Comparison

## Slide 12: Small Scale Battery Tests
Thermal runaway ignition tests
3 x 3 x 2 array of cardboard boxes (18 boxes)
18” cube boxes with 2.5lb shredded paper
1 box of 100 Li-ion batteries
250W cartridge heater
Heat release rate
Total energy
Radiant heat flux
Plume temperature
Battery initiated fire scenario
Battery contribution

## Slide 13: Small Scale Battery Tests

## Slide 14: Small Scale Battery Tests

## Slide 15: Small Scale Battery Tests
Chart: Cardboard Boxes VS Cardboard Boxes and Batteries
288 MJ
298 MJ

## Slide 16: Small Scale Battery Tests
Battery failure spread fire to surrounding combustibles
Fire load contribution from batteries was minor
Batteries continued to burn after main fire load was consumed

## Slide 17: Large Scale Container Fires
Rigid A2N type container
Aluminum / Lexan
77 boxes with shredded paper
Electronic ignition of floor level corner box
Energy release rate
Heat flux
Plume temperature
Smoke emission and detection time

## Slide 18: Large Scale Container Fire (video)

## Slide 19: Large Scale Container Fire

## Slide 20: Large Scale Container Test
Chart: Rigid Cargo Container Test #1 (A2N Al/Lexan)
(04:38) Wisps of smoke coming out of container door
(10:14) Flame outside container at corner where ignition started
(05:13) Flame visible inside container
(07:05) Estimated time when smoke exiting container would be at a detectable level
(09:20) Lexan starting to melt
(14:36) Peak heat release rate 3.6MW
7.5 minutes

## Slide 21: Large Scale Container Tests
Collapsible DMZ type container
FR Polypropylene
77 boxes with shredded paper
Electronic ignition of floor level corner box
IR camera
Energy release rate
Heat flux
Plume temperature
Smoke emission and detection time

## Slide 22: Large Scale Container Test (video)

## Slide 23: Large Scale Container Test

## Slide 24: Large Scale Container Tests
Chart: Collapsible Cargo Container Test #1 (DMZ FRPP)
(11:00) Wisps of smoke coming out of the bottom of the container at the opposite side from the ignition box
(12:50) Wisps of smoke coming out of the top of the container
(19:39) Flames visible underneath rain fly
(20:46) Flames inside container visible on IR cam
(21:30) Estimated time when smoke exiting container would be at a detectable level
(22:00) Flames outside of container
(03:00) Smoke inside container (IR cam)
2.2 minutes
(23:44) Peak heat release rate 8.45MW

## Slide 25: Large Scale Container Tests
Chart: Cargo Container Fire Tests

## Slide 26: Container Fire Test Observations
Rigid A2N
  Peak HRR 3.6MW & 3.7MW
  Time between detectable smoke emission and peak HRR 7.5 minutes &10.5 minutes
  Smoke exits through unintentional paths
Collapsible DMZ
  Peak HRR 8.45MW & 7.1MW
  Time between detectable smoke emission and peak HRR 2.2 minutes & 1.9 minutes
  Construction materials add to fire load
  Operations/procedures may inadvertently slow detection (rain fly)

## Slide 27: Thank you!
This test program was accomplished thanks to the support from the FAA UPS and ATF.